SECTION 09 91 00.10

COMMERCIAL AND LIGHT COMMERCIAL/RESIDENTIAL PAINTING

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2021 -  2024 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Commercial painting, including surface preparation, for projects in the United States.
1.	Interior commercial painting.
2.	Interior high-performance commercial painting.
3.	Exterior commercial painting.
B.	Light commercial/residential painting, including surface preparation, for projects in the United States.
1.	Interior light commercial/residential painting.
2.	Exterior light commercial/residential painting.
C.	Commercial painting, including surface preparation, for projects in Canada.
1.	Interior commercial painting.
2.	Interior high-performance commercial painting.
3.	Exterior commercial painting.
D.	Light commercial/residential painting, including surface preparation, for projects in Canada. 
1.	Interior light commercial/residential painting. 
2.	Exterior light commercial/residential painting.
1.2	RELATED SECTIONS - INTERIOR 
A.	Division 3 - Concrete - Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place including Plaster (Walls, Ceilings, Concrete - (Floors, non-vehicular).
B.	Division 4 - Interior Concrete Block.
C.	Division 5 - Metal - Galvanized.
D.	Division 6 - Wood - Doors, Trim, Paneling.
E.	Division 9 - Drywall - (Walls, Ceilings, Gypsum Board and similar items).
1.3	RELATED SECTIONS - EXTERIOR
A.	Division 3 - Concrete - Cementitious Siding, Flexboard, Transite Board, Shingles (Non-Roof), Common Brick, Stucco, Tilt-up, Precast, and Poured-in-place Cement.
B.	Division 4 - Concrete Block, Floors (Non-Vehicular).
C.	Division 5 - Metal - Galvanized, Miscellaneous Iron, Ornamental Iron, Structural Iron and Steel, Ferrous Metal.
D.	Division 6 - Wood - Decks, Exterior including pressure treated lumber, Floors (non-Vehicular).
E.	Division 7 - Wood - Siding, Trim, Shutters, Sashes, Hardboard-Bare/Primed, Architectural PVC, Plastic, Fiberglass, Azek, Vinyl Siding, EIFS, Synthetic Stucco.
1.4	REFERENCES
A.	American National Standards Institute (ANSI) - Performance Standards.
B.	Asthma and Allergy Foundation of America and Allergy Standards, Ltd. 
1.	The Certified Asthma and Allergy Friendly Mark. A registered certification mark. 
C.	American Society for Testing Materials (ASTM) - Testing Methods.
D.	Cradle to Cradle Products Innovation Institute. 
1.	Cradle to Cradle Certification. 
E.	Environmental Protection Agency; Electronic Code of Federal Regulations (CFR): 
1.	40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings; U.S. Environmental Protection Agency; current edition. 
F.	Green Seal Standards (GS-11): 
1.	GS-11; May 20, 1993. 
G.	Master Paint Institute (MPI #) - Established paint categories and standards.
H.	National Paint and Coatings Association (NPCA) - Gloss Standard. 
I.	Occupational Safety and Health Act (OSHA) - Safety Standards.
J.	Ozone Transmission Commission (OTC) - Established levels of Volatile Organic Compounds.
K.	Paint Decorating Contractors of America (PDCA) - Application Standard.
L.	Society of Protective Coatings (SSPC):
1.	SSPC (PM1) - Steel Structures Painting Manual, Vol. 1, Good Painting Practice; 1993, Third Edition.
2.	SSPC (PM2) - Steel Structures Painting Manual, Vol. 2, Systems and Specifications; 1995, Seventh Edition.
M.	South Coast Air Quality Management District (SCAQMD):  
1.	SCAQMD Rule #1168; October 3, 2003. 
N.	US Green Building Council, (USGBC) - Green Seal standards for LEED paint credits. 
1.5	DEFINITIONS
A.	Commercial as used in this Section refers to a product well suited for a commercial application.
B.	DFT as used in this Section refers to the Dry Film Thickness of the coating.
C.	Enamel refers to any acrylic or alkyd (oil) base paint which dries leaving an eggshell, pearl, satin, semi-gloss or high gloss enamel finish.
D.	DTM as used in this Section refers to paint that is applied Direct To Metal.
E.	LEED as used in this Section refers to Leadership in Energy and Environmental Design. Products listed meet LEED criteria for environmentally safe interior primers, paints and coatings.
F.	OTC as used in this Section refers to the Ozone Transmission Commission. OTC has established the following VOC levels for the Northeastern United States. Products shall meet the following OTC limits for VOC's.
1.	Interior flat paints: 100 grams per liter or less, per gallon.
2.	Interior enamels: 150 grams per liter or less, per gallon.
3.	Interior stains: 250 grams per liter or less, per gallon.
4.	Interior primers: 200 grams per liter or less, per gallon.
5.	Rust preventive coatings: 400 grams per liter or less, per gallon.
6.	Dry fog coatings: 400 grams per liter or less, per gallon.
7.	Floor coatings: 250 grams per liter or less, per gallon.
G.	Premium as used in this Section refers to the best quality product "top of the line".
H.	VOC as used in this Section refers to Volatile Organic Compounds found in primers, paints, sealers and stains. The level of VOCs appears after each product listed in the Schedule in grams per liter (g/L).
I.	Paints are available in a wide range of sheens or glosses, as measured by a gloss meter from a 60 and/or 85 degree angle from vertical, as a percentage of the amount of light that is reflected. The following terms are used to describe the gloss of our products. The list below is provided for general guidance; refer to the technical data sheet for the actual gloss/sheen level for each product.
1.	Flat - Less than 5 Percent.
2.	Eggshell - 5 - 20 Percent.
3.	Satin - 20 - 35 Percent.
4.	Semi-Gloss - 30 - 65 Percent.
5.	Gloss - Over 65 Percent.
1.6	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	LEED Certification Product Data:
1.	See Section 01 00 00 - General Requirements.
2.	Submittals Required:
a.	MRc3 Resource Reuse (LEED Form).
b.	MRc4 Recycled Content (LEED Form).
c.	MRc5 Local and Regional Materials (LEED Form).
d.	EQc4.2 Low Emitting Materials - Paint (VOC Certification Letter).
C.	Product Data: Provide a complete list of all products to be used, with the following information for each:
1.	Manufacturer's name, product name and/or catalog number, and general product category.
2.	Cross-reference to specified paint system(s) that the product is to be used in; include description of each system.
D.	Samples: Submit three paper samples, 5 inches by 7 inches (127mm x 178mm) in size, illustrating selected colors for each color and system selected with specified coats cascaded.
E.	Manufacturer's Instructions: Indicate special surface preparation procedures.
F.	Maintenance Data: Submit data on cleaning, touch-up, and repair of painted and coated surfaces.
1.7	QUALITY ASSURANCE
A.	Manufacturer Qualifications: All primary products specified in this section will be supplied by a single manufacturer with a minimum of ten years experience.
B.	Installer Qualifications: All products listed in this section are to be applied by a Painting Contractor with a minimum of five years demonstrated experience in surface preparation and field application of the same type and scope as specified.
C.	Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.	Mock-up areas designated by Architect.
2.	Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
3.	Approved mock-up areas will serve as the standard for remaining Work.
4.	Refinish mock-up area as required to produce acceptable Work.
1.8	DELIVERY, STORAGE, AND HANDLING
A.	Store products in manufacturer's unopened packaging until ready for installation.
B.	Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.
C.	Disposal:
1.	Never pour leftover coating down any sink or drain. Use up material on the job or seal can and store safely for future use.
2.	Do not incinerate closed containers.
3.	For specific disposal or recycle guidelines, contact the local waste management agency or district. Recycle whenever possible.
1.9	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.10	WARRANTY
A.	Inspection of all surfaces to be coated must be done by the manufacturer's representative to insure proper preparation prior to application. All thinners, fillers, primers and finish coatings shall be from the same manufacturer to support a product warranty. Products other than those submitted shall be accompanied by a letter stating its fitness for use and compatibility.
B.	At project closeout, provide to the Owner or owner's representative an executed copy of the Manufacturer's standard form outlining the terms and conditions of and any exclusions to their Limited Warranty against Manufacturing Defect.
1.11	EXTRA MATERIALS
A.	At project closeout, supply the Owner or owner's representative one gallon of each product for touch-up purposes. Cans shall be clearly marked with color name, number and type of paint.
B.	At project closeout, provide the color mixture name and code to the Owner or owner's representative for accurate future color matching.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: Benjamin Moore & Co. (United States), which is located at:<BR />101 Paragon Dr<BR />Montvale, NJ 07645<BR />Toll Free Tel: 866-708-9181<BR />Email: request info (info@benjaminmoore.com);Web: https://www.benjaminmoore.com | https://www.benjaminmoore.com/en-ca 
B.	Substitutions: Coronado Paint Company.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	LEED CRITERIA
A.	LEED Version 3 - 2009: EQ CR4.2 Low Emitting Materials: 1 Credit - Paint.
1.	All architectural paints and coatings used must meet the VOC limits of Green Seal Standard GS-11, 1993.
2.	Interior: 50 g/l VOC or less for Flats, 150 g/l VOC for Non Flats, and 200 g/l or less for primer sealers.
3.	Anti-Corrosive Coatings GC-03, 1997: Interior 250 g/l VOC or less any sheen.
4.	Clear wood finishes, floor coatings, stains, and shellacs applied to interior elements: District (SCAQMD) Rule 1113, Architectural Coatings, rules in effect on January 1, 2004.
5.	Clear wood finishes: varnish 350 g/L; lacquer 550 g/L; Floor coatings; 100 g/L, waterproofing sealers 250 g/L; sanding sealers 275 g/L; Shellacs: Clear 730 g/L; pigmented 550 g/L; Stains: 250 g/L.
B.	LEED Version 4:
1.	All interior paints and coatings wet-applied on site must meet the applicable VOC limits of the California Air Resources Board (CARB) 2007, Suggested Control Measure (SCM) for Architectural Coatings, or the South Coast Air Quality Management District (SCAQMD) Rule 1113, effective June 3, 2011 (50g/l or less for interior flats, 100 g/l or less for non-flats, 150 g/l or less for non-flats high gloss).
2.	Ninety percent of all interior paints and coatings must be tested and determined compliant in accordance with California Department of Public Health (CDPH) Standard Method v1.1-2010.
2.3	MATERIALS - GENERAL
A.	Volatile Organic Compound (VOC) Content:
1.	Provide coatings that comply with the most stringent requirements specified in the following:
a.	40 CFR 59, Subpart D-National Volatile Organic Compound Emission Standards for Architectural Coatings.
b.	Determination of VOC Content: Testing and calculation in accordance with 40 CFR 59, Subpart D (EPA Method 24), exclusive of colorants added to a tint base and water added at project site; or other method acceptable to authorities having jurisdiction.
1)	All references to (0 g/L) are Zero VOCs according to EPA Method 24. 
B.	Compatibility: Provide materials that are compatible with one another and the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.
2.4	MIXING AND TINTING
A.	Except where specifically noted in this section, all paint shall be ready-mixed and pre-tinted. Agitate all paint prior to and during application to ensure uniform color, gloss, and consistency.
B.	Thinner addition shall not exceed manufacturer's printed recommendations. Do not use kerosene or other organic solvents to thin water-based paints.
C.	Where paint is to be sprayed, thin according to manufacturer's current guidelines.
2.5	COMMERCIAL INTERIOR PAINT SYSTEMS - UNITED STATES
A.	CONCRETE - (Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place) including PLASTER - (Walls, Ceilings).
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
d.	Semi-Gloss Finish High Performance
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
e.	Eggshell/ Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
f.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
g.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System:
a.	Gloss Finish (Water Base)
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech 100% Solid Epoxy Pre-Primer V155 (6 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
b.	Gloss Finish
1)	First Coat: Corotech 100% Solid Epoxy Pre-Primer V155 (6 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell Finish
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
B.	CONCRETE: Ceilings.
1.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
c.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Dryfall Latex Flat 395 (46 g/L), MPI # 118.
2)	Second Coat: Benjamin Moore Dryfall Latex Flat 395 (46 g/L), MPI # 118.
C.	MASONRY: CMU - Concrete, Split Face, Scored, Smooth, High Density, Low Density, Fluted.
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L) MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
d.	Eggshell / Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
e.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell/Satin Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
d.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
e.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
D.	METAL: Aluminum, Galvanized.
1.	Latex Systems:
a.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, X-Green 141, LEED 2009, LEED V4.
b.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Satin Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
d.	Semi-Gloss High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
e.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
f.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
g.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System:
a.	Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
d.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
E.	METAL: Galvanized; Ceilings, Duct work.
1.	Multi-Surface Acrylic Coating System:
a.	Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
2.	Dryfall Waterborne Topcoats:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
c.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
F.	METAL - (Structural Steel Columns, Joists, Trusses, Beams, Miscellaneous and Ornamental Iron, Structural Iron, Ferrous Metal)
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
c.	Semi-Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
e.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System:
a.	Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Alkyd Metal Primer P06 (323 g/L), MPI # 79.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Alkyd Metal Primer P06 (323 g/L), MPI # 79.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Eggshell Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
4.	Urethane System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
5.	Dryfall Waterborne Topcoats:
a.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
G.	WOOD - (Walls, Ceilings, Doors, Trim):
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi - Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
c.	Eggshell / Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Waterborne Satin Impervo N314 (137 g/L), MPI # 43, LEED Credit.
3)	Third Coat: Benjamin Moore Waterborne Satin Impervo N314 (137 g/L), MPI # 43, LEED Credit.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System:
a.	Gloss Finish (Water base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish (Water Base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell Finish (Water Base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Stain and Varnish System:
a.	Gloss Finish:
1)	First Coat: Lenmar Waterborne Interior Wiping Stain 1WB.1300 (240 g/L), MPI # 186 LEED Credit.
2)	Second Coat: Lenmar Waterborne Aqua-Plastic Urethane Gloss 1WB.1400 (322 g/L), MPI # 121, 130.
3)	Third Coat: Lenmar Waterborne Aqua-Plastic Urethane Gloss 1WB.1400 (322 g/L), MPI # 121, 130.
b.	Satin Finish:
1)	First Coat: Lenmar Waterborne Interior Wiping Stain 1WB.1300 (240 g/L), MPI # 186 LEED Credit.
2)	Second Coat: Lenmar Waterborne Aqua-Plastic Urethane Satin, 1WB.1427 (335 g/L), MPI # 121, 128.
3)	Third Coat: Lenmar Waterborne Aqua-Plastic Urethane Satin, 1WB.1427 (335 g/L), MPI # 121, 128.
H.	DRYWALL - (Walls, Ceilings, Gypsum Board and similar items)
1.	Latex Systems:
a.	Satin Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified
b.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer N372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Semi-Gloss N376 (0 g/L) MPI # 54, X-Green 54, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Eco Spec WB Semi-Gloss N376 (0 g/L) MPI # 54, X-Green 54, LEED V4, CHPS Certified.
c.	Eggshell / Satin System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009 LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
d.	Eggshell / Satin System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer N372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Eggshell N374 (0 g/L), MPI # 52, X-Green 52, 139, X-Green 139, X- Green 145, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Eco Spec WB Eggshell N374 (0 g/L), MPI # 52, X-Green 52, 139, X-Green 139, X-Green 145, LEED V4, CHPS Certified.
e.	Low Sheen System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat System
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
g.	Flat System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer N372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Flat N373 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED V4.
3)	Third Coat: Benjamin Moore Eco Spec WB Flat N373 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED V4.
2.	Epoxy System (Water Base):
a.	Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell/Low Luster System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
I.	Concrete - (Floors, non-vehicular):
1.	Latex Systems:
a.	Semi-Gloss System:
1)	First Coat: Insl-X Tough Shield Floor and Patio TS-3 (167 g/L).
2)	Second Coat: Insl-X Tough Shield Floor and Patio TS-3 (167 g/L).
b.	Satin System:
1)	First Coat: Insl-X Tough Shield Floor and Patio TS-3 (167 g/L).
2)	Second Coat: Insl-X Tough Shield Floor and Patio TS-3 (167 g/L).
2.6	COMMERCIAL HIGH PERFORMANCE INTERIOR PAINT SYSTEMS - UNITED STATES
A.	CONCRETE - Smooth (Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Eggshell/Low Sheen:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2.	Alkyd System (Water Base):
a.	Gloss Finish (Water base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss N794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
4.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss/High Luster Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Eggshell/Low Luster Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy Systems (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
3)	Third Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
6.	Urethane System (Water Base):
a.	Gloss Finish Single Component:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
B.	CONCRETE - (Ceilings).
1.	MultiSurface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
2)	Second Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
2.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
C.	MASONRY - (CMU - Concrete, Split Face, Scored, Smooth, High Density, Low Density, Fluted, Stucco).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Low Sheen:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Flat Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3)	Third Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Alkyd System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3)	Third Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3.	Alkyd System (Solvent Base Finish):
a.	Urethane Modified:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
4.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
c.	Semi-Gloss/High Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
d.	Semi-Gloss/High Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
e.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy Systems (Solvent Base Finish):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
3)	Third Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
6.	Urethane Systems (Water Base).
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
7.	Urethane Systems (Solvent Base Finish):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss DFT (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss DFT (305 g/L), MPI # 83, 174.
D.	Non-Ferrous- (Galvanized and Aluminum):
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
d.	Low Sheen:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
e.	Flat Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Alkyd System (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3)	Third Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
3)	Third Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
4.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
e.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy Systems (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
6.	Urethane Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
7.	Urethane Systems (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L) MPI # 83, 174.
8.	Multi-Surface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
2)	Second Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
9.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Benjamin Moore Dryfall Latex Flat 395 (46 g/L), MPI # 118.
2)	Second Coat: Benjamin Moore Dryfall Latex Flat 395 (46 g/L), MPI # 118.
10.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
E.	METAL - (Structural Steel Columns, Joists, Trusses, Beams, Miscellaneous and Ornamental Iron, Structural Iron, Ferrous Metal).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
d.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
e.	Low Sheen:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
f.	Flat Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Alkyd System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3)	Third Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
b.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer P04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
3)	Third Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
4.	Epoxy Systems (Water Base):
a.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit..
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009
5.	Epoxy System (Solvent Base):
a.	Semi-Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy Primer V150 (330 g/L).
2)	Second Coat Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
6.	Urethane System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
7.	Urethane System (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy Primer V150 (330 g/L).
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy Primer V150 (330 g/L).
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
F.	METAL - (Ceilings - Structural Steel, Joists, Trusses, Beams).
1.	MultiSurface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic 80 Line (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
c.	Eggshell Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
d.	Flat Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
G.	WOOD - (Doors, Trim, Partitions, Frames).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
c.	Low Sheen/Satin:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Alkyd System (Water Based):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3)	Third Coat: Corotech Water Reducible Alkyd Enamel V210 (331 g/L), MPI # 157.
3.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
4.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy System (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
H.	DRYWALL - (Walls, Ceilings, Gypsum Board)
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss N540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss N539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Low Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell N538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat N536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
c.	Eggshell Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
I.	PLASTER - (Walls, Ceilings)
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009. .
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
c.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2.7	COMMERCIAL EXTERIOR PAINT SYSTEMS - UNITED STATES
A.	CONCRETE (Cementitious Siding, Flexboard, Transite Board, Shingles (Non-Roof), Common Brick, Stucco, Tilt-up, Precast, and Poured-in-place Cement).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
c.	Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
e.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben Waterborne Exterior Flat 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Waterborne Exterior Flat 541 (44 g/L), MPI # 10.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
g.	High Build Coating:
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2.	Elastomeric System: Not including cementitious siding, Flexboard, Transite board or shingles (non-roof).
a.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Interior/Exterior Acrylic High Build Masonry Primer N068 (97g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3)	Third Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3.	Textured and Smooth Systems:
a.	Textured (Water Based Finish):
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth 3194 (90 g/L), LEED Credit.
2)	Second Coat:
a)	Finish Texture- Fine: Coronado Texcrete WB Acrylic Masonry Waterproofer Sand Finish 3192 (78 g/L), LEED Credit.
b)	Finish Texture- Smooth: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 Line (90 g/L), LEED Credit.
c)	Finish Texture- Medium: Coronado Texcrete WB Acrylic Masonry Waterproofer Medium Finish 3196 Line (20 g/L), MPI # 42, LEED Credit.
b.	Smooth (Water Based Finish):
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2)	Second Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
4.	Stain System:
a.	Solid Color Waterborne Finish:
1)	First Coat: Coronado TuffCrete Waterborne Acrylic Concrete Stain CST-2000 (153 g/L), MPI # 58.
2)	Second Coat: Coronado TuffCrete Waterborne Acrylic Concrete Stain CST-2000 (153 g/L), MPI # 58.
B.	MASONRY: Concrete Masonry Units (CMU) - Cinder or Concrete Block.
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Coronado Cryli Cote 100% Acrylic Gloss House & Trim Paint 2 (94 g/L).
3)	Third Coat: Coronado Cryli Cote 100% Acrylic Gloss House & Trim Paint 2 (94 g/L).
b.	Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
c.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
d.	Satin Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Coronado Cryli Cote 100% Acrylic Satin House & Trim Paint 410 (83 g/L).
3)	Third Coat: Coronado Cryli Cote 100% Acrylic Satin House & Trim Paint 410 (83 g/L).
e.	Satin Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Coronado Cryli Cote 100% Acrylic Flat House & Trim Paint 10 (44 g/L), MPI # 10.
3)	Third Coat: Coronado Cryli Cote 100% Acrylic Flat House & Trim Paint 10 (44 g/L), MPI # 10.
g.	Flat-Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
h.	High Build Coating
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2.	Elastomeric System:
a.	Flat Finish
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler 206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3)	Third Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3.	Textured Masonry System:
a.	Textured (Water Based Finish)
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2)	Second Coat: Coronado Texcrete WB Textured Waterproofer
a)	Finish Texture Sand: 3192 (78 g/L), LEED Credit.
b)	Finish Texture Medium: 3196 (20 g/L) MPI # 42, LEED Credit.
b.	Smooth (Water Based)
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2)	Second Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
4.	Stain System:
a.	Solid Color Waterborne Stain Finish:
1)	First Coat: Insl-X TuffCrete Solvent Acrylic Concrete Stain & Waterproofing Sealer CST-5100 (651 g/L), MPI # 58, 104.
2)	Second Coat: Insl-X TuffCrete Solvent Acrylic Concrete Stain & Waterproofing Sealer CST-5100 (651 g/L), MPI # 58, 104.
5.	Clear Water Repellant:
a.	Clear Finish
1)	First Coat: Coronado Texcrete Silicone Water Repellant 194 (21 g/L), MPI # 117, LEED Credit.
2)	Second Coat: Coronado Texcrete Silicone Water Repellant 194 (21 g/L), MPI # 117, LEED Credit.
C.	CONCRETE: Concrete Floors (non-vehicular), Patios, Porches, Steps and Platforms.
1.	Acrylic System Water-Based:
a.	Floor Finish:
1)	First Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen N122 (45 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen N122 (45 g/L), LEED 2009.
D.	METAL: Aluminum, Galvanized.
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
b.	Gloss Finish- Early Moisture Resistant Finish
1)	First Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic DTM Semi-Gloss Enamel HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP Acrylic DTM Semi-Gloss Enamel HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
e.	Satin Finish- Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
g.	Flat Finish- Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
E.	METAL: Misc. Iron, Ornamental Iron, Structural Iron and Steel, Ferrous Metal.
1.	Latex Systems:
a.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
b.	Semi-Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
F.	WOOD: Decks, Exterior including pressure treated lumber, Floors (non-Vehicular), Platforms.
1.	Acrylic Water-Based Floor System:
a.	Floor Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen N122 (45 g/L), LEED 2009.
2.	Stain Systems:
a.	Solid Color Acrylic Latex:
1)	First Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain 640 (93 g/L), MPI # 16.
2)	Second Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain 640 (93 g/L), MPI # 16.
b.	Semi-Transparent Stain:
1)	First Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain N638 (92 g/L), MPI # 156.
2)	Second Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain N638 (92 g/L), MPI # 156.
c.	Clear Stain:
1)	First Coat: Benjamin Moore Arborcoat Waterproofer 320 (34 g/L).
G.	WOOD: Siding, Trim, Shutters, Sashes, Hardboard-Bare/Primed.
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
b.	Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
e.	Satin Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
g.	Flat Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
2.	Stain - Water Reducible Systems:
a.	Semi-Transparent:
1)	First Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain N638 (92 g/L) MPI # 156.
2)	Second Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain N638 (92 g/L) MPI # 156.
b.	Solid Color:
1)	First Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain 640 (93 g/L) MPI # 16.
2)	Second Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain 640 (93 g/L) MPI # 16.
H.	ARCHITECTURAL PVC, PLASTIC, FIBERGLASS
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
b.	Semi-Gloss:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
c.	Satin Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
d.	Flat Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
I.	DRYWALL: Gypsum Board, Exterior Drywall.
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss 543 (45 g/L), MPI # 11.
b.	Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, HP29 (147 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore ben Exterior Low Luster 542 (45 g/l), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior Low Luster (45 g/l), MPI # 15.
e.	Satin Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre N401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore ben Waterborne Exterior Flat 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Waterborne Exterior Flat 541 (44 g/L), MPI # 10.
g.	Flat Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish N400 (42 g/L) MPI # 10.
J.	VINYL SIDING EIFS, SYNTHETIC STUCCO:
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L) MPI # 11.
b.	Gloss Finish - Vinyl Safe Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss N403 (43 g/L), MPI # 11, 311.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin N448 (46 g/L), MPI # 15.
e.	Satin Finish - Vinyl Safe Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Regal Select Exterior Revive 544 (36 g/L).
3)	Third Coat: Regal Select Exterior Revive 544 (36 g/L).
f.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
g.	Flat Finish - Vinyl Safe Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer N023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish N447 (45 g/L), MPI # 10.
2.8	LIGHT COMMERCIAL/RESIDENTIAL INTERIOR PAINT SYSTEMS - UNITED STATES
A.	CONCRETE - Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place including Plaster (Walls, Ceilings):
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Flat Acrylic Finish 24 (47 g/L), LEED 2009.
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
e.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS.
f.	Matte Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
i.	Low Sheen Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
l.	Eggshell Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
m.	Eggshell Specialty Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
n.	Eggshell  Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
o.	Eggshell Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
p.	Eggshell High Performance Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151.
q.	Satin/Pearl Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
r.	Satin/Pearl Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
s.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
t.	Satin Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/ Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
u.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
v.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
w.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
x.	Semi-Gloss Specialty Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
y.	Semi-Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
z.	Semi-Gloss High Performance Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
aa.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
ab.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L) MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 Finish (48 g/L), LEED v4, qualifies for CHPS credit.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
c.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
B.	Metal- Galvanized:
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
e.	Flat Commercial Option:
1)	First Coat: First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS.
f.	Matte Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
i.	Low Sheen Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
l.	Eggshell Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
m.	Eggshell Specialty Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
n.	Eggshell  Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
o.	Eggshell Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145 and 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145 and 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
p.	Eggshell High Performance Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151.
q.	Satin/Pearl Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
r.	Satin/ Pearl Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
s.	Satin/Pearl Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
t.	Satin Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
u.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
v.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
w.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
x.	Semi-Gloss Specialty Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
y.	Semi-Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
z.	Semi-Gloss High Performance Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
aa.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
ab.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L) MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer 790 (44 g/L), MPI # 172, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer 790 (44 g/L), MPI # 172, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED v4, qualifies for CHPS credit.
c.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer 790 (44 g/L), MPI # 172, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
C.	Wood- Doors, Trim, Paneling:
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
e.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS.
f.	Matte Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
i.	Low Sheen Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
l.	Eggshell Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
m.	Eggshell Specialty Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
n.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
o.	Eggshell Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
p.	Eggshell High Performance Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151.
q.	Satin/Pearl Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
r.	Satin/Pearl Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
s.	Satin Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish60 (<150 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
t.	Satin Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
u.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
v.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
w.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
x.	Semi-Gloss Specialty Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
y.	Semi-Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
z.	Semi-Gloss High-Performance Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L).
aa.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
ab.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
2.	Waterborne Alkyd System:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss 793 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
c.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
D.	DRYWALL - (Walls, Ceilings, Gypsum Board and similar items):
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
e.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS.
f.	Matte Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
i.	Low Sheen Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
l.	Eggshell Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
m.	Eggshell Specialty Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
n.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
o.	Eggshell Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
p.	Satin/Pearl Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
q.	Satin/Pearl Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
r.	Satin Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Satin Finish 60 (<150 g/L), LEED 2009.
s.	Satin Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
t.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
u.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
v.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Sure Seal Latex Primer Sealer 027 (48 g/L), MPI # 6, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
w.	Semi-Gloss Specialty Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (48.2 g/L), MPI # # 6, 17, 17 X-Green, 39, 137, 137 X-Green, Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
x.	Semi-Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146 and 146 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, LEED v4, qualifies for CHPS credit.
y.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer N534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
z.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin Finish 792 (48 g/L), LEED v4, qualifies for CHPS credit.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
c.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
E.	Concrete - (Floors, non-vehicular):
1.	Latex System- Self Priming:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel N122 (45 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel N122 (45 g/L), LEED 2009.
b.	Satin Better Option:
1)	First Coat: Benjamin Moore Insl-x Tough Shield Floor and Patio Coating TS-3XXX (169 g/L).
2)	Second Coat: Benjamin Moore Insl-x Tough Shield Floor and Patio Coating TS-3XXX (169 g/L).
c.	Satin Good Option:
1)	First Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L), MPI # 58.
2)	Second Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L), MPI # 58.
F.	Interior Concrete Block:
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish 547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish W625 (0 g/L), MPI # 53, 53 X-Green, LEED v4, qualifies for CHPS credit.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Acrylic Flat Finish 24 (47 g/L), LEED 2009.
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Flat Finish 473 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
e.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish N536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS.
f.	Matte Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, CHPS.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish 522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Matte Finish 548 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, LEED v4, qualifies for CHPS credit.
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish 484 (82 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
i.	Low Sheen Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, CHPS, qualifies for CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen N537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS.
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish 524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, LEED v4, qualifies for CHPS credit.
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish 549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, LEED v4, qualifies for CHPS credit.
l.	Eggshell Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish W626 (0 g/L), MPI # 44, 44 X-Green, LEED v4, qualifies for CHPS credit.
m.	Eggshell Specialty Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Eggshell Finish 474 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
n.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X interior Eggshell Finish 485 (88.4 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
o.	Eggshell Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish N538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, LEED v4, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
p.	Satin/Pearl Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish 526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
q.	Satin/Pearl Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish 550 (0g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, LEED v4, qualifies for CHPS credit.
r.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Coronado Tough Walls Satin Finish 60 (<150 g/L), LEED 2009.
3)	Third Coat: Benjamin Moore Coronado Tough Walls Satin Finish 60 (<150 g/L), LEED 2009.
s.	Satin Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (86 g/L), qualifies for LEED v4, qualifies for CHPS low emitting credit.
t.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish 528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
u.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish 551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
v.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish W627 (0 g/L), LEED v4, qualifies for CHPS credit.
w.	Semi-Gloss Specialty Option:
1)	First Coat: Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Silver Interior Latex Semi-Gloss Finish 476 (0 g/L), Qualifies for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS Low Emitting Credit.
x.	Semi-Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146 and 146 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish N539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146 and 146 X-Green, LEED v4, qualifies for CHPS credit.
y.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish N540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, LEED v4, qualifies for CHPS credit.
z.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System:
a.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin 792 (48 g/L), LEED v4, qualifies for CHPS credit.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish 793 (48 g/L), LEED v4, qualifies for CHPS credit.
c.	High-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish N794 (46 g/L), MPI # 157, 157 X-Green, LEED v4, qualifies for CHPS credit.
2.9	LIGHT COMMERCIAL/RESIDENTIAL EXTERIOR PAINT SYSTEMS - UNITED STATES
A.	CONCRETE - Cementitious Siding, Flexboard, Transite Board, Shingles (Non-Roof), Common Brick, Stucco, Tilt-up, Precast, and Poured-in-place Cement:
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
b.	Flat Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
c.	Flat Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Flat Finish 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Flat Finish 541 (44 g/L), MPI # 10.
d.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
e.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
f.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore MoorGard 100% Acrylic Low Lustre House Paint N103 (38 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore MoorGard 100% Acrylic Low Lustre House Paint N103 (38 g/L), MPI # 214.
g.	Low Lustre Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Low Lustre Finish 542 (45 g/L), MPI # 15.
h.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
i.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
j.	Satin Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
k.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
l.	Satin Commercial Option
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
m.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
n.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore MoorGlo Acrylic Soft Gloss House Paint N096 (144 g/L). 
3)	Third Coat: Benjamin Moore MoorGlo Acrylic Soft Gloss House Paint N096 (144 g/L).
o.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Soft Gloss Finish 543 (45 g/L), MPI # 11.
p.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
q.	Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
r.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
2.	Latex High-Build Options- Self Priming:
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish N400 (42 g/L), MPI # 10.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish N400 (42 g/L), MPI # 10. 
b.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish N401 (40 g/L), MPI # 15, 315. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish N401 (40 g/L), MPI # 15, 315.
c.	Soft Gloss Best Option: 
1)	First Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish N403 (43 g/L), MPI # 11. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish N403 (43 g/L), MPI # 11. 
3.	Elastomeric System- Not including Cementitious Siding, Flexboard, Transite Board or Shingles (non-roof): 
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Flat 359 (93 g/L).
3)	Third Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Flat 359 (93 g/L).
b.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer 608 (46 g/L), MPI # 3, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Low Lustre 360 (95 g/L).
3)	Third Coat: Ultra Spec Masonry Elastomeric Waterproofing Coating Low Lustre 360 (95 g/L).
B.	Concrete Block:
1.	Latex System Options:
a.	Flat Best Options:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
b.	Flat Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
c.	Flat Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
d.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
e.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
f.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
g.	Low Lustre Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
h.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
i.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
j.	Satin Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
k.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
l.	Satin Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
m.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
n.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
o.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
p.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
q.	Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
r.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), MPI # 4, 4 X-Green, LEED v4.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
C.	Concrete- Floors (Non-Vehicular):
1.	Latex System Options- Self Priming:
a.	Best Low Sheen Option:
1)	First Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel N122 (45 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel N122 (45 g/L), LEED 2009.
b.	Better Low Sheen Option:
1)	First Coat: Benjamin Moore Insl-x Tough Shield Floor and Patio Coating TS-3XXX (169 g/L).
2)	Second Coat: Benjamin Moore Insl-x Tough Shield Floor and Patio Coating TS-3XXX (169 g/L).
c.	Good Low Sheen Option:
1)	First Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L) MPI # 58.
2)	Second Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L) MPI # 58.
d.	Best High-Gloss Option:
1)	First Coat: Benjamin Moore Latex Floor & Patio High Sheen Enamel 121 (43.7 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Latex Floor & Patio High Sheen Enamel 121 (43.7 g/L), LEED 2009.
D.	Metal- Galvanized:
1.	Latex Systems:
a.	Flat Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
b.	Flat Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (45 g/L), MPI # 10.
c.	Flat Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
d.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
e.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
f.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
g.	Low Lustre Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
h.	Low Lustre Commercial Option
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
i.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
j.	Satin Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
k.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
l.	Satin Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
m.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
n.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
o.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
p.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
q.	Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
r.	Gloss Commercial Option
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
2.	Direct To Metal (Latex Options):
a.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, 153.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, 153.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss HP29 (147 g/L), MPI # 141,153.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss HP29 (147 g/L), MPI # 141,153.
c.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153.
d.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153.
2)	Second Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153.
e.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
f.	Gloss Better Option:
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154.
g.	Gloss Good Option: 
1)	First Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
2)	Second Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
E.	METAL- Misc. Iron, Ornamental Iron, Structural Iron and Steel, Ferrous Metal:
1.	Latex Options:
a.	Best Flat Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
b.	Flat Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (45 g/L), MPI # 10.
c.	Flat Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
d.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
e.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L) MPI # 15, 315.
f.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
g.	Low Lustre Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
h.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
i.	Satin Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
j.	Satin Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
k.	Satin Good Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
l.	Satin Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
m.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
n.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L). 
o.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
p.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
q.	Gloss Better Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154.
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154.
r.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), MPI # 107, 107 X-Green, 134, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
2.	Direct to Metal-Latex Options:
a.	Best Low Lustre Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, 153.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, 153.
b.	Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss HP29 (147 g/L), MPI # 141,153.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss HP29 (147 g/L), MPI # 141,153.
c.	Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153.
d.	Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153.
2)	Second Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153.
e.	Gloss Best Option:
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
f.	Gloss Better Option:
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154.
g.	Gloss Good Option: 
1)	First Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
2)	Second Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
F.	WOOD- Decks, Exterior including pressure treated lumber, Floors (non-Vehicular):
1.	Water-Based/Waterborne Alkyd Options:
a.	Best Translucent Option:
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent N623 (21 g/L), MPI # 33.
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent N623 (21 g/L), MPI # 33.
b.	Better Translucent Option:
1)	First Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain 7400 Series (180 g/L).
2)	Second Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain 7400 Series (180 g/L).
c.	Best Semi-Transparent Option:
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent 638 (92 g/L), MPI # 156.
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent 638 (92 g/L), MPI # 156.
d.	Better Semi-Transparent Option:
1)	First Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain 7600 Series (180 g/L), MPI # 156.
2)	Second Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain 7600 Series (180 g/L), MPI # 156.
e.	Best Semi-Solid Option:
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi- Solid Stain 639 (93 g/L).
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi Transparent Stain 639 (93 g/L).
f.	Best Solid Option:
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain 640 (95 g/L), MPI # 16.
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain 640 (95 g/L), MPI # 16.
g.	Better Solid Option:
1)	First Coat: Benjamin Moore Maxum Solid Color Deck Stain 8500 Series (175 g/L).
2)	Second Coat: Benjamin Moore Maxum Solid Color Deck Stain 8500 Series (175 g/L).
2.	Solvent Bases Options:
a.	Specialty Clear Option:
1)	First Coat: Benjamin Moore Arborcoat Exterior Waterproofer 320 (34 g/L).
2)	Second Coat: Benjamin Moore Arborcoat Exterior Waterproofer 320 (34 g/L).
b.	Best Translucent Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent 326 (340 g/L), MPI # 13, 33.
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent 326 (340 g/L), MPI # 13, 33.
c.	Better Translucent Option:
1)	First Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L).
2)	Second Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L).
d.	Best Semi-Transparent Option:
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Transparent C328 (229 g/L), MPI # 13, 33.
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Transparent C328 (229 g/L), MPI # 13, 33.
e.	Better Semi-Transparent Option:
1)	First Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L).
2)	Second Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L).
f.	Best Semi-Solid Option:
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid C329 (226 g/L).
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid C329 (226 g/L).
3.	Solvent Bases Options- Bleeding Woods:
a.	Best Translucent Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer 366 (345 g/L), MPI # 5.
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent 326 (340 g/L), MPI # 13, 33.
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent 326 (340 g/L), MPI # 13, 33.
b.	Better Translucent Option:
1)	First Coat: Benjamin Moore Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5,
2)	Second Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L).
3)	Third Coat: Benjamin Moore Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L).
c.	Best Semi-Transparent Option:
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer 366 (345 g/L), MPI # 5.
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Transparent C328 (229 g/L), MPI # 13, 33.
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Transparent C328 (229 g/L), MPI # 13, 33.
d.	Better Semi-Transparent Option:
1)	First Coat: Benjamin Moore Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5,
2)	Second Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L).
3)	Third Coat: Benjamin Moore Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L).
e.	Best Semi-Solid Options:
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer 366 (345 g/L), MPI # 5.
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid C329 (226 g/L).
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid C329 (226 g/L).
G.	WOOD- Siding, Trim, Shutters, Sashes, Hardboard-Bare/Primed:
1.	Latex System Options:
a.	Best Ultra Flat/Solid Stain Option:
1)	First Coat: Benjamin Moore Arborcoat Waterborne Ultra Flat Solid Stain 610 (72.2 g/L), MPI # 16.
2)	Second Option: Benjamin Moore Arborcoat Waterborne Ultra Flat Solid Stain 610 (72.2 g/L), MPI # 16.
b.	Better Ultra Flat/Solid Stain Option:
1)	First Coat: Benjamin Moore Maxum Solid Color Siding Stain B2000 Series (144 g/L), MPI # 16.
2)	Second Coat: Benjamin Moore Maxum Solid Color Siding Stain B2000 Series (144 g/L), MPI # 16.
c.	Best Flat Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
d.	Better Flat Option:
1)	First Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
e.	Good Flat Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10
f.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
g.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
h.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
i.	Low Lustre Good Option:
1)	First Coat: First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, CHPS.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
j.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
k.	Satin Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
l.	Satin Better Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
m.	Satin Good Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
n.	Satin Commercial Option
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
o.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
p.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
q.	Soft Gloss/ Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
r.	Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309, 48 g/L.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309, 48 g/L.
s.	Gloss Better Option:
1)	First Coat: Benjamin Moore Coronado Super Kote 5000 Interior Acrylic Latex Primer Sealer 40 Line (46 g/L), MPI #50, CHPS.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
t.	Gloss Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
H.	Architectural PVC, Plastic, Fiberglass, Azek:
1.	Latex Options:
a.	Best Flat Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
b.	Better Flat Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
c.	Good Flat Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10
d.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
e.	Low Lustre Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
3)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
f.	Low Lustre Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
g.	Low Lustre Good Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
h.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
i.	Satin Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
j.	Satin Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
k.	Satin Good Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
l.	Satin Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
m.	Soft Gloss/ Semi-Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L). 
n.	Soft Gloss/ Semi-Gloss Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
o.	Soft Gloss/ Semi-Gloss Good Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
p.	Gloss Best Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L).
q.	Gloss Better Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. (Direct To Metal) Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. (Direct To Metal) Acrylic Gloss Enamel HP28 (142 g/L), MPI # 114, 154, 164.
r.	Gloss Good Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
s.	Gloss Commercial Option
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
I.	Vinyl Siding, EIFS, Synthetic Stucco:
1.	Latex Options:
a.	Best Vinyl Siding EIFS Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior REVIVE 544 (36 g/L).
3)	Third Coat: Benjamin Moore Regal Select Exterior REVIVE 544 (36 g/L).
b.	Best Flat Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish 629 (45 g/L), MPI # 10.
c.	Better Flat Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorLife Flat Finish W105 (44 g/L), MPI # 10.
d.	Good Flat Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish 541 (44 g/L), MPI # 10.
e.	Flat Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish N447 (45 g/L), MPI # 10.
f.	Best Low Lustre Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish 634 (44 g/L), MPI # 15, 315.
g.	Better Low Lustre Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGard Low Lustre Finish W103 (36 g/L), MPI # 214.
h.	Good Low Lustre Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish 542 (45 g/L), MPI # 15.
i.	Low Lustre Commercial Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish N455 (48 g/L), MPI # 214.
j.	Best Satin Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish 631 (44 g/L).
k.	Better Satin Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
3)	Third Coat: Benjamin Moore Coronado Cryli Cote 100% Acrylic Exterior Paint Satin 410 (88 g/L).
l.	Good Satin Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
3)	Third Coat: Benjamin Moore Coronado Super Kote 5000 Exterior Acrylic Satin 803 (95 g/L).
m.	Commercial Satin Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish N448 (46 g/L), MPI # 15.
n.	Best Soft Gloss/ Semi-Gloss Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish 632 (46 g/L).
o.	Better Soft Gloss/ Semi-Gloss Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer N023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, LEED v4, qualifies for CHPS credit.
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint - MoorGlo Soft Gloss Finish W096 (42 g/L).
p.	Good Soft Gloss/ Semi-Gloss Synthetic Stucco Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish 543 (45 g/L), MPI # 11.
q.	Best Gloss Option:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer 046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, LEED v4, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309, 48 g/L.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309, 48 g/L.
r.	Better Gloss Option:
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39.
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
s.	Commercial Gloss Option:
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer N558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish N449 (46 g/L), MPI # 11.
2.10	COMMERCIAL INTERIOR PAINT SYSTEMS - CANADA
A.	CONCRETE - (Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place) including PLASTER - (Walls, Ceilings).
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Semi-Gloss Finish High Performance
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
d.	Eggshell/ Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
e.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Waterborne Alkyd System:
a.	Gloss Finish (Water Base)
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell Finish (Water Base):
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech 100% Solid Epoxy Pre-Primer V155 (6 g/L), LEED 2009.
2)	Second Coat Epoxy V440 (K206 g/L).
b.	Gloss Finish
1)	First Coat: Corotech 100% Solid Epoxy Pre-Primer V155 (6 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
4.	Pre Catalyzed Waterborne Epoxy
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
B.	CONCRETE: Ceilings.
1.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
c.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Dryfall Latex Flat K395 (46 g/L), MPI # 118.
2)	Second Coat: Benjamin Moore Dryfall Latex Flat K395 (46 g/L), MPI # 118.
C.	MASONRY: CMU - Concrete, Split Face, Scored, Smooth, High Density, Low Density, Fluted.
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Acrylic Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, 141 X-Green, LEED, LEED V4, CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Acrylic Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, 141 X-Green, LEED, LEED V4, CHPS.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Natura Waterborne Interior Semi-Gloss K514 (0 g/L), MPI # 54, X-Green 54, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Natura Waterborne Interior Semi-Gloss K514 (0 g/L), MPI # 54, X-Green 54, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
d.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Acrylic Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, 140 X-Green, LEED, LEED V4, CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Acrylic Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, 140 X-Green, LEED, LEED V4, CHPS.
e.	Eggshell / Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
f.	Eggshell / Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Natura Waterborne Interior Eggshell K513 (0 g/L), MPI # 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Natura Waterborne Interior Eggshell KK513 (0 g/L), MPI # 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
g.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
h.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
i.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Natura Waterborne Interior Flat Finish K512 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Natura Waterborne Interior Flat Finish K512 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Acrylic System:
a.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell/Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (206 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
4.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
D.	METAL: Aluminum, Galvanized.
1.	Latex Systems:
a.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. FP29 Acrylic Semi-Gloss Enamel (45 g/L), MPI # 141, X-Green 141, 153, 153 X-Green, LEED.
3)	Third Coat: Ultra Spec HP D.T.M. FP29 Acrylic Semi-Gloss Enamel (45 g/L), MPI # 141, X-Green 141, 153, 153 X-Green, LEED.
b.	Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Semi-Gloss High Performance:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
d.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
e.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
g.	Flat Finish
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Natura Waterborne Interior Flat Finish K512 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Natura Waterborne Interior Flat Finish K512 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System (Waterborne):
a.	Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
4.	Pre-Catalyzed Epoxy (Waterborne):
a.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
E.	METAL: Galvanized; Ceilings, Duct work.
1.	Multi-Surface Acrylic Coating System:
a.	Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
2.	Dryfall Waterborne Topcoats:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
c.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
F.	METAL - (Structural Steel Columns, Joists, Trusses, Beams, Miscellaneous and Ornamental Iron, Structural Iron, Ferrous Metal)
1.	Latex Systems:
a.	Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
c.	Semi-Gloss Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
d.	Eggshell Finish High Performance:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
e.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System (Waterborne):
a.	Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish Waterborne Alkyd:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
c.	Eggshell Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
4.	Urethane System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
5.	Dryfall Waterborne Topcoats:
a.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67 g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
G.	WOOD - (Walls, Ceilings, Doors, Trim):
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi - Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
c.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Alkyd System (Waterborne):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
b.	Semi-Gloss Finish (Water Base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48g/L), LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell Finish (Water Base):
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Satin K792 (48 g/L), LEED 2009, LEED V4, CHPS Certified.
3.	Stain and Varnish System:
a.	Gloss Finish:
1)	First Coat: Lenmar Waterborne Interior Wiping Stain 1WB.1300 (240 g/L), MPI # 186 LEED Credit.
2)	Second Coat: Lenmar Waterborne Aqua-Plastic Urethane Gloss 1WB.1400 (322 g/L), MPI # 121, 130.
3)	Third Coat: Lenmar Waterborne Aqua-Plastic Urethane Gloss 1WB.1400 (322 g/L), MPI # 121, 130.
b.	Satin Finish:
1)	First Coat: Lenmar Waterborne Interior Wiping Stain 1WB.1300 (240 g/L), MPI # 186 LEED Credit.
2)	Second Coat: Lenmar Waterborne Aqua-Plastic Urethane Satin, 1WB.1427 (335 g/L), MPI # 121, 128.
3)	Third Coat: Lenmar Waterborne Aqua-Plastic Urethane Satin, 1WB.1427 (335 g/L), MPI # 121, 128.
H.	DRYWALL - (Walls, Ceilings, Gypsum Board and similar items)
1.	Latex Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified
b.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer F372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Semi-Gloss F376 (0 g/L) MPI # 54, X-Green 54, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Eco Spec WB Semi-Gloss F376 (0 g/L) MPI # 54, X-Green 54, LEED V4, CHPS Certified.
c.	Eggshell / Satin System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009 LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
d.	Eggshell / Satin System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer F372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Eggshell F374 (0 g/L), MPI # 52, X-Green 52, 139, X-Green 139, X- Green 145, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Eco Spec WB Eggshell NF374 (0 g/L), MPI # 52, X-Green 52, 139, X-Green 139, X-Green 145, LEED V4, CHPS Certified.
e.	Low Sheen System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, X-Green 44, 144, X-Green 144, LEED 2009, LEED V4, CHPS Certified.
f.	Flat System
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
g.	Flat System:
1)	First Coat: Benjamin Moore Eco Spec WB Primer F372 (0 g/L) MPI # 50, X-Green 50, 149, X-Green 149, LEED V4 CHPS Certified.
2)	Second Coat: Benjamin Moore Eco Spec WB Flat F373 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED V4.
3)	Third Coat: Benjamin Moore Eco Spec WB Flat F373 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED V4.
2.	Epoxy System (Water Base):
a.	Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell/Low Luster System:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2.11	COMMERCIAL HIGH PERFORMANCE INTERIOR PAINT SYSTEMS - CANADA
A.	CONCRETE - Smooth (Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
b.	Semi-Gloss Finish High Performance:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Eggshell/Low Sheen:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS. Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2.	Alkyd System (Waterborne):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High Gloss F794 (48 g/L), MPI # 157, X-Green 157, LEED 2009, LEED V4.
3.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Semi-Gloss/High Luster Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
4.	Pre-Catalyzed Epoxy (Waterborne):
a.	Eggshell/Low Luster Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy Systems (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
3)	Third Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
6.	Urethane System (Water Base):
a.	Gloss Finish Single Component:
1)	First Coat: Corotech Waterborne Bonding Primer V175 (85 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (Two Component Product) (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (Two Component Product) (10 g/L), LEED Credit.
B.	CONCRETE - (Ceilings).
1.	MultiSurface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit.
2)	Second Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit.
2.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
C.	MASONRY - (CMU - Concrete, Split Face, Scored, Smooth, High Density, Low Density, Fluted, Stucco).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
b.	Semi-Gloss Finish:
1)	First Coat Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: : Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: : Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Flat Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3)	Third Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Alkyd System (Solvent Base Finish):
a.	Alkyd Urethane Modified:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
c.	Semi-Gloss/High Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
4.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss/High Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell/Low Luster Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
5.	Epoxy Systems (Solvent Base Finish):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
3)	Third Coat: Corotech Polyamide Epoxy V400 (341 g/L), MPI # 82, 98, 108, 177.
6.	Urethane Systems (Water Base).
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
7.	Urethane Systems (Solvent Base Finish):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Block Filler V114 (43 g/L), LEED 2009.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss DFT (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss DFT (305 g/L), MPI # 83, 174.
D.	Non-Ferrous- (Galvanized and Aluminum):
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
d.	Low Sheen:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
e.	Flat Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Acrylic System:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3)	Third Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
3.	Urethane System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
3)	Third Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
4.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
5.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
6.	Urethane Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
7.	Urethane Systems (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L) MPI # 83, 174.
8.	Multi-Surface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
2)	Second Coat: Corotech Quick Dry Acrylic Spray DTM Gloss V300 (87 g/L), MPI # 114, LEED Credit, SSPC Paint Spec. 24.
9.	Dryfall Waterborne Systems:
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
2)	Second Coat: Benjamin Moore Dry Fall Latex Semi-Gloss 397 (43 g/L), MPI # 226.
b.	Flat Finish:
1)	First Coat: Benjamin Moore Dryfall Latex Flat K395 (46 g/L), MPI # 118.
2)	Second Coat: Benjamin Moore Dryfall Latex Flat K395 (46 g/L), MPI # 118.
10.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
E.	METAL - (Structural Steel Columns, Joists, Trusses, Beams, Miscellaneous and Ornamental Iron, Structural Iron, Ferrous Metal).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Corotech Acrylic DTM Enamel Gloss V330 (199 g/L), MPI # 154, 164, LEED 2009, LEED V4.
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
3)	Third Coat: Corotech Acrylic DTM Enamel Semi-Gloss V331 (204 g/L), MPI # 153.
d.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
e.	Low Sheen:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
2.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
b.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Super Spec HP Acrylic Metal Primer KP04 (47 g/L), MPI # 107, X-Green 107, 134, LEED 2009, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
3)	Third Coat: Benjamin Moore Super Spec HP Urethane Alkyd Gloss Enamel P22 (394 g/L), MPI # 9, 48.
3.	Epoxy Systems (Water Base):
a.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
4.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009
5.	Urethane System (Water Base):
a.	Gloss Finish:
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
3)	Third Coat: Corotech Waterborne Urethane Gloss V540 (10 g/L), LEED Credit.
6.	Urethane System (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy Primer V150 (330 g/L).
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Gloss V500 (229 g/L), MPI # 72, 78, 83, 105.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Polyamide Epoxy Primer V150 (330 g/L).
2)	Second Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
3)	Third Coat: Corotech Aliphatic Acrylic Urethane Semi-Gloss V510 (305 g/L), MPI # 83, 174.
F.	METAL - (Ceilings - Structural Steel, Joists, Trusses, Beams).
1.	MultiSurface Acrylic Coating:
a.	Gloss Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic 80 (224 g/L), MPI # 114, 154, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic 80 (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi-Gloss Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Semi-Gloss 112 (67g/L), MPI # 226.
c.	Eggshell Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
d.	Flat Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Latex Flat N110 (46 g/L), MPI # 118.
2.	Dryfall Alkyd Topcoats:
a.	Flat Finish:
1)	First Coat: Corotech Prep All Universal Metal Primer V132 (394 g/L).
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 (346 g/L), MPI # 55.
G.	WOOD- (Doors, Trim, Partitions, Frames).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Gloss 80 (224 g/L), MPI # 114, 154, LEED Credit.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
3)	Third Coat: Coronado Rust Scat Waterborne Acrylic Semi-Gloss 90 (134 g/L), MPI # 153, LEED Credit.
c.	Low Sheen/Satin:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Low Sheen K537 (0 g/L), MPI # 44, 144, LEED, LEED V4, CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Low Sheen K537 (0 g/L), MPI # 44, 144, LEED, LEED V4, CHPS.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED, LEED V4, CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED, LEED V4, CHPS.
2.	Alkyd System (Waterborne):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd K794 (46 g/L), MPI # 157, X-Green 157, LEED, CHPS.
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd K794 (46 g/L), MPI # 157, X-Green 157, LEED, CHPS.
3.	Alkyd System (Solvent Base Finish):
a.	Gloss Finish Urethane Modified:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
3)	Third Coat: Corotech Alkyd Urethane Gloss V200 (336 g/L), MPI # 9, 27, 48.
4.	Epoxy System (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
b.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
5.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
6.	Epoxy System (Solvent Base):
a.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
b.	Gloss Finish:
1)	First Coat: Corotech Waterborne Bonding Primer V175, LEED Credit.
2)	Second Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
3)	Third Coat: Corotech Waterborne Amine Epoxy V440 (K206 g/L).
H.	DRYWALL - (Walls, Ceilings, Gypsum Board).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, 147 X-Green, 141, X-Green 141, LEED 2009, LEED V4, CHPS Certified.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
c.	Low Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Latex Eggshell K538 (0 g/L), MPI # 52, X-Green 52, 145, X-Green 145, 139, X-Green 139, LEED 2009, LEED V4, CHPS Certified.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer K534 (0 g/L), MPI # 50, X-Green 50, 149, X-Green 149, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Flat K536 (0 g/L), MPI # 53, X-Green 53, 143, X-Green 143, LEED 2009, LEED V4, CHPS Certified.
2.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
I.	PLASTER - (Walls, Ceilings)..
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Acrylic Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, 141 X-Green, LEED, LEED V4, CHPS.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Acrylic Gloss K540 (0 g/L), MPI # 54, X-Green 54, 147, X-Green 147, 141, 141 X-Green, LEED, LEED V4, CHPS.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009, LEED V4.
c.	Low Sheen Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2.	Epoxy Systems (Water Base):
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3)	Third Coat: Corotech Acrylic Epoxy V450 (168 g/L).
3.	Pre-Catalyzed Epoxy (Waterborne):
a.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009. .
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L), LEED 2009.
b.	Eggshell Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
3)	Third Coat: Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151, LEED 2009.
2.12	COMMERCIAL EXTERIOR PAINT SYSTEMS - CANADA
A.	CONCRETE (Cementitious Siding, Flexboard, Transite Board, Shingles (Non-Roof), Common Brick, Stucco, Tilt-up, Precast, and Poured-in-place Cement).
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
b.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
c.	Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
e.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore ben Waterborne Exterior Flat K542 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Waterborne Exterior Flat K542 (44 g/L), MPI # 10.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
2.	Elastomeric System: Not including cementitious siding, Flexboard, Transite board or shingles (non-roof).
a.	Flat Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, LEED, CHPS.
2)	Second Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3)	Third Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3.	Stain System:
a.	Solid Color Waterborne Finish:
1)	First Coat: Coronado TuffCrete Waterborne Acrylic Concrete Stain CST-2000 (153 g/L), MPI # 58.
2)	Second Coat: Coronado TuffCrete Waterborne Acrylic Concrete Stain CST-2000 (153 g/L), MPI # 58.
B.	MASONRY: Concrete Masonry Units (CMU) - Cinder or Concrete Block.
1.	Latex Systems:
a.	Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
b.	Semi-Gloss Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified..
c.	Satin Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Coronado Cryli Cote 100% Acrylic Satin House & Trim Paint 410 (83 g/L).
3)	Third Coat: Coronado Cryli Cote 100% Acrylic Satin House & Trim Paint 410 (83 g/L).
d.	Satin Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
e.	Flat Finish:
1)	First Coat: Coronado Super Kote 5000 Production Block Filler 958-11 (35 g/L), MPI # 4, X-Green 4, LEED V4, CHPS Certified.
2)	Second Coat: Coronado Cryli Cote 100% Acrylic Flat House & Trim Paint 10 (44 g/L), MPI # 10.
3)	Third Coat: Coronado Cryli Cote 100% Acrylic Flat House & Trim Paint 10 (44 g/L), MPI # 10.
f.	Flat-Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
g.	High Build Coating
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2.	Elastomeric System:
a.	Flat Finish
1)	First Coat: Benjamin Moore Super Spec Masonry Interior/Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4, X-Green 4, LEED 2009, LEED V4, CHPS Certified.
2)	Second Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3)	Third Coat: Benjamin Moore Super Spec Masonry 100% Acrylic Elastomeric Coating Flat 056 (99 g/L).
3.	Textured Masonry System:
a.	Textured (Water Based Finish)
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2)	Second Coat: Coronado Texcrete WB Textured Waterproofer
a)	Finish Texture Sand: 3192 (78 g/L), LEED Credit.
b)	Finish Texture Medium: 3196 (20 g/L) MPI # 42, LEED Credit.
b.	Smooth (Water Based)
1)	First Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
2)	Second Coat: Coronado Texcrete WB Acrylic Masonry Waterproofer Smooth Finish 3194 (90 g/L), LEED Credit.
4.	Stain System:
a.	Solid Color Waterborne Stain Finish:
1)	First Coat: Insl-X TuffCrete Solvent Acrylic Concrete Stain & Waterproofing Sealer CST-5100 (651 g/L), MPI # 58, 104.
2)	Second Coat: Insl-X TuffCrete Solvent Acrylic Concrete Stain & Waterproofing Sealer CST-5100 (651 g/L), MPI # 58, 104.
5.	Clear Water Repellant:
a.	Clear Finish
1)	First Coat: Coronado Texcrete Silicone Water Repellant 194 (21 g/L), MPI # 117, LEED Credit.
2)	Second Coat: Coronado Texcrete Silicone Water Repellant 194 (21 g/L), MPI # 117, LEED Credit.
C.	CONCRETE: Concrete Floors (non-vehicular), Patios, Porches, Steps and Platforms.
1.	Acrylic System Water-Based:
a.	Floor Finish:
1)	First Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen K122 (45 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen K122 (45 g/L), LEED 2009.
D.	METAL: Aluminum, Galvanized.
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
b.	Gloss Finish- Early Moisture Resistant Finish
1)	First Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
2)	Second Coat: Benjamin Moore Ultra Spec D.T.M. Acrylic Gloss Enamel KP28 (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED 2009, LEED V4.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic DTM Semi-Gloss Enamel KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
2)	Second Coat: Benjamin Moore Ultra Spec HP Acrylic DTM Semi-Gloss Enamel KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED 2009.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
e.	Low Lustre/ Satin Finish- Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
g.	Flat Finish- Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L), MPI # 10.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L), MPI # 10.
E.	METAL: Misc. Iron, Ornamental Iron, Structural Iron and Steel, Ferrous Metal.
1.	Latex Systems:
a.	Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel (45 g/L), MPI # 114, X-Green 114, 154, X-Green 154, 164, LEED.
b.	Semi-Gloss Finish
1)	First Coat: Corotech Acrylic Metal Primer V110 (199 g/L), LEED Credit.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss Enamel, KP29 (45 g/L), MPI # 141, X-Green 141, 153, X-Green 153, LEED.
F.	WOOD: Decks, Exterior including pressure treated lumber, Floors (non-Vehicular), Platforms.
1.	Acrylic Water-Based Floor System:
a.	Floor Finish:
1)	First Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen K122 (45 g/L), LEED 2009.
2)	Second Coat: Benjamin Moore Floor & Patio Latex Enamel Low Sheen K122 (45 g/L), LEED 2009.
2.	Stain Systems:
a.	Solid Color Acrylic Latex:
1)	First Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain K640 (93 g/L), MPI # 16.
2)	Second Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain K640 (93 g/L), MPI # 16.
b.	Semi-Transparent Stain:
1)	First Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain K638 (92 g/L), MPI # 156.
2)	Second Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain K638 (92 g/L), MPI # 156.
c.	Clear Stain:
1)	First Coat: Benjamin Moore Arborcoat Waterproofer K320 (34 g/L).
G.	WOOD: Siding, Trim, Shutters, Sashes, Hardboard-Bare/Primed.
1.	Latex Systems:
a.	Soft Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
b.	Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
e.	Low Lustre - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
g.	Flat Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
2.	Stain - Water Reducible Systems:
a.	Semi-Transparent:
1)	First Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain K638 (92 g/L) MPI # 156.
2)	Second Coat: Benjamin Moore Arborcoat Semi-Transparent Deck & Siding Stain K638 (92 g/L) MPI # 156.
b.	Solid Color:
1)	First Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain K640 (93 g/L) MPI # 16.
2)	Second Coat: Benjamin Moore Arborcoat Solid Deck & Siding Stain K640 (93 g/L) MPI # 16.
H.	ARCHITECTURAL PVC, PLASTIC, FIBERGLASS
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
b.	Soft-Gloss:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
c.	Satin Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
d.	Flat Finish:
1)	First Coat: Insl-X Stix Waterborne Bonding Primer SXA-110 (47 g/L).
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
I.	DRYWALL: Gypsum Board, Exterior Drywall.
1.	Latex Systems:
a.	Soft-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ben Waterborne Exterior Soft-Gloss K543 (45 g/L), MPI # 11.
b.	Soft-Gloss Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Latex Semi-Gloss K539 (0 g/L), MPI # 43, X-Green 43, 146, X-Green 146, 140, X-Green 140, LEED 2009, LEED V4, CHPS Certified.
d.	Low Lustre Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore ben Exterior Low Lustre K542 (45 g/l), MPI # 15.
3)	Third Coat: Benjamin Moore ben Exterior Low Lustre (45 g/l), MPI # 15.
e.	Low Lustre - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Low Lustre K401 (40 g/L), MPI # 15, 315.
f.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore ben Waterborne Exterior Flat K542 (44 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore ben Waterborne Exterior Flat K542 (44 g/L), MPI # 10.
g.	Flat Finish - Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, X-Green 17, 39, 50, X-Green 50, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
3)	Third Coat: Benjamin Moore Regal Select Exterior High-Build Flat Finish K400 (42 g/L) MPI # 10.
J.	VINYL SIDING EIFS, SYNTHETIC STUCCO:
1.	Latex Systems:
a.	Gloss Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L) MPI # 11.
b.	Soft-Gloss Finish - Vinyl Safe Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
c.	Semi-Gloss Finish:
1)	First Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
2)	Second Coat: Benjamin Moore Regal Select Exterior High-Build Soft-Gloss K403 (43 g/L), MPI # 11, 311.
d.	Satin Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin K448 (46 g/L), MPI # 15.
e.	Flat Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
f.	Flat Finish - Vinyl Safe Early Moisture Resistant Finish:
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Primer K/F023 (44 g/L), MPI # 6, 17, X-Green 17, 39, 137, X-Green 137, LEED Credit, CHPS Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
3)	Third Coat: Benjamin Moore Ultra Spec Exterior Flat Finish K447 (45 g/L), MPI # 10.
2.13	LIGHT COMMERCIAL/RESIDENTIAL INTERIOR PAINT SYSTEMS - Canada 
A.	CONCRETE - Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place including Plaster (Walls, Ceilings): 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
e.	Matte Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
f.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
g.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
h.	Low Sheen Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
i.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
j.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
k.	Eggshell Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
l.	Eggshell Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
m.	Eggshell Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
n.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
o.	Eggshell High Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151.
p.	Satin/Pearl Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
q.	Satin/Pearl Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
r.	Satin/Pearl Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
s.	Satin/Pearl Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
t.	Satin/Pearl Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
u.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
v.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
w.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
x.	Semi-Gloss Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
y.	Semi-Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
z.	Semi-Gloss High Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
aa.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ab.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L), MPI # 114, 114 X-Green. 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L) MPI # 114, 114 X-Green. 
2.	Waterborne Alkyd System: 
a.	Matte Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Pearl Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.
B.	Metal - Galvanized: 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
e.	Flat Commercial Option: 
1)	First Coat: First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
f.	Matte Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
i.	Low Sheen Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
l.	Eggshell Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
m.	Eggshell Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
n.	Eggshell Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145 and 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145 and 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit.
o.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
p.	Eggshell High Performance Option: 
1)	First Coat: Benjamin Moore Corotech Acrylic Metal Primer V110 (199 g/L). 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
q.	Satin/Pearl Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
r.	Satin/Pearl Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
s.	Satin/Pearl Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
t.	Satin/Pearl Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Satin/Pearl Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
v.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
w.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
x.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
y.	Semi-Gloss Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
z.	Semi-Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
aa.	Semi-Gloss High Performance Option: 
1)	First Coat: Benjamin Moore Corotech Acrylic Metal Primer V110 (199 g/L). 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
ab.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ac.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L), MPI # 114, 114 X-Green. 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L) MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System: 
a.	Matte Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Pearl Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.
3.	Direct To Metal (Latex Options): 
a.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
b.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
2)	Second Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
c.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
d.	Gloss Better Option: 
1)	First Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164. 
2)	Second Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
C.	Wood - Doors, Trim, Paneling: 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
e.	Matte Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
f.	Matte Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
g.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
h.	Low Sheen Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
i.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
j.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
k.	Eggshell Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
l.	Eggshell Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
m.	Eggshell Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
n.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
o.	Eggshell High Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
p.	Satin/Pearl Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
q.	Satin/Pearl Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
r.	Satin/Pearl Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
s.	Satin/Pearl Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
t.	Satin/Pearl Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
u.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
v.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
w.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
x.	Semi-Gloss Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
y.	Semi-Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
z.	Semi-Gloss High-Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-04XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
aa.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ab.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
2.	Waterborne Alkyd System: 
a.	Matte Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Satin Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.
D.	DRYWALL - (Walls, Ceilings, Gypsum Board and similar items): 
1.	Latex Systems: 
a.	Ceiling Best Paint: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Waterborne Ceiling Paint K508 (0 g/L), qualifies for LEED v4 Credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Waterborne Ceiling Paint K508 (0 g/L), qualifies for LEED v4 Credit, qualifies for CHPS credit. 
b.	Ceiling Better Paint: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Muresco Ceiling White K258 (44 g/L).  
3)	Third Coat:  Benjamin Moore Muresco Ceiling White K258 (44 g/L).  
c.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
e.	Flat Good Option: 
1)	First Coat: Benjamin Moore Eco Spec WB Interior Latex Primer F372 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
f.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
g.	Matte Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
h.	Matte Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
i.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
j.	Low Sheen Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Finish K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
k.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
l.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
m.	Eggshell Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
n.	Eggshell Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
o.	Eggshell Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
p.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
q.	Eggshell High Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
r.	Satin/Pearl Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
s.	Satin/Pearl Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
t.	Satin/Pearl Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
u.	Satin/Pearl Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
v.	Satin/Pearl Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
w.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
x.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551, (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
y.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
z.	Semi-Gloss Specialty Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
aa.	Semi-Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ab.	Semi-Gloss High-Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-04XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
ac.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Primer K534 (0 g/L), MPI # 50, 50 X-Green, 149, 149 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ad.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
2.	Waterborne Alkyd System: 
a.	Matte Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Matte Finish K791 (46.5 g/L), MPI # 165, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Satin Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
d.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Advance Waterborne Interior Alkyd Primer K790 (44 g/L), MPI # 172, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.
E.	Concrete - (Floors, non-vehicular): 
1.	Latex System - Self Priming: 
a.	Low Sheen Best Option: 
1)	First Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel F122 (45 g/L), qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel F122 (45 g/L), qualifies for LEED v4 credit. 
b.	Concrete Stain Better Option: 
1)	First Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L), MPI # 58. 
2)	Second Coat: Benjamin Moore Insl-x TuffCrete Waterborne Acrylic Concrete Stain CST-2XXX (178 g/L), MPI # 58.
F.	Interior Concrete Block: 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Flat Finish K547 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Flat Finish K625 (0 g/L), MPI # 53, 53 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
d.	Flat Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Flat Finish F373 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
e.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish K536 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS. 
f.	Matte Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, CHPS. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Matte Finish K522 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
g.	Matte Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Ulti-Matte K552 (0 g/L), MPI # 53, 53 X-Green, 143, 143 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
h.	Matte Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish K484 (82 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
i.	Low Sheen Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, CHPS, qualifies for CHPS. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen K537 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS. 
j.	Eggshell Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Eggshell Finish K524 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
k.	Eggshell Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Eggshell Finish K549 (0 g/L), MPI # 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
l.	Eggshell Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Eggshell Finish K626 (0 g/L), MPI # 44, 44 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
m.	Eggshell Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Eggshell Finish F374 (0 g/L), MPI # 52, 52 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
n.	Eggshell Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish K538 (0 g/L), MPI # 52, 52 X-Green, 139, 139 X-Green, 145, 145 X-Green, qualifies for LEED v4 credit, Cradle to Cradle Certified Silver, qualifies for CHPS credit. 
o.	Eggshell Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish K485 (88.4 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
p.	Eggshell High Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Eggshell V342 (73 g/L), MPI # 151. 
q.	Satin/Pearl Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Satin Finish K526 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
r.	Satin/Pearl Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Pearl Finish K550 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
s.	Satin/Pearl Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
3)	Third Coat: Benjamin Moore ben Interior Latex Pearl Finish K628 (0 g/L), MPI # 43, 43 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
t.	Satin/Pearl Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Pearl Finish F375 (0 g/L), LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Satin/Pearl Scuff Resistant Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Pearl Finish K486 (86 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
v.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore AURA Waterborne Interior Semi-Gloss Finish K528 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
w.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Regal Select Waterborne Interior Semi-Gloss Finish K551 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
x.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore ben Interior Latex Semi-Gloss Finish K627 (0 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
y.	Semi-Gloss Specialty Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Eco Spec WB Interior Latex Semi-Gloss Finish F376 (0 g/L), MPI # 54, 54 X-Green, LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
z.	Semi-Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146 and 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi-Gloss Finish K539 (0 g/L), MPI # 43, 43 X-Green, 140, 140 X-Green, 146 and 146 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
aa.	Semi-Gloss High-Performance Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-04XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
3)	Third Coat: Benjamin Moore Corotech Pre-Catalyzed Waterborne Epoxy Semi-Gloss V341 (71 g/L). 
ab.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Gloss Finish K540 (0 g/L), MPI # 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
ac.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L), MPI # 114, 114 X-Green. 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L), MPI # 114, 114 X-Green.
2.	Waterborne Alkyd System: 
a.	Satin Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Pearl Finish K792 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
b.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd Semi-Gloss Finish K793 (48 g/L), qualifies for LEED v4 credit, qualifies for CHPS credit. 
c.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
3)	Third Coat: Benjamin Moore Advance Waterborne Interior Alkyd High-Gloss Finish K794 (46 g/L), MPI # 157, 157 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.
2.14	LIGHT COMMERCIAL/RESIDENTIAL EXTERIOR PAINT SYSTEMS - Canada 
A.	CONCRETE - Cementitious Siding, Flexboard, Transite Board, Shingles (Non-Roof), Common Brick, Stucco, Tilt-up, Precast, and Poured-in-place Cement: 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit.  
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Flat Finish K541 (44 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Flat Finish K541 (44 g/L), MPI # 10. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15.
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit.
2)	Second Coat: Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/ Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben 100% Acrylic Exterior Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben 100% Acrylic Exterior Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
o.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
p.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
2.	Elastomeric System - Not including Cementitious Siding, Flexboard, Transite Board or Shingles (non-roof): 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Flat K359 (93 g/L). 
3)	Third Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Flat K359 (93 g/L). 
b.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior / Exterior 100% Acrylic Masonry Sealer K608 (46 g/L), MPI # 3, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Low Lustre K360 (95 g/L). 
3)	Third Coat: Benjamin Moore Ultra Spec Masonry Elastomeric Waterproofing Coating Low Lustre K360 (95 g/L).
B.	Concrete Block: 
1.	Latex System Options: 
a.	Flat Best Options: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Super Spec Masonry Inter / Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Super Spec Masonry Inter / Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10,15.
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Super Spec Masonry Inter / Exterior Hi-Build Block Filler K206 (45 g/L), MPI # 4. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
o.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior/ Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
p.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler K571 (45 g/L), MPI # 4, 4 X-Green, qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
C.	Concrete - Floors (Non-Vehicular): 
1.	Latex System Options - Self Priming: 
a.	Low Sheen Best Option: 
1)	First Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel F122 (45 g/L), qualifies for LEED v4 credit. 
2)	Second Coat: Benjamin Moore Latex Floor & Patio Low Sheen Enamel F122 (45 g/L), qualifies for LEED v4 credit. 
b.	High-Gloss Best Option: 
1)	First Coat: Benjamin Moore Latex Floor & Patio High Sheen Enamel K121 (43.7 g/L). 
2)	Second Coat: Benjamin Moore Latex Floor & Patio High Sheen Enamel K121 (43.7 g/L).
D.	Metal - Galvanized: 
1.	Latex Systems: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit.  
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
o.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
p.	Gloss Commercial Option 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
2.	Direct To Metal (Latex Options): 
a.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
b.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Semi-Gloss 90 (135 g/L), MPI # 153. 
c.	Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
2)	Second Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
d.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
e.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Interior / Exterior Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
f.	Gloss Good Option: 
1)	First Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164. 
2)	Second Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
E.	METAL - Misc. Iron, Ornamental Iron, Structural Iron and Steel, Ferrous Metal: 
1.	Latex Options: 
a.	Best Flat Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit.  
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L) MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
o.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
p.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer FP04 (48 g/L), MPI # 107, 107 X-Green, 134, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
2.	Direct to Metal-Latex Options: 
a.	Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi-Gloss FP29 (147 g/L), MPI # 141,153. 
b.	Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
2)	Second Coat: Benjamin Moore Corotech Acrylic Semi-Gloss DTM V331 (204 g/L), MPI # 153. 
c.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel FP28 (142 g/L), MPI # 114, 154, 164. 
d.	Gloss Better Option: 
1)	First Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164. 
2)	Second Option: Benjamin Moore Corotech Acrylic Gloss DTM V330 (199 g/L), MPI # 154, 164.
F.	Wood - Decks, Exterior including pressure treated lumber, Floors (non-Vehicular): 
1.	Non-Bleeding Wood-Water-Based/Waterborne Alkyd Stain Options (Self-Priming): 
a.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent K623 (21 g/L), MPI # 33. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent K623 (21 g/L), MPI # 33. 
b.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain B7400 Series (180 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain B7400 Series (180 g/L). 
c.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent F638 (92 g/L), MPI # 156. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent F638 (92 g/L), MPI # 156. 
d.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain B7600 Series (180 g/L), MPI # 156. 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain B7600 Series (180 g/L), MPI # 156. 
e.	Semi-Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi-Solid Stain K639 (93 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi-Transparent Stain K639 (93 g/L). 
f.	Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain K640 (95 g/L), MPI # 16. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain K640 (95 g/L), MPI # 16. 
g.	Solid Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Solid Color Deck Stain B8500 Series (175 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Solid Color Deck Stain B8500 Series (175 g/L).
2.	Non-Bleeding Wood Solvent Based Stain Options (Self-Priming): 
a.	Clear Specialty Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Waterproofer K320 (34 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Waterproofer K320 (34 g/L). 
b.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
c.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
d.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
e.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
f.	Semi-Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L).
3.	Bleeding Wood (Redwood & Cedar) - Oil Based Stain Options: 
a.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
b.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5, 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
3)	Third Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
c.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
d.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5, 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
3)	Third Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
e.	Semi-Solid Best Options: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L). 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L).
G.	WOOD - Siding, Trim, Shutters, Sashes, Hardboard-Bare/Primed: 
1.	Non-Bleeding Wood-Water-Based/Waterborne Alkyd Stain Options (Self-Priming): 
a.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent K623 (21 g/L), MPI # 33. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Translucent K623 (21 g/L), MPI # 33. 
b.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain B7400 Series (180 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain B7400 Series (180 g/L). 
c.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent F638 (92 g/L), MPI # 156. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Stain Semi-Transparent F638 (92 g/L), MPI # 156. 
d.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain B7600 Series (180 g/L), MPI # 156. 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain B7600 Series (180 g/L), MPI # 156. 
e.	Semi-Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi-Solid Stain K639 (93 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Semi-Transparent Stain K639 (93 g/L). 
f.	Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain K640 (95 g/L), MPI # 16. 
2)	Second Coat: Benjamin Moore Arborcoat Waterborne Exterior Solid Color Stain K640 (95 g/L), MPI # 16. 
g.	Solid Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Solid Color Deck Stain B8500 Series (175 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Solid Color Deck Stain B8500 Series (175 g/L).
2.	Non-Bleeding Wood Solvent Based Stain Options (Self-Priming): 
a.	Clear Specialty Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Waterproofer K320 (34 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Waterproofer K320 (34 g/L). 
b.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
c.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
d.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
e.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
f.	Semi-Solid Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L). 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L).
3.	Bleeding Wood (Redwood & Cedar) - Oil Based Stain Options: 
a.	Translucent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Finish Translucent K326 (340 g/L), MPI # 13, 33. 
b.	Translucent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5, 
2)	Second Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
3)	Third Coat: Benjamin Moore Coronado Maxum Translucent Deck & Siding Stain C7300 Series (234 g/L). 
c.	Semi-Transparent Best Option: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi-Transparent K328 (229 g/L), MPI # 13, 33. 
d.	Semi-Transparent Better Option: 
1)	First Coat: Benjamin Moore Coronado Maxum Deck & Siding Primer B800 (348 g/L), MPI # 5, 
2)	Second Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
3)	Third Coat: Benjamin Moore Coronado Maxum Semi-Transparent Deck & Siding Stain C7500 Series (229 g/L). 
e.	Semi-Solid Best Options: 
1)	First Coat: Benjamin Moore Arborcoat Exterior Oil Primer K366 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L). 
3)	Third Coat: Benjamin Moore Arborcoat Exterior Oil Stain Semi Solid K329 (226 g/L).
4.	Non-Bleeding Wood Latex System Options: 
a.	Ultra Flat/Solid Best Stain Option (Self-Priming): 
1)	First Coat: Benjamin Moore Arborcoat Waterborne Ultra Flat Solid Stain K610 (72.2 g/L), MPI # 16. 
2)	Second Option: Benjamin Moore Arborcoat Waterborne Ultra Flat Solid Stain K610 (72.2 g/L), MPI # 16. 
b.	Ultra Flat/Solid Better Stain Option (Self-Priming): 
1)	First Coat: Benjamin Moore Coronado Maxum Solid Color Siding Stain B2000 Series (144 g/L), MPI # 16. 
2)	Second Coat: Benjamin Moore Coronado Maxum Solid Color Siding Stain B2000 Series (144 g/L), MPI # 16. 
c.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
d.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10.
e.	Flat Good Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
f.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
g.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
h.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
i.	Low Lustre Good Option: 
1)	First Coat: First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, CHPS. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
j.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
k.	Satin Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
l.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
m.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
n.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit.  
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11.
o.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
p.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, 48 g/L. 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, 48 g/L. 
q.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Coronado Super Kote 5000 Interior Acrylic Latex Primer Sealer 40 Line (46 g/L), MPI #50, CHPS. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
r.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
5.	Alkyd Primer System - Recommended for Bleeding Type Wood (such as Redwood & Cedar): 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10.
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start Exterior Wood Primer K094 (345 g/L), MPI # 5. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, 48 g/L. 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, 48 g/L. 
o.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
H.	Architectural PVC, Plastic, Fiberglass, Azek: 
1.	Latex Options: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-04XX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Low Lustre Finish K401 (40 g/L), MPI # 10, 15. 
g.	Low Lustre Good Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
h.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
i.	Satin Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
j.	Satin Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
k.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
l.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Soft Gloss Finish K403 (43 g/L), MPI # 11. 
m.	Soft Gloss/Semi-Gloss Good Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
n.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309 (48 g/L). 
o.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
p.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
I.	Vinyl Siding, EIFS: 
1.	Latex Options: 
a.	Flat Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Flat Finish K629 (45 g/L), MPI # 10. 
b.	Flat Better Option: 
1)	First Coat: Benjamin Moore Fresh Start Multi-Purpose Latex Primer F023 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Regal Select Exterior Paint High Build Flat Finish K400 (42 g/L), MPI # 10. 
c.	Flat Good Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Flat Finish K541 (44 g/L), MPI # 10. 
d.	Flat Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Flat Finish K447 (45 g/L), MPI # 10. 
e.	Low Lustre Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
3)	Third Coat: Benjamin Moore Aura Exterior Paint Low Lustre Finish K634 (44 g/L), MPI # 15, 315. 
f.	Low Lustre Better Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Low Lustre Finish K542 (45 g/L), MPI # 15. 
g.	Low Lustre Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Low Lustre Finish K455 (48 g/L), MPI # 214. 
h.	Satin Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Paint Satin Finish K631 (44 g/L). 
i.	Commercial Satin Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Satin Finish K448 (46 g/L), MPI # 15. 
j.	Soft Gloss/Semi-Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
3)	Third Coat: Benjamin Moore Aura Waterborne Exterior Semi-Gloss Finish K632 (46 g/L). 
k.	Soft Gloss/Semi-Gloss Better Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore ben Exterior 100% Acrylic Soft Gloss Finish K543 (45 g/L), MPI # 11. 
l.	Gloss Best Option: 
1)	First Coat: Benjamin Moore Fresh Start High-Hiding All Purpose Primer K046 (44 g/L), MPI # 6, 17, 17 X-Green, 39, 50, 50X-Green, 137, 137 X-Green, qualifies for LEED v4 credit, qualifies for CHPS credit. 
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, (48 g/L).
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel L309, (48 g/L).
m.	Gloss Better Option: 
1)	First Coat: Benjamin Moore Insl-X Aqua Lock Plus AQ-0XXX (50 g/L), MPI # 39. 
2)	Second Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
3)	Third Coat: Benjamin Moore Coronado Rust Scat WB Acrylic Enamel Gloss 80 (224 g/L), MPI # 114, 154. 
n.	Gloss Commercial Option: 
1)	First Coat: Benjamin Moore Ultra Spec EXT Primer K558 (45 g/L), MPI # 6. 
2)	Second Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11. 
3)	Third Coat: Benjamin Moore Ultra Spec EXT Gloss Finish K449 (46 g/L), MPI # 11.
PART 3    EXECUTION 
3.1	EXAMINATION 
A.	The Contractor shall review the product manufacturer's special instructions for surface preparation, application, temperature, re-coat times, and product limitations. 
B.	The Contractor shall review product health and safety precautions listed by the manufacturer. 
C.	The Contractor shall be responsible for enforcing on site health and safety requirements associated with the Work. 
D.	Do not begin installation until substrates have been properly prepared. 
E.	Ensure that surfaces to receive paint are dry immediately prior to application. 
F.	Ensure that moisture-retaining substrates to receive paint have moisture content within tolerances allowed by coating manufacturer. Where exceeding the following values, promptly notify Architect and obtain direction before beginning work. 
1.	Concrete and Masonry: 3-5 percent. Allow new concrete to cure a minimum of 28 days. 
2.	Exterior Wood: 17 percent. 
3.	Interior Wood: 15 percent. 
4.	Interior Finish Detail Woodwork, Including Trim, and Casework: 10 percent. 
5.	Plaster and Gypsum: 15 percent. 
6.	Concrete Slab-On-Grade: Perform calcium chloride test over 24 hour period or other acceptable test to manufacturer. Verify acceptable moisture transmission and pH levels. 
G.	Examine surfaces to receive coatings for surface imperfections and contaminants that could impair performance or appearance of coatings, including but not limited to, loose primer, rust, scale, oil, grease, mildew, algae, or fungus, stains or marks, cracks, indentations, or abrasions. 
H.	Correct conditions that could impair performance or appearance of coatings in accordance with specified surface preparation procedures before proceeding with coating application. 
3.2	PREPARATION - GENERAL 
A.	Clean surfaces thoroughly prior to coating application. 
B.	Do not start work until surfaces to be finished are in proper condition to produce finished surfaces of uniform, satisfactory appearance. 
C.	Stains and Marks: Remove completely, if possible, using materials and methods recommended by coating manufacturer; cover stains and marks which cannot be completely removed with isolating primer or sealer recommended by coating manufacturer to prevent bleed-through. 
D.	Remove Mildew, Algae, and Fungus using materials and methods recommended by coating manufacturer. 
E.	Remove dust and loose particulate matter from surfaces to receive coatings immediately prior to coating application. 
F.	Remove or protect adjacent hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items not indicated to receive coatings. 
G.	Move or protect equipment and fixtures adjacent to surfaces indicated to receive coatings to allow application of coatings. 
H.	Protect adjacent surfaces not indicated to receive coatings. 
I.	Prepare surfaces in accordance with manufacturer's instructions for specified coatings and indicated materials, using only methods and materials recommended by coating manufacturer. 
3.3	SURFACE PREPARATION 
A.	Concrete and Concrete Masonry: Clean surfaces free of loose particles, sand, efflorescence, laitance, form oil, curing compounds, and other substances which could impair coating performance or appearance. 
B.	Concrete Floors: Remove contaminants which could impair coating performance or appearance. Verify moisture transmission and alkaline-acid balance recommended by coating manufacturer; mechanically abrade surface to achieve 80-100 grit medium-sandpaper texture. 
C.	Existing Coatings: 
1.	Remove surface irregularities by scraping or sanding to produce uniform substrate for coating application; apply one coat primer of type recommended by coating manufacturer for maximum coating adhesion. 
2.	If presence of lead in existing coatings is suspected, cease surface preparation and notify Architect immediately. 
D.	Gypsum Board: Repair cracks, holes and other surface defects with joint compound to produce surface flush with adjacent surfaces. 
E.	Masonry Surfaces - Restored: Remove loose particles, sand, efflorescence, laitance, cleaning compounds and other substances that could impair coating performance or appearance. 
F.	Metals - Aluminum, Mill-Finish: Clean and etch surfaces with a phosphoric acid-water solution or water based industrial cleaner. Flush with clean water and allow to dry, before applying primer coat. 
G.	Metals - Copper: Clean surfaces with pressurized steam, pressurized water, or solvent washing. 
H.	Metals - Ferrous, Unprimed: Remove rust or scale, if present, by wire brush cleaning, power tool cleaning, or sandblast cleaning; remove grease, oil, and other contaminants which could impair coating performance or appearance by solvent cleaning, with phosphoric-acid solution cleaning of welds, bolts and nuts; spot-prime repaired welds with specified primer. 
I.	Metals - Ferrous, Shop-Primed: Remove loose primer and rust, if present, by scraping and sanding, feathering edges of cleaned areas to produce uniform flat surface; solvent-clean surfaces and spot-prime bare metal with specified primer, feathering edges to produce uniform flat surface. 
J.	Metals - Galvanized Steel (not passivated): Clean with a water-based industrial strength cleaner, apply an adhesion promoter followed by a clean water rinse. Alternately, wipe down surfaces using clean, lint-free cloths saturated with xylene or lacquer thinner; followed by wiping the surface dry using clean, lint-free cloths. 
K.	Metals - Galvanized Steel, Passivated: Clean with water-based industrial strength cleaner. After the surface has been prepared, apply recommended primer to a small area. Allow primer to cure for 7 days, and test adhesion using the "cross-hatch adhesion tape test" method in accordance with ASTM D 3359. If the adhesion of the primer is positive, proceed with a recommended coating system for galvanized metal. 
L.	Metals - Stainless Steel: Clean surfaces with pressurized steam, pressurized water, or water-based industrial cleaner. 
M.	Plaster: Repair cracks, holes and other surface defects as required to maintain proper surface adhesion. Apply patching plaster or Joint compound and sand to produce surface flush with adjacent undamaged surface. Allow a full cure prior to coating application as recommended by the patching compound manufacturer's recommendations. 
N.	Polyvinyl Chloride (PVC) Pipe: remove contaminants and markings with denatured alcohol scuff sand and wipe with solvent for maximum adhesion. Test adhesion before starting the job. 
O.	Fiberglass Doors - remove contaminants with cleaning solvent (alcohol) scuff sand and wipe. Test adhesion of primer before starting job. 
P.	Textiles - Insulated Coverings, Canvas or Cotton: Clean using high-pressure air and solvent of type recommended for material. 
Q.	Wood: 
1.	Seal knots, pitch streaks, and sap areas with sealer recommended by coating manufacturer; fill nail recesses and cracks with filler recommended by coating manufacturer; sand surfaces smooth. 
2.	Remove mill marks and ink stamped grade marks. 
3.	Apply primer coat to back of wood trim and paneling. 
R.	Wood Doors: Seal door tops and bottoms prior to finishing. 
S.	Wood Doors - Field-Glazed Frames and Sash: Prime or seal glazing channels prior to glazing. 
3.4	APPLICATION - GENERAL 
A.	Application of primers, paints, stains or coatings, by the Contractor, will serve as acceptance that surfaces were properly prepared in accordance with the manufacturer's recommendation. 
B.	Apply each coat to uniform coating thickness in accordance with manufacturer's instructions, not exceeding manufacturer's specified maximum spread rate for indicated surface; thins, brush marks, roller marks, orange-peel, or other application imperfections are not permitted. 
C.	Allow manufacturer's specified drying time, and ensure correct coating adhesion, for each coat before applying next coat. 
D.	Inspect each coat before applying next coat; touch-up surface imperfections with coating material, feathering, and sanding if required; touch-up areas to achieve flat, uniform surface without surface defects visible from 5 feet (1.5 m). 
E.	Remove dust and other foreign materials from substrate immediately prior to applying each coat. 
F.	Where paint application abuts other materials or other coating color, terminate coating with a clean sharp termination line without coating overlap. 
G.	Where color changes occur between adjoining spaces, through framed openings that are of same color as adjoining surfaces, change color at outside stop corner nearest to face of closed door. 
H.	Re-prepare and re-coat unsatisfactory finishes; refinish entire area to corners or other natural terminations. 
3.5	CLEANING 
A.	Clean excess coating materials, and coating materials deposited on surfaces not indicated to receive coatings, as construction activities of this section progress; do not allow to dry. 
B.	Re-install hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items that have been removed to protect from contact with coatings. 
C.	Reconnect equipment adjacent to surfaces indicated to receive coatings. 
D.	Relocate to original position equipment and fixtures that have been moved to allow application of coatings. 
E.	Remove protective materials. 
3.6	PROTECTION AND REPAIR 
A.	Protect completed coating applications from damage by subsequent construction activities until completion of painting project. 
B.	Touch-up coatings damaged by subsequent construction activities. 

END OF SECTION
  
 	All references to (0 g/L) are Zero VOCs according to EPA Method 24. The CERTIFIED ASTHMA & ALLERGY FRIENDLY Mark is a Registered Certification Mark of the ASTHMA AND ALLERGY FOUNDATION OF AMERICA and ALLERGY STANDARDS, LTD. Cradle to Cradle Certifiedï¿½ is a certification mark licensed by the Cradle to Cradle Products Innovation Institute. These products are not endorsed by or a division of CHPS.  These products are provided by Benjamin Moore & Co., not CHPS.