SECTION 09 91 23

INTERIOR PAINTING - COMMERCIAL/RESIDENTIAL SYSTEMS - UNITED STATES

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2008 -  2024 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Commercial interior painting systems; United States.
1.	Concrete ceilings.
2.	Masonry rough or pitted.
3.	Masonry smooth.
4.	Metal ferrous.
5.	Metal non-ferrous.
6.	Drywall.
7.	Cured plaster.
8.	Wood and engineered wood products.
1.2	RELATED SECTIONS - INTERIOR 
A.	Division 3 - Concrete - Walls and Ceilings, Poured Concrete, Precast Concrete, Unglazed Brick, Cement Board, Tilt-Up, Cast-In-Place including Plaster (Walls, Ceilings, Concrete - (Floors, non-vehicular).
B.	Division 4 - Interior Concrete Block.
C.	Division 5 - Metal - Galvanized.
D.	Division 6 - Wood - Doors, Trim, Paneling.
E.	Division 9 - Drywall - (Walls, Ceilings, Gypsum Board, and similar items).
1.3	REFERENCES
A.	American National Standards Institute (ANSI) - Performance Standards.
B.	Asthma and Allergy Foundation of America and Allergy Standards, Ltd.
1.	The Certified Asthma and Allergy Friendly Mark. A registered certification mark.
C.	American Society for Testing Materials (ASTM) - Testing Methods.
D.	Cradle to Cradle Products Innovation Institute.
1.	Cradle to Cradle Certification.
E.	Environmental Protection Agency; Electronic Code of Federal Regulations (CFR):
1.	40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings; U.S. Environmental Protection Agency; current edition.
F.	Green Seal Standards (GS-11):
1.	GS-11; May 20, 1993.
G.	Master Paint Institute (MPI No.) - Established paint categories and standards.
H.	National Paint and Coatings Association (NPCA) - Gloss Standard.
I.	Occupational Safety and Health Act (OSHA) - Safety Standards.
J.	Ozone Transmission Commission (OTC) - Established levels of Volatile Organic Compounds.
K.	Paint Decorating Contractors of America (PDCA) - Application Standard.
L.	Society of Protective Coatings (SSPC):
1.	SSPC (PM1) - Steel Structures Painting Manual, Vol. 1, Good Painting Practice; 1993, Third Edition.
2.	SSPC (PM2) - Steel Structures Painting Manual, Vol. 2, Systems and Specifications; 1995, Seventh Edition.
M.	South Coast Air Quality Management District (SCAQMD): 
1.	SCAQMD Rule No.1168; October 3, 2003.
N.	US Green Building Council, (USGBC) - Green Seal standards for LEED paint credits.
1.4	DEFINITIONS
A.	Commercial as used in this Section refers to a product well suited for a commercial application.
B.	DFT as used in this Section refers to the Dry Film Thickness of the coating.
C.	Enamel refers to any acrylic or alkyd (oil) base paint which dries leaving an eggshell, pearl, satin, semi-gloss, or high gloss enamel finish.
D.	DTM as used in this Section refers to paint that is applied Direct To Metal.
E.	LEED as used in this Section, refers to Leadership in Energy and Environmental Design. Products listed meet LEED criteria for environmentally safe interior primers, paints, and coatings.
F.	OTC as used in this Section refers to the Ozone Transmission Commission. OTC has established the following VOC levels for the Northeastern United States. Products shall meet the following OTC limits for VOC's.
1.	Interior flat paints: 100 grams per liter or less, per gallon.
2.	Interior enamels: 150 grams per liter or less, per gallon.
3.	Interior stains: 250 grams per liter or less, per gallon.
4.	Interior primers: 200 grams per liter or less, per gallon.
5.	Rust preventive coatings: 400 grams per liter or less, per gallon.
6.	Dry fog coatings: 400 grams per liter or less, per gallon.
7.	Floor coatings: 250 grams per liter or less, per gallon.
G.	Premium as used in this Section refers to the best quality product "top of the line".
H.	VOC as used in this Section refers to Volatile Organic Compounds found in primers, paints, sealers, and stains. The level of VOCs appears after each product listed in the Schedule in grams per liter (g/L).
I.	Paints are available in a wide range of sheens or glosses, as measured by a gloss meter from a 60 and/or 85 degree angle from vertical, as a percentage of the amount of light that is reflected. The following terms are used to describe the gloss of our products. The list below is provided for general guidance; refer to the technical data sheet for the actual gloss/sheen level for each product.
1.	Flat - Less than 5 Percent.
2.	Eggshell - 5 - 20 Percent.
3.	Satin - 20 - 35 Percent.
4.	Semi-Gloss - 30 - 65 Percent.
5.	Gloss - Over 65 Percent.
1.5	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	LEED Certification Product Data:
1.	See Section 01 00 00 - General Requirements.
2.	Submittals Required:
a.	MRc3 Resource Reuse (LEED Form).
b.	MRc4 Recycled Content (LEED Form).
c.	MRc5 Local and Regional Materials (LEED Form).
d.	EQc4.2 Low Emitting Materials - Paint (VOC Certification Letter).
C.	Product Data: Provide a complete list of all products to be used, with the following information for each:
1.	Manufacturer's name, product name and/or catalog number, and general product category.
2.	Cross-reference to specified paint system(s) that the product is to be used in; include description of each system.
D.	Samples: Submit three paper samples, 5 inches by 7 inches (127mm x 178mm) in size, illustrating selected colors for each color and system selected with specified coats cascaded.
E.	Manufacturer's Instructions: Indicate special surface preparation procedures.
F.	Maintenance Data: Submit data on cleaning, touch-up, and repair of painted and coated surfaces.
1.6	QUALITY ASSURANCE
A.	Manufacturer Qualifications: All primary products specified in this section will be supplied by a single manufacturer with a minimum of ten years' experience.
B.	Installer Qualifications: All products listed in this section are to be applied by a Painting Contractor with a minimum of five years demonstrated experience in surface preparation and field application of the same type and scope as specified.
C.	Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.	Mock-up areas designated by Architect.
2.	Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
3.	Approved mock-up areas will serve as the standard for remaining Work.
4.	Refinish mock-up area as required to produce acceptable Work.
1.7	DELIVERY, STORAGE, AND HANDLING
A.	Store products in manufacturer's unopened packaging until ready for installation.
B.	Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.
C.	Disposal:
1.	Never pour leftover coating down any sink or drain. Use up material on the job or seal can and store safely for future use.
2.	Do not incinerate closed containers.
3.	For specific disposal or recycle guidelines, contact the local waste management agency or district. Recycle whenever possible.
1.8	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.9	WARRANTY
A.	Inspection of all surfaces to be coated must be done by the manufacturer's representative to insure proper preparation prior to application. All thinners, fillers, primers, and finish coatings shall be from the same manufacturer to support a product warranty. Products other than those submitted shall be accompanied by a letter stating its fitness for use and compatibility.
B.	At project closeout, provide to the Owner or owner's representative an executed copy of the Manufacturer's standard form outlining the terms and conditions of and any exclusions to their Limited Warranty against Manufacturing Defect.
1.10	EXTRA MATERIALS
A.	At project closeout, supply the Owner or owner's representative one gallon of each product for touch-up purposes. Cans shall be clearly marked with color name, number, and type of paint.
B.	At project closeout, provide the color mixture name and code to the Owner or owner's representative for accurate future color matching.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: Benjamin Moore & Co. (United States), which is located at:<BR />101 Paragon Dr<BR />Montvale, NJ 07645<BR />Toll Free Tel: 866-708-9181<BR />Email: request info (info@benjaminmoore.com);Web: https://www.benjaminmoore.com | https://www.benjaminmoore.com/en-ca 
B.	Substitutions: Coronado Paint Company.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	LEED CRITERIA
A.	LEED Version 3 - 2009: EQ CR4.2 Low Emitting Materials: 1 Credit - Paint.
1.	All architectural paints and coatings used must meet the VOC limits of Green Seal Standard GS-11, 1993.
2.	Interior: 50 g/L VOC or less for Flats, 150 g/L VOC for Non Flats, and 200 g/L or less for primer sealers.
3.	Anti-Corrosive Coatings GC-03, 1997: Interior 250 g/L VOC or less any sheen.
4.	Clear wood finishes, floor coatings, stains, and shellacs applied to interior elements: District (SCAQMD) Rule 1113, Architectural Coatings, rules in effect on January 1, 2004.
5.	Clear wood finishes: varnish 350 g/L; lacquer 550 g/L; Floor coatings; 100 g/L, waterproofing sealers 250 g/L; sanding sealers 275 g/L; Shellacs: Clear 730 g/L; pigmented 550 g/L; Stains: 250 g/L.
B.	LEED Version 4:
1.	All interior paints and coatings wet-applied on site must meet the applicable VOC limits of the California Air Resources Board (CARB) 2007, Suggested Control Measure (SCM) for Architectural Coatings, or the South Coast Air Quality Management District (SCAQMD) Rule 1113, effective June 3, 2011 (50 g/L or less for interior flats, 100 g/L or less for non-flats, 150 g/L or less for non-flats high gloss).
2.	Ninety percent of all interior paints and coatings must be tested and determined compliant in accordance with California Department of Public Health (CDPH) Standard Method v1.1-2010.
2.3	MATERIALS - GENERAL
A.	Volatile Organic Compound (VOC) Content:
1.	Provide coatings that comply with the most stringent requirements specified in the following:
a.	40 CFR 59, Subpart D-National Volatile Organic Compound Emission Standards for Architectural Coatings.
b.	Determination of VOC Content: Testing and calculation in accordance with 40 CFR 59, Subpart D (EPA Method 24), exclusive of colorants added to a tint base and water added at project site; or other method acceptable to authorities having jurisdiction.
1)	All references to (0 g/L) are Zero VOCs according to EPA Method 24.
B.	Compatibility: Provide materials that are compatible with one another, and the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.
2.4	MIXING AND TINTING
A.	Except where specifically noted in this section, all paint shall be ready-mixed and pre-tinted. Agitate all paint prior to and during application to ensure uniform color, gloss, and consistency.
B.	A thinner addition shall not exceed the manufacturer's printed recommendations. Do not use kerosene or other organic solvents to thin water-based paints.
C.	Where paint is to be sprayed, thin according to manufacturer's current guidelines.
2.5	COMMERCIAL INTERIOR PAINT SYSTEMS - UNITED STATES
A.	Interior Concrete Ceilings:
1.	Dryfall:
a.	Acrylic Latex- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Acrylic Latex Flat N110 Line (46 g/L), MPI No.118.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Acrylic Latex Flat N110 Line (46 g/L), MPI No.118.
b.	Latex- Flat:
1)	Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Fist Coat: Benjamin Moore Latex Dry Fall Flat 395 (37.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 118.
3)	Second Coat: Benjamin Moore Latex Dry Fall Flat 395 (37.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 118.
c.	Alkyd Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 Line (368 g/L), MPI No. 55.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Alkyd Flat 105 Line (368 g/L), MPI No. 55.
d.	Latex- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Latex Dry Fall Eggshell 396 (43 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 155.
3)	Third Coat: Benjamin Moore Latex Dry Fall Eggshell 396 (43 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 155.
e.	Acrylic Latex- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Dry Fall Acrylic Latex Semi-Gloss 112 Line (68 g/L), MPI No. 226.
3)	Third Coat: Coronado Super Kote 5000 Dry Fall Acrylic Latex Semi-Gloss 112 Line (68 g/L), MPI No. 226.
f.	Latex- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Latex Dry Fall Semi-Gloss 397 (43 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 226.
3)	Third Coat: Benjamin Moore Latex Dry Fall Semi-Gloss 397 (43 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 226.
B.	Interior Masonry: Rough or Pitted:
1.	Block Filler Coatings:
a.	Vinyl Acrylic- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Block Filler Flat 244 (35 g/L).
3)	Third Coat: Benjamin Moore Block Filler Flat 244 (35 g/L).
b.	Latex Production Block Filler:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Latex Production Block Filler Flat 958 Line (37 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 4 and 4 X-Green.
3)	Third Coat: Coronado Super Kote 5000 Latex Production Block Filler Flat 958 Line (37 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 4 and 4 X-Green.
2.	Knockdown Coatings:
a.	Acrylic Latex- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green. 
2)	Second Coat: Benjamin Moore Acrylic Knockdown Flat 343 (45.5 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
b.	Acrylic Latex- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Acrylic Knockdown Satin 344 (46 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Acrylic Knockdown Satin 344 (46 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
3.	Architectural Paint Systems:
a.	Latex Easy to Apply- Matte: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
b.	Latex Easy to Clean- Matte:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
c.	Latex Ultra-Premium- Matte:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Aura Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore Aura Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
d.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
e.	Acrylic Latex Quick Turnaround- Flat: 
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
f.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
g.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
h.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
i.	Acrylic Latex Quick Turnaround- Low- Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
j.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
k.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
l.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
m.	Latex Professional Grade- Eggshell:
1)	First Coat: First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
n.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
o.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
p.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
q.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green. 
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green. 
r.	Acrylic Latex Quick Turn Around- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
s.	Latex Professional Grade- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
t.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
v.	Latex Premium- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
w.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
x.	Acrylic Latex Quick Turn Around- Semi Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
y.	Acrylic Latex Quick Turn Around- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
z.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
aa.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
ab.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ac.	Latex Easy to Clean- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Semi- Gloss N551 (96.1 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Semi- Gloss N551 (96.1 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 54, 141, 147.
ad.	Latex Premium- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
4.	Waterborne Alkyd- Semi- Gloss:
a.	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
b.	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
c.	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
5.	Waterborne Alkyd- High- Gloss:
a.	First Coat: Benjamin Moore Ultra Spec Hi-Build Masonry Block Filler 571 (45 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emissions Certified, MPI No. 4, 4 X-Green.
b.	Second Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
c.	Third Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
C.	Interior Masonry: Smooth:
1.	Knockdown Coatings:
a.	Acrylic/ Latex Knockdown- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Acrylic Knockdown Flat 343 (45.5 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Acrylic Knockdown Flat 343 (45.5 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
b.	Acrylic/ Latex Knockdown- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Acrylic Knockdown Satin 344 (46 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Acrylic Knockdown Satin 344 (46 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
2.	Block Filler:
a.	Vinyl Acrylic- Flat:
1)	First Coat: Consult with Benjamin Moore Representative to see if Primer Coat is needed.
2)	Second Coat: Benjamin Moore Block Filler Flat 244 (35 g/L).
3)	Third Coat: Benjamin Moore Block Filler Flat 244 (35 g/L).
b.	Vinyl Acrylic- Flat
1)	First Coat: Consult with Benjamin Moore Representative to see if Primer Coat is needed.
2)	Second Coat: Coronado Super Kote 5000 Latex Production Block Filler Flat Line 958 (37 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 4 and 4 X-Green.
3)	Third Coat: Coronado Super Kote 5000 Latex Production Block Filler Flat Line 958 (37 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 4 and 4 X-Green.
3.	Architectural Coatings:
a.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
b.	Latex Easy to Clean- Matte:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
c.	Latex Premium- Matte:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
d.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
e.	Acrylic Latex Quick Turn Around- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
f.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
g.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
h.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
i.	Acrylic Latex Quick Turn Around- Low Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
j.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
k.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
l.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
m.	Latex Professional Grade- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green
n.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
o.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
p.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
q.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
r.	Acrylic Latex Quick Turn Around- Satin
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
s.	Latex Professional Grade- Satin/ Pearl
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
t.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Latex Premium- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
v.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
w.	Acrylic Latex Value Driven- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
x.	Acrylic Latex Quick Turn Around- Satin:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Cat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
y.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
z.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
aa.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ab.	Latex Easy to Clean- Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Semi- Gloss N551 (96.1 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Semi- Gloss N551 (96.1 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 54, 141, 147.
ac.	Latex Premium- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
ad.	Waterborne Alkyd- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
ae.	Waterborne Alkyd- High- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec Masonry Interior/Exterior 100 percent Acrylic Sealer 608 (46 g/L), Qualifies for LEED v4 Credit, qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 3, 3 X-Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
D.	Interior Metal: Ferrous:
1.	Direct To Metal Coatings:
a.	Alkyd- Low Lustre:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Low Lustre P23 (370 g/L), Master Painters Institute No. 79.
3)	Third Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Low Lustre P23 (370 g/L), Master Painters Institute No. 79.
b.	Acrylic- Low Lustre:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 153, MPI High Performance No. 141.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 153, MPI High Performance No. 141.
c.	High- Performance Pre- Catalyzed Waterborne Epoxy- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
d.	Polyurethane Enamel- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Satin Finish 651 (381 g/L).
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Satin Finish 651 (381 g/L).
e.	High- Performance Mastic Urethane- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech DTM Mastic Urethane Satin V572 (246 g/L).
3)	Third Coat: Benjamin Moore Corotech DTM Mastic Urethane Satin V572 (246 g/L).
f.	High- Performance Acrylic Urethane- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Satin V392 (148 g/L).
3)	Third Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Satin V392 (148 g/L).
g.	Alkyd- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Semi- Gloss P24 (391 g/L), Master Painter Institute No. 81.
3)	Third Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Semi- Gloss P24 (391 g/L), Master Painter Institute No. 81.
h.	Acrylic- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi- Gloss HP29 (148 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 141, 153, 163.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi- Gloss HP29 (148 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 141, 153, 163.
i.	Polyurethane Enamel- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Semi- Gloss 13 (394.9 g/L).
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Semi- Gloss 13 (394.9 g/L).
j.	High- Performance Acrylic Enamel- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Semi- Gloss V331 (204 g/L), Masters Painters Institute MPI No. 153.
3)	Third Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Semi- Gloss V331 (204 g/L), Masters Painters Institute MPI No. 153.
k.	High- Performance Pre- Catalyzed Waterborne Epoxy- Semi- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
l.	Acrylic- High- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (147.7 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, Master Painters Institute MPI No. 114, 154, 164.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (147.7 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, Master Painters Institute MPI No. 114, 154, 164.
m.	Polyurethane Enamel- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Gloss 31 (381 g/L), Master Painters Institute MPI No. 48.
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Gloss 31 (381 g/L), Master Painters Institute MPI No. 48.
n.	High- Performance Mastic Urethane- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech DTM Mastic Urethane Gloss V570 (235 g/L).
3)	Third Coat: Benjamin Moore Corotech DTM Mastic Urethane Gloss V570 (235 g/L).
o.	High- Performance Acrylic Enamel Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Gloss V330 (220 g/L), Masters Painters Institute MPI No. 154, 164.
3)	Third Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Gloss V330 (220 g/L), Masters Painters Institute MPI No. 154, 164.
p.	High- Performance Acrylic Urethane Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Gloss V390 (146 g/L).
3)	Third Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Gloss V390 (146 g/L).
q.	High- Performance Quick Dry Acrylic- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Waterborne Enamel Quick Dry Acrylic Spray D.T.M. V300 (99.4 g/L), Masters Painters Institute MPI No. 114.
3)	Third Coat: Benjamin Moore Corotech Waterborne Enamel Quick Dry Acrylic Spray D.T.M. V300 (99.4 g/L), Masters Painters Institute MPI No. 114.
r.	High- Performance Water Reducible Alkyd Enamel- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Water Reducible Alkyd Enamel V210 (333 g/L).
3)	Third Coat: Benjamin Moore Corotech Water Reducible Alkyd Enamel V210 (333 g/L).
2.	Urethanes:
a.	High Performance Urethane- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V510 (315 g/L), Master Painters Institute MPI No. 83 and 174.
3)	Third Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V510 (315 g/L), Master Painters Institute MPI No. 83 and 174.
b.	High- Performance- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V500 (247.5 g/L), Masters Painters Institute MPI No. 72, 83, 105 and 205.
3)	Third Coat: Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V500 (247.5 g/L), Masters Painters Institute MPI No. 72, 83, 105 and 205.
c.	High- Performance Polyester- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Polyester Urethane Gloss V520 (332 g/L).
3)	Third Coat: Benjamin Moore Corotech Polyester Urethane Gloss V520 (332 g/L).
d.	High- Performance Waterborne- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Waterborne Urethane Gloss V540 (12.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 105 and 205 (Graffiti Protection Top-Coat), 256.
3)	Third Coat: Benjamin Moore Corotech Waterborne Urethane Gloss V540 (12.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 105 and 205 (Graffiti Protection Top-Coat), 256.
e.	High- Performance- High- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane High- Gloss V515 (447 g/L), Master Painters Institute MPI No. 83* (*with anti-skid additive), 105 (SHOP/OEM use) and 205.
3)	Third Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane High- Gloss V515 (447 g/L), Master Painters Institute MPI No. 83* (*with anti-skid additive), 105 (SHOP/OEM use) and 205.
3.	Architectural Paint Systems:
a.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
b.	Latex Easy to Clean- Matte: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
c.	Latex Premium- Matte: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
d.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
e.	Acrylic Latex Quick Turn Around- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
f.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
g.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
h.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
i.	Acrylic Latex Quick Turn Around- Low- Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
j.	Latex Professional Grade- Low- Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
k.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
l.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
m.	Latex Professional Grade- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
n.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
o.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
p.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
q.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
r.	Acrylic Latex Quick Turn Around- Satin:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
s.	Latex Professional Grade- Satin/ Pearl: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
t.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
v.	Latex Premium- Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
w.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
x.	Acrylic Latex Value Driven- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
y.	Acrylic Latex Quick Turn Around Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
z.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
aa.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
ab.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ac.	Latex Easy to Clean- Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
ad.	Latex Premium- Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
ae.	Waterborne Alkyd- Semi-Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
E.	Interior Metal: Non-Ferrous:
1.	Direct To Metal Coatings:
a.	Alkyd- Low Lustre:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Low Lustre P23 (370 g/L), Master Painters Institute No. 79.
3)	Third Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Low Lustre P23 (370 g/L), Master Painters Institute No. 79.
b.	Acrylic- Low Lustre: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 153, MPI High Performance No. 141.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Low Lustre Enamel HP25 (145 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters 
c.	High- Performance Pre- Catalyzed Waterborne Epoxy-Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
d.	Polyurethane Enamel- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Satin Finish 651 (381 g/L).
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Satin Finish 651 (381 g/L).
e.	High- Performance Mastic Urethane- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech DTM Mastic Urethane Satin V572 (246 g/L).
3)	Third Coat: Benjamin Moore Corotech DTM Mastic Urethane Satin V572 (246 g/L).
f.	High- Performance Acrylic Urethane- Satin: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Satin V392 (148 g/L).
3)	Third Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Satin V392 (148 g/L).
g.	Alkyd- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Semi- Gloss P24 (391 g/L), Master Painter Institute No. 81.
3)	Third Coat: Benjamin Moore Super Spec HP D.T.M. Alkyd Semi- Gloss P24 (391 g/L), Master Painter Institute No. 81.
h.	Acrylic- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi- Gloss HP29 (148 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 141, 153, 163.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Semi- Gloss HP29 (148 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 141, 153, 163.
i.	Polyurethane Enamel- Semi- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Semi- Gloss 13 (394.9 g/L).
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Semi- Gloss 13 (394.9 g/L).
j.	High- Performance Acrylic Enamel Semi- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Semi- Gloss V331 (204 g/L), Masters Painters Institute MPI No. 153.
3)	Third Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Semi- Gloss V331 (204 g/L), Masters Painters Institute MPI No. 153.
k.	High- Performance Pre- Catalyzed Waterborne Epoxy- Semi- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
l.	Acrylic- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (147.7 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, Master Painters Institute MPI No. 114, 154, 164.
3)	Third Coat: Benjamin Moore Ultra Spec HP D.T.M. Acrylic Gloss Enamel HP28 (147.7 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, Master Painters Institute MPI No. 114, 154, 164.
m.	Polyurethane Enamel- Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Gloss 31 (381 g/L), Master Painters Institute MPI No. 48.
3)	Third Coat: Coronado Rust Scat Polyurethane Int/Ext Enamel Coating Gloss 31 (381 g/L), Master Painters Institute MPI No. 48.
n.	High- Performance Mastic Urethane- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech DTM Mastic Urethane Gloss V570 (235 g/L).
3)	Third Coat: Benjamin Moore Corotech DTM Mastic Urethane Gloss V570 (235 g/L).
o.	High- Performance Acrylic Enamel- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Gloss V330 (220 g/L), Masters Painters Institute MPI No. 154, 164.
3)	Third Coat: Benjamin Moore Corotech Acrylic D.T.M. Enamel Gloss V330 (220 g/L), Masters Painters Institute MPI No. 154, 164.
p.	High- Performance Acrylic Urethane Gloss: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Gloss V390 (146 g/L).
3)	Third Coat: Benjamin Moore Corotech Command Waterborne Acrylic Urethane Gloss V390 (146 g/L).
q.	High- Performance Quick Dry Acrylic- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Waterborne Enamel Quick Dry Acrylic Spray D.T.M. V300 (99.4 g/L), Masters Painters Institute MPI No. 114.
3)	Third Coat: Benjamin Moore Corotech Waterborne Enamel Quick Dry Acrylic Spray D.T.M. V300 (99.4 g/L), Masters Painters Institute MPI No. 114.
r.	High- Performance Water Reducible Alkyd Enamel- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Water Reducible Alkyd Enamel V210 (333 g/L).
3)	Third Coat: Benjamin Moore Corotech Water Reducible Alkyd Enamel V210 (333 g/L).
s.	Latex High Gloss Enamel- High- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 114 and 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 114 and 114 X-Green.
t.	Latex High Gloss Enamel- High- Glos:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 114 and 114 X-Green.
3)	Third Coat: Benjamin Moore Impervex Latex High Gloss Enamel W309 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 114 and 114 X-Green.
2.	Urethanes
a.	High- Performance- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V510 (315 g/L), Master Painters Institute MPI No. 83 and 174.
3)	Third Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V510 (315 g/L), Master Painters Institute MPI No. 83 and 174.
b.	High- Performance- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V500 (247.5 g/L), Masters Painters Institute MPI No. 72, 83, 105 and 205.
3)	Third Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane Gloss V500 (247.5 g/L), Masters Painters Institute MPI No. 72, 83, 105 and 205.
c.	High- Performance Polyester- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Polyester Urethane Gloss V520 (332 g/L).
3)	Third Coat: Benjamin Moore Corotech Polyester Urethane Gloss V520 (332 g/L).
d.	High- Performance Waterborne- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Waterborne Urethane Gloss V540 (12.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 105 and 205 (Graffiti Protection Top-Coat), 256.
3)	Third Coat: Benjamin Moore Corotech Waterborne Urethane Gloss V540 (12.9 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, MPI No. 105 and 205 (Graffiti Protection Top-Coat), 256.
e.	High- Performance- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane High- Gloss V515 (447 g/L), Master Painters Institute MPI No. 83* (*with anti-skid additive), 105 (SHOP/OEM use) and 205.
3)	Third Coat: Benjamin Moore Corotech Aliphatic Acrylic Urethane High- Gloss V515 (447 g/L), Master Painters Institute MPI No. 83* (*with anti-skid additive), 105 (SHOP/OEM use) and 205.
3.	Architectural Coatings:
a.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
b.	Latex Easy to Clean- Matte: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
c.	Latex Premium- Matte:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
d.	Acrylic Latex Value Driven- Flat: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
e.	Acrylic Latex Quick Turn Around- Flat: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
f.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
g.	Latex Zero VOCs and Zero Emissions- Flat: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
h.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
i.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission.
2)	Second Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
j.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
k.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
l.	Latex Professional Grade- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
m.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
n.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
o.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
p.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
q.	Acrylic Latex Quick Turn Around- Satin:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
r.	Latex Professional Grade- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
s.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
t.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
u.	Latex Premium- Satin:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
v.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit.
w.	Acrylic Latex Value Driven- Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
x.	Acrylic Latex Quick Turn Around- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
y.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
z.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
aa.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ab.	Latex Easy to Clean- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
ac.	Latex Premium- Semi- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
ad.	Waterborne Alkyd- Semi-Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
ae.	Waterborne Alkyd- High- Gloss: 
1)	First Coat: Benjamin Moore Ultra Spec HP Acrylic Metal Primer HP04 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified Master Painters Institute MPI No. 107, 107 X-Green, 134.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
F.	Interior Drywall:
1.	Architectural Paint Systems:
a.	Scuff Resistance- Matte:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
b.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
c.	Latex Easy to Clean- Matte:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
d.	Latex High Humidity Environments- Matte:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
e.	Latex Premium- Matte:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
f.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
g.	Acrylic Latex Quick Turn Around- Flat: 
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
h.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
i.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
j.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
k.	Ceiling Paint- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Benjamin Moore Muresco Ceiling White 258 (47.8 g/L).
3)	Third Coat: Benjamin Moore Muresco Ceiling White 258 (47.8 g/L).
l.	Ceiling Paint- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Benjamin Moore Waterborne Ceiling Paint 508 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Waterborne Ceiling Paint 508 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
m.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
n.	Acrylic Latex Quick Turn Around- Low Sheen/ Eggshell:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
o.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
p.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
q.	Latex Professional Grade- Eggshell
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
r.	Scuff Resistance- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
s.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
t.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
v.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
w.	Acrylic Latex Quick Turn Around- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
x.	Latex Professional Grade- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
y.	Scuff Resistance- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
z.	Latex Easy to Apply- Satin/ Pearl: 
1)	First Coat: First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
aa.	Latex High Humidity Environments- Satin:
1)	First Coat: First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
3)	Third Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
ab.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
ac.	Latex Premium- Satin: 
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
ad.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
ae.	Acrylic Latex Value Driven- Semi-Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
af.	Acrylic Latex Quick Turn Around- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for product recommendations.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
ag.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
ah.	Scuff Resistance- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
ai.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
aj.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ak.	Latex Easy to Clean- Semi-Gloss:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
al.	Latex Premium- Semi- Gloss:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
am.	Waterborne Alkyd- Semi- Gloss: 
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
an.	Waterborne Alkyd- High Gloss:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
2.	High Performance Coatings
a.	High- Performance Coating- Eggshell:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
b.	High- Performance Coating- Semi- Gloss:
1)	First Coat: Benjamin Moore Drywall Primer 380 (11.4 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 50.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
G.	Interior Plaster (Cured):
1.	Architectural Paint Systems:
a.	Scuff Resistance- Matte:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
b.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
c.	Latex Easy to Clean- Matte:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
d.	Latex Premium- Premium: 
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
e.	Latex High Humidity Environments- Matte:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
f.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
g.	Acrylic Latex Quick Turn Around- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
h.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
i.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
j.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
k.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
l.	Acrylic Latex Quick Turn Around- Low Sheen/ Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
m.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
n.	Latex Professional Grade- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green
o.	Scuff Resistance- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
p.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
q.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
r.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
s.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
t.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green. Or Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
u.	Architectural Paint Systems- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
v.	Latex Professional Grade- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
w.	Scuff Resistance- Satin/ Pearl:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
x.	Latex High Humidity Environments- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
3)	Third Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
y.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
z.	Latex Premium- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
aa.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
ab.	Acrylic Latex Value Driven- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
ac.	Acrylic Latex Quick Turn Around- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
ad.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
ae.	Scuff Resistance- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
af.	Latex Zero VOCs and Zero Emissions- Semi- Gloss:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
ag.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ah.	Latex Easy to Clean- Semi- Gloss: 
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
ai.	Latex Premium- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
aj.	Waterborne Alkyd- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
ak.	Waterborne Alkyd- High- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior/Exterior Alkyd High Gloss N794 (44 g/L), MPI No.157.
2.	High- Performance Coatings:
a.	High- Performance Pre- Catalyzed Waterborne Epoxy- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
b.	High- Performance Pre- Catalyzed Waterborne Epoxy- Semi- Gloss: 
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
H.	Interior Wood and Engineered Wood Products:
1.	Architectural Paint Systems:
a.	Scuff Resistance- Matte:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Matte Finish C484 (49.5 g/L).
b.	Latex Easy to Apply- Matte:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Matte N624 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
c.	Latex Easy to Clean- Matte:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Matte N548 (49.6 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
d.	Latex High Humidity Environments- Matte:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore AURA Bath and Spa Waterborne Interior Paint and Primer Matte 532 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
e.	Latex Premium- Matte:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Matte N522 (1.8 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 142, 143, 142 X-Green, 143 X-Green.
f.	Acrylic Latex Value Driven- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Flat 301 Line (42 g/L).
g.	Acrylic Latex Quick Turn Around- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Flat 28 Line (50 g/L), MPI No. 53.
h.	Latex Professional Grade- Flat:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Flat Finish T535 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 53, 53 X-Green, 143, 143 X-Green.
i.	Latex Zero VOCs and Zero Emissions- Flat:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Flat Finish N373 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 53, 53 X-Green, 142, 143, 143 X-Green.
j.	Latex Easy to Clean- Flat:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Flat N547 (47.9 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 142, 143, MPI X-Green 142, 143.
k.	Ceiling Paint- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Muresco Ceiling White 258 (47.8 g/L).
3)	Third Coat: Benjamin Moore Muresco Ceiling White 258 (47.8 g/L).
l.	Ceiling Paint- Flat:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Waterborne Ceiling Paint 508 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
m.	Acrylic Latex Quick Turn Around- Low Sheen Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Low-Sheen Eggshell 1130 (95.8 g/L), MPI No. 44.
n.	Latex Professional Grade- Low Sheen:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Low Sheen Eggshell Finish T537 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, No. 44, 44 X-Green, 138, 138 X-Green, 144, 144 X-Green.
o.	Acrylic Latex Value Driven- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Eggshell 302 Line (43.3 g/L).
p.	Acrylic Latex Quick Turn Around- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Eggshell 30 Line (50 g/L), MPI No. 44.
q.	Latex Professional Grade- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Eggshell Finish T538 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. No. 52, 52 X- Green, 139, 139 X-Green, 145, 145 X-Green.
r.	Scuff Resistance- Eggshell:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Eggshell Finish C485 (46.8 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
s.	Latex Zero VOCs and Zero Emissions- Eggshell:
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Eggshell Finish N374 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 52, 52 X-Green, 139.
t.	Latex Easy to Apply- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Eggshell N626 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
u.	Latex Easy to Clean- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Eggshell N549 (47.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI 138, MPI X-Green 138.
v.	Latex Premium- Eggshell:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint Eggshell N524 (1.5 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 138, 138 X-Green.
w.	Architectural Paint Systems- Satin:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Satin 1160 Line (95 g/L), MPI No. 43.
x.	Latex Professional Grade- Satin:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Satin/ Pearl Finish T545 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 43, 43 X-Green, 140, 140 X-Green, 146, 146 X-Green.
y.	Scuff Resistance- Satin:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Satin Finish 486 (95 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
z.	Latex High Humidity Environments- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
3)	Third Coat: Benjamin Moore Kitchen and Bath 100 percent Acrylic Satin Finish W322 (37.1 g/L).
aa.	Latex Easy to Apply- Satin/ Pearl:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Satin/ Pearl N628 (0 g/L), Eligible for LEED v4, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ab.	Latex Easy to Clean- Pearl:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N550 (46.2 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit.
ac.	Latex Premium- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Satin N526 (2.4 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 140, 140 X-Green.
ad.	Waterborne Alkyd- Satin:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
3)	Third Coat: Benjamin Moore ADVANCE Interior Paint- Satin 792 (48 g/L), Qualifies for LEED v4, Qualifies for CHPS low emitting credit. 
ae.	Acrylic Latex Value Driven- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
3)	Third Coat: Coronado Super Kote 3000 Acrylic Latex Semi-Gloss 304 Line (94 g/L).
af.	Acrylic Latex Quick Turn Around- Semi- Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
3)	Third Coat: Coronado Super Kote 5000 Acrylic Latex Enamel Semi-Gloss 32 Line (50 g/L), MPI No. 54.
ag.	Latex Professional Grade- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
3)	Third Coat: Benjamin Moore Ultra Spec 500 Interior Semi- Gloss Finish T546 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS Low Emitting Credit, MPI No. 54, 54 X-Green, 141, 141 X-Green, 147, 147 X-Green.
ah.	Scuff Resistance- Semi- Gloss:
1)	First Coat: Benjamin Moore Ultra Spec 500 Interior Latex Primer N534 (0 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
2)	Second Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
3)	Third Coat: Benjamin Moore Ultra Spec Scuff-X Interior Semi- Gloss Finish 487 (37.7 g/L), Eligible for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified.
ai.	Latex Zero VOCs and Zero Emissions- Semi-Gloss: 
1)	First Coat: Benjamin Moore Eco Spec Interior Latex Primer N372 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit.
2)	Second Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
3)	Third Coat: Benjamin Moore Eco Spec Interior Latex Semi-Gloss Finish N376 (0 g/L), Eligible for LEED v4 Credit, CDPH v1 Emissions Certified, Qualifies for CHPS low emitting credit, Certified Asthma and Allergy Friendly, MPI No. 54, 54 X-Green, 141.
aj.	Latex Easy to Apply- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
3)	Third Coat: Benjamin Moore ben Premium Interior Acrylic Paint and Primer Semi-Gloss N627 (0 g/L), Eligible for LEED v4 Credit, CDPH Emissions Certified, Qualifies for CHPS low emitting credit.
ak.	Latex Easy to Clean- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
3)	Third Coat: Benjamin Moore Regal Select Interior Paint Pearl N551 (96.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, Master Painters Institute MPI No. 54, 141, 147.
al.	Latex Premium- Semi- Gloss:
1)	First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
3)	Third Coat: Benjamin Moore AURA Interior Paint- Semi-Gloss N528 (3.1 g/L), Eligible for LEED v4, CDPH Emissions Certified, Eligible for CHPS low emitting credit, MPI No. 141, 141 X-Green.
am.	Waterborne Alkyd- Semi- Gloss:
1)	First Coat: First Coat: Benjamin Moore Fresh Start Undercoater and Primer/ Sealer 032 (338 g/L), MPI No. 45, 136. Or Benjamin Moore Fresh Start High- Hiding All Purpose Primer 046 (48 g/L), Qualifies for LEED v4 Credit, Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Master Painters Institute MPI No. 6, 17, 17 X-Green, 39, 50, 50 X-Green, 137, 137 X Green.
2)	Second Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
3)	Third Coat: Benjamin Moore ADVANCE Waterborne Interior Alkyd Semi-Gloss 793 (43 g/L).
2.	High Performance Coatings:
a.	High- Performance Pre- Catalyzed Waterborne Epoxy- Eggshell:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Eggshell V342 (75 g/L), Qualifies for CHPS low emitting credit, CDPH v1 Emission Certified, Masters Painters Institute MPI No.151.
b.	High- Performance Pre- Catalyzed Waterborne Epoxy- Semi-Gloss:
1)	First Coat: Consult TDS or Benjamin Moore Representative for Primer Coat information.
2)	Second Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153.
3)	Third Coat: Benjamin Moore Corotech Pre- Catalyzed Waterborne Epoxy Semi- Gloss V341 (75 g/L), Eligible for LEED v4 Credit, CDPH v1 Emission Certified, Qualifies for CHPS low emitting credit, Masters Painters Institute MPI No. 141, 153. 
PART 3    EXECUTION
3.1	EXAMINATION
A.	The Contractor shall review the product manufacturer's special instructions for surface preparation, application, temperature, re-coat times, and product limitations.
B.	The Contractor shall review product health and safety precautions listed by the manufacturer.
C.	The Contractor shall be responsible for enforcing on site health and safety requirements associated with the Work.
D.	Do not begin installation until the substrates have been properly prepared.
E.	Ensure that surfaces to receive paint are dry immediately prior to application.
F.	Ensure that moisture-retaining substrates to receive paint have moisture content within tolerances allowed by coating manufacturer. Where exceeding the following values, promptly notify Architect and obtain direction before beginning work.
1.	Concrete and Masonry: 3-5 percent. Allow new concrete to cure a minimum of 28 days.
2.	Exterior Wood: 17 percent.
3.	Interior Wood: 15 percent.
4.	Interior Finish Detail Woodwork, Including Trim, and Casework: 10 percent.
5.	Plaster and Gypsum: 15 percent.
6.	Concrete Slab-On-Grade: Perform calcium chloride test over 24 hour period or other acceptable test to manufacturer. Verify acceptable moisture transmission and pH levels.
G.	Examine surfaces to receive coatings for surface imperfections and contaminants that could impair performance or appearance of coatings, including but not limited to, loose primer, rust, scale, oil, grease, mildew, algae, or fungus, stains or marks, cracks, indentations, or abrasions.
H.	Correct conditions that could impair performance or appearance of coatings in accordance with specified surface preparation procedures before proceeding with coating application.
3.2	PREPARATION - GENERAL
A.	Clean surfaces thoroughly prior to coating application.
B.	Do not start work until surfaces to be finished are in proper condition to produce finished surfaces of uniform, satisfactory appearance.
C.	Stains and Marks: Remove completely, if possible, using materials and methods recommended by coating manufacturer; cover stains and marks which cannot be completely removed with isolating primer or sealer recommended by coating manufacturer to prevent bleed-through.
D.	Remove Mildew, Algae, and Fungus using materials and methods recommended by coating manufacturer.
E.	Remove dust and loose particulate matter from surfaces to receive coatings immediately prior to coating application.
F.	Remove or protect adjacent hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items not indicated to receive coatings.
G.	Move or protect equipment and fixtures adjacent to surfaces indicated to receive coatings to allow application of coatings.
H.	Protect adjacent surfaces not indicated to receive coatings.
I.	Prepare surfaces in accordance with manufacturer's instructions for specified coatings and indicated materials, using only methods and materials recommended by coating manufacturer.
3.3	SURFACE PREPARATION
A.	Concrete and Concrete Masonry: Clean surfaces free of loose particles, sand, efflorescence, laitance, form oil, curing compounds, and other substances which could impair coating performance or appearance.
B.	Concrete Floors: Remove contaminants which could impair coating performance or appearance. Verify moisture transmission and alkaline-acid balance recommended by coating manufacturer; mechanically abrade surface to achieve 80-100 grit medium-sandpaper texture.
C.	Existing Coatings:
1.	Remove surface irregularities by scraping or sanding to produce uniform substrate for coating application; apply one coat primer of type recommended by coating manufacturer for maximum coating adhesion.
2.	If presence of lead in existing coatings is suspected, cease surface preparation, and notify Architect immediately.
D.	Gypsum Board: Repair cracks, holes, and other surface defects with joint compound to produce surface flush with adjacent surfaces.
E.	Masonry Surfaces - Restored: Remove loose particles, sand, efflorescence, laitance, cleaning compounds and other substances that could impair coating performance or appearance.
F.	Metals - Aluminum, Mill-Finish: Clean and etch surfaces with a phosphoric acid-water solution or water based industrial cleaner. Flush with clean water and allow to dry, before applying primer coat.
G.	Metals - Copper: Clean surfaces with pressurized steam, pressurized water, or solvent washing.
H.	Metals - Ferrous, Unprimed: Remove rust or scale, if present, by wire brush cleaning, power tool cleaning, or sandblast cleaning; remove grease, oil, and other contaminants which could impair coating performance or appearance by solvent cleaning, with phosphoric-acid solution cleaning of welds, bolts, and nuts; spot-prime repaired welds with specified primer.
I.	Metals - Ferrous, Shop-Primed: Remove loose primer and rust, if present, by scraping and sanding, feathering edges of cleaned areas to produce uniform flat surface; solvent-clean surfaces and spot-prime bare metal with specified primer, feathering edges to produce uniform flat surface.
J.	Metals - Galvanized Steel (not passivated): Clean with a water-based industrial strength cleaner, apply an adhesion promoter followed by a clean water rinse. Alternately, wipe down surfaces using clean, lint-free cloths saturated with xylene or lacquer thinner; followed by wiping the surface dry using clean, lint-free cloths.
K.	Metals - Galvanized Steel, Passivated: Clean with water-based industrial strength cleaner. After the surface has been prepared, apply recommended primer to a small area. Allow primer to cure for 7 days, and test adhesion using the "crosshatch adhesion tape test" method in accordance with ASTM D 3359. If the adhesion of the primer is positive, proceed with a recommended coating system for galvanized metal.
L.	Metals - Stainless Steel: Clean surfaces with pressurized steam, pressurized water, or water-based industrial cleaner.
M.	Plaster: Repair cracks, holes and other surface defects as required to maintain proper surface adhesion. Apply patching plaster or Joint compound and sand to produce surface flush with adjacent undamaged surface. Allow a full cure prior to coating application as recommended by the patching compound manufacturer's recommendations.
N.	Polyvinyl Chloride (PVC) Pipe: remove contaminants and markings with denatured alcohol scuff sand and wipe with solvent for maximum adhesion. Test adhesion before starting the job.
O.	Fiberglass Doors - remove contaminants with cleaning solvent (alcohol) scuff sand and wipe. Test adhesion of primer before starting job.
P.	Textiles - Insulated Coverings, Canvas or Cotton: Clean using high-pressure air and solvent of type recommended for material.
Q.	Wood:
1.	Seal knots, pitch streaks, and sap areas with sealer recommended by coating manufacturer; fill nail recesses and cracks with filler recommended by coating manufacturer; sand surfaces smooth.
2.	Remove mill marks and ink stamped grade marks.
3.	Apply primer coat to back of wood trim and paneling.
R.	Wood Doors: Seal door tops and bottoms prior to finishing.
S.	Wood Doors - Field-Glazed Frames and Sash: Prime or seal glazing channels prior to glazing.
3.4	APPLICATION - GENERAL
A.	Application of primers, paints, stains, or coatings, by the Contractor, will serve as acceptance that surfaces were properly prepared in accordance with the manufacturer's recommendation.
B.	Apply each coat to uniform coating thickness in accordance with manufacturer's instructions, not exceeding manufacturer's specified maximum spread rate for indicated surface; thins, brush marks, roller marks, orange-peel, or other application imperfections are not permitted.
C.	Allow manufacturer's specified drying time, and ensure correct coating adhesion, for each coat before applying next coat.
D.	Inspect each coat before applying the next coat; touch-up surface imperfections with coating material, feathering, and sanding if required; touch-up areas to achieve flat, uniform surface without surface defects visible from 5 feet (1.5 m).
E.	Remove dust and other foreign materials from substrate immediately prior to applying each coat.
F.	Where paint application abuts other materials or other coating color, terminate coating with a clean sharp termination line without coating overlap.
G.	Where color changes occur between adjoining spaces, through framed openings that are of same color as adjoining surfaces, change color at outside stop corner nearest to face of closed door.
H.	Re-prepare and re-coat unsatisfactory finishes; refinish entire area to corners or other natural terminations.
3.5	CLEANING
A.	Clean excess coating materials, and coating materials deposited on surfaces not indicated to receive coatings, as construction activities of this section progress; do not allow to dry.
B.	Re-install hardware, electrical equipment plates, mechanical grilles and louvers, lighting fixture trim, and other items that have been removed to protect from contact with coatings.
C.	Reconnect equipment adjacent to surfaces indicated to receive coatings.
D.	Relocate to original position equipment and fixtures that have been moved to allow application of coatings.
E.	Remove protective materials.
3.6	PROTECTION AND REPAIR
A.	Protect completed coating applications from damage by subsequent construction activities until completion of painting project.
B.	Touch-up coatings damaged by subsequent construction activities.

END OF SECTION