SECTION 09 90 00

PAINTS AND COATINGS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2004 -  2024 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Exterior Paint Systems: Surface preparation and field painting of exposed exterior items and surfaces.
B.	Exterior stain and natural finish woodwork systems.
C.	Interior Paint Systems: Surface preparation and field painting of exposed interior items and surfaces.
D.	Interior stain and natural finish woodwork systems.
E.	Exterior High Performance Coating Systems: Surface preparation and field application of exterior high-performance coating systems to items and surfaces scheduled.
F.	Interior High Performance Coating Systems: Surface preparation and field application of interior high-performance coating systems to items and surfaces scheduled.
1.2	RELATED SECTIONS
A.	Section 03 30 00 - Cast-in-Place Concrete.
B.	Section 05 12 13 - Architecturally-Exposed Structural Steel Framing.
C.	Section 05 50 00 - Metal Fabrications.
D.	Section 06 20 00 - Finish Carpentry.
E.	Section 08 11 13.13 - Standard Hollow Metal Doors and Frames.
F.	Section 09 21 16.33 - Gypsum Board Area Separation Wall Assemblies.
G.	Section 22 05 00 - Common Work Results for Plumbing.
H.	Section 26 05 00 - Common Work Results for Electrical.
1.3	REFERENCES
A.	American Society for Testing and Materials (ASTM) D 16 - Standard Terminology for Paint, Related Coatings, Materials, and Applications.
B.	Steel Structures Painting Council (SSPC) SP6 - Commercial Blast Cleaning Procedures.
C.	Steel Structures Painting Council (SSPC) SP10 - Near White Blast Cleaning Procedure.
1.4	DEFINITIONS
A.	General: Standard coating terms in accordance with ASTM D523.
1.	Gloss Level 1 (Flat): Not more than 5 units at 60 degrees and 10 units at 85 degrees, in accordance with ASTM D523.
2.	Gloss Level 2 (Low Sheen): Not more than 10 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.
3.	Gloss Level 3 (Eggshell): 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.
4.	Gloss Level 4 (Satin): 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, in accordance with ASTM D523.
5.	Gloss Level 5 (Semi-Gloss): 35 to 70 units at 60 degrees, in accordance with ASTM D523.
6.	Gloss Level 6 (Gloss): 70 to 85 units at 60 degrees, in accordance with ASTM D523.
7.	Gloss Level 7 (High-Gloss): More than 85 units at 60 degrees, in accordance with ASTM D523.
B.	Environments: The following terms distinguish between different corrosive exposures:
1.	Severe Environments: Highly corrosive industrial atmospheres. Sustained exposure to high humidity and condensation and with frequent cleaning using strong chemicals. Environments with heavy concentrations of strong chemical fumes and frequent splashing and spilling of harsh chemical products are severe environments.
2.	Moderate Environments: Corrosive industrial atmospheres with intermittent exposure to high humidity and condensation, occasional mold and mildew development, and regular cleaning with strong chemicals. Environments with exposure to heavy concentrations of chemical fumes and occasional splashing and spilling of chemical products are moderate environments.
3.	Mild Environment: industrial atmospheres with normal exposure to moderate humidity and condensation, occasional mold and mildew development, and infrequent cleaning with strong chemicals. Environments with low levels of mild chemical fumes and occasional splashing and spilling of chemical products are mild environments. Normal outdoor weathering is also considered a mild environment.
1.5	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	Product Data: For each paint system indicated, including:
1.	Material List: An inclusive list of required coating materials. Indicate each material and cross reference specific coating, finish system, and application. Identify each material by manufacturer's catalog number and general classification.
2.	Preparation instructions and recommendations.
3.	Manufacturer's Information: Manufacturer's technical information, including label analysis and instructions for handling, storing, and applying each coating material.
C.	Selection Samples: For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.
D.	Verification Samples: For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.
1.6	QUALITY ASSURANCE
A.	Installer Qualifications: A firm or individual experienced in applying paints and coatings similar in material, design, and extent to those indicated for this Project, whose work has resulted in applications with a record of successful in-service performance.
B.	Obtain block fillers and primers for each coating system from the same manufacturer as the finish coats.
C.	Paint exposed surfaces. If an item or a surface is not specifically mentioned, paint the item, or surface the same as similar adjacent materials or surfaces. If a color of finish is not indicated, Architect will select from standard colors and finishes available.
D.	Do not paint prefinished items, concealed surfaces, finished metal surfaces, operating parts, and labels.
E.	Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and application workmanship.
1.	Finish areas designated by Architect.
2.	Do not proceed with remaining work until workmanship, color, and sheen are approved by Architect.
3.	Refinish mock-up area as required to produce acceptable work.
1.7	DELIVERY, STORAGE, AND HANDLING
A.	Deliver materials to Project site in manufacturer's original, unopened packages and containers bearing manufacturer's name and label:
B.	Store materials not in use in tightly covered containers in a well-ventilated area at a minimum ambient temperature of 45 deg F (7 deg C). Maintain storage containers in a clean condition, free of foreign materials and residue.
1.8	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's absolute limits.
B.	Apply waterborne paints only when temperatures of surfaces to be painted and surrounding air are between 50 and 90 deg F (10 and 32 deg C).
C.	Apply solvent-thinned paints only when temperatures of surfaces to be painted and surrounding air are between 45 and 95 deg F (7 and 35 deg C).
D.	Do not apply paint in snow, rain, fog, or mist: or when relative humidity exceeds 85 percent: or at temperatures less than 5 deg F (3 deg C) above the dew point: or to damp or wet surfaces.
1.	Painting may continue during inclement weather if surfaces and areas to be painted are enclosed and heated within temperature limits specified by manufacturer during application and drying periods.
1.9	EXTRA MATERIALS
A.	Furnish extra paint materials from the same production run as the materials applied in the quantities described below. Package with protective covering for storage and identify with labels describing contents. Deliver extra materials to Owner.
B.	Quantity: Furnish Owner with an additional three percent, but not less than 1 gal (3.8 l) or 1 case, as appropriate, of each material and color applied.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: PPG Architectural Finishes, Incorporated - PPG Paints, which is located at:<BR />400 Bertha Lamme Dr.<BR />Cranberry Township, PA 16066<BR />Toll Free Tel: 888-PPG-IDEA<BR />Fax: 888-434-3127<BR />Email: request info (brian.joyce@ppg.com);Web: https://www.ppgpaints.com 
1.	Basis of Design: PPG Paints as manufactured and supplied by PPG Architectural Finishes, Incorporated.
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	PAINT MATERIALS GENERAL
A.	Material Compatibility: Provide block fillers, primers, and finish-coat materials that are compatible with one another and with the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.
B.	VOC Classification: Provide high-performance coating materials, including primers, undercoats, and finish-coat materials, that meet the applicable local, state, or federal VOC requirements.
C.	Color: Refer to Finish Schedule and Paint Legend for paint colors.
2.3	EXTERIOR PAINT FINISH SYSTEMS
A.	Acrylic Finish: Two finish coats over a primer.
1.	Substrate:
a.	Concrete, stucco, and brick masonry; other than concrete masonry units.
b.	Mineral-fiber-reinforced cement panels.
c.	Exterior gypsum soffit board.
2.	Primer:
a.	PPG Paints. Seal Grip Gripper Interior/Exterior 100 Percent Acrylic Latex Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	PPG Paints. Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI. Applied Dry Film Thickness: 1.4 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House Paint Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Flat, 72-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 1 High Build Acrylic Finish:
a.	PPG Paints. Perma-Crete High Build 100 Percent Acrylic Topcoat, 4-22XI Series. Applied Dry Film Thickness: 3.2 mils min.
5.	Exterior Gloss Level 2 Acrylic Finish:
a.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
6.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mil min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Satin, 76-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
7.	Exterior Gloss Level 3 and 4 High Build Acrylic Finish:
a.	PPG Paints. Perma-Crete High Build 100 Percent Acrylic Topcoat, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
8.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex Paint, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Semi-Gloss, 78-45XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
9.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
10.	Exterior Acrylic Texture Finish:
a.	PPG Paints. Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
11.	Exterior Elastomeric Coating:
a.	PPG Paints. Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
B.	Acrylic Finish: Two finish coats over a block filler.
1.	Substrate: Exterior Concrete Masonry Units:
2.	Block Filler: Acrylic:
a.	PPG Paints. Speedhide Interior/Exterior Masonry Latex Block Filler, 6-7. Applied Dry Film Thickness: 7.1 mils min.
b.	PPG Paints. Speedhide Interior/Exterior Masonry Hi-Fill Latex Block Filler, 6-15XI. Applied Dry Film Thickness: 8.0 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House Paint Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Flat, 72-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 1 High Build Acrylic Finish:
a.	PPG Paints. Perma-Crete High Build 100 Percent Acrylic Topcoat, 4-22XI Series. Applied Dry Film Thickness: 3.2 mils min.
5.	Exterior Gloss Level 2 Acrylic Finish:
a.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
6.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mil min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Satin, 76-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
7.	Exterior Gloss Level 3 and 4 High Build Acrylic Finish:
a.	PPG Paints. Perma-Crete High Build 100 Percent Acrylic Topcoat, 4-422 Series. Applied Dry Film Thickness: 3.0 mils min.
8.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex Paint, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Semi-Gloss, 78-45XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
9.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
10.	Exterior Acrylic Texture Finish:
a.	PPG Paints. Perma-Crete 100 Percent Acrylic Texture Coating, 4-50 Series. Applied Dry Film Thickness: 6.8 mils min.
11.	Exterior Elastomeric Coating:
a.	PPG Paints. Perma-Crete Pitt-Flex Elastomeric Coating, 4-110XI Series. Applied Dry Film Thickness: 5.4 mils min.
C.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Smooth wood siding.
b.	Wood trim.
c.	Plywood.
d.	Smooth exterior wood surfaces.
2.	Primer:
a.	PPG Paints. Seal Grip Gripper Interior/Exterior 100 Percent Acrylic Latex Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	PPG Paints. Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Seal Grip Interior/Exterior Alkyd Primer, 17-941NF. Applied Dry Film Thickness: 2.2 mils min.
3.	Exterior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House Paint Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Flat, 72-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 2 Acrylic Finish:
a.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
5.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Satin, 76-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
6.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex Paint, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Semi-Gloss, 78-45XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
7.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
8.	Exterior Gloss Level 6 Alkyd Enamel Low Odor Finish:
a.	PPG Paints. Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
D.	Acrylic or Alkyd Finish: Two finish coats over a rust-inhibitive primer.
1.	Substrates:
a.	Ferrous metal.
b.	Zinc-coated metal.
c.	Aluminum.
2.	Acrylic Primer : PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Primer: PPG Paints. Speedhide Alkyd Metal Primer, 6-208 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Exterior Gloss Level 1 Acrylic Paint Finish:
a.	PPG Paints. Speedhide Exterior House Paint Flat Latex, 6-610XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Flat, 72-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Flat, 519-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Flat, 759-10 Series. Applied Dry Film Thickness: 2.3 mils min.
5.	Exterior Gloss Level 2 Acrylic Finish:
a.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Eggshell, 589-10 Series. Applied Dry Film Thickness: 1.6 mils min.
6.	Exterior Gloss Level 3 and 4 Acrylic Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Satin-Acrylic Latex, 6-2045XI Series. Applied Dry Film Thickness: 1.0 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Satin, 76-45XI Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Satin, 739-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Satin, 769-10 Series. Applied Dry Film Thickness: 2.2 mils min.
e.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Exterior Gloss Level 5 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Exterior House and Trim Semi-Gloss Acrylic Latex Paint, 6-900XI Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Sun Proof Exterior 100 percent Acrylic Latex Semi-Gloss, 78-45XI Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Acri-Shield Max Exterior 100 percent Acrylic Latex Semi-Gloss, 649-10 Series. Applied Dry Film Thickness: 1.6 mils min.
d.	PPG Paints. Permanizer Exterior 100 percent Acrylic Latex Semi-Gloss, 749-10 Series. Applied Dry Film Thickness: 2.1 mils min.
e.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Exterior Gloss Level 5 Alkyd Enamel Finish:
a.	PPG Paints. HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Exterior Gloss Level 6 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
10.	Exterior Gloss Level 6 Alkyd Enamel Finish:
a.	PPG Paints. 7-Line Industrial Gloss-Oil Interior/Exterior Enamel, 7-282 Series. Applied Dry Film Thickness: 2.0 mils min.
2.4	EXTERIOR STAIN SYSTEMS
A.	Alkyd-Based Toner Wood Finish: Penetrating sealer/finish system applied on properly cleaned and prepared wood surface.
1.	Substrate:
a.	Stained Woodwork: Provide the following stain finishes over new exterior woodwork, for use with both vertical siding/trim and horizontal deck applications unless otherwise stated.
2.	Sealer/Finish Coat:
a.	PPG Paints. Flood CWF-OIL Penetrating Oil Wood Finish, FLD447. Apply two coats using a wet-on-wet application.
b.	PPG Paints. ProLuxe SRD Wood Finish (Transparent Matte). Apply 1 coat, SIK240 Series.
c.	PPG Paints. ProLuxe SRD RE Wood Finish (Transparent Matte), SIK250 Series. Apply 1 coat.
d.	PPG Paints. ProLuxe Premium Deck Wood Finish (Transparent Satin), SIK440 Series. Apply two coats.
B.	Alkyd-Based Toner Wood Finish Penetrating sealer/finish system applied on properly cleaned and prepared vertical wood surface. Not for deck applications.
1.	Substrate: Vertical Siding/Trim Applications:
2.	Sealer Coat:
a.	PPG Paints. ProLuxe 1 Primary RE Wood Finish (Transparent Matte), SIK410 Series. Use with SIK430 Series 23 Top Coat RE Wood Finish.
3.	Finish Coat:
a.	PPG Paints. ProLuxe 23 Top Coat RE Wood Finish (Transparent Satin), SIK430 Series. Apply 2 coats over SIK410 Series 1 Primary RE Wood Finish.
4.	Sealer/Finish Coat:
a.	PPG Paints. ProLuxe Door and Window Wood Finish (Transparent Satin), SIK480 Series. Apply 3 coats.
b.	ProLuxe. Log and Siding Wood Finish (Transparent Satin), SIK420 Series. Apply 2 coats.
5.	Clear Coat:
a.	PPG Paints. ProLuxe Door and Window Wood Finish (Transparent Satin), SIK48003. Apply over SIK480 Series as needed to maintain sheen.
6.	Clear Maintenance Coat:
a.	PPG Paints. ProLuxe Maintenance RE Wood Finish (Clear Satin), SIK61003. Apply over SIK420 or SIK 430 Series as needed to maintain sheen. Vertical applications only.
C.	Acrylic-Oil Toner Wood Finish: Penetrating sealer/finish system.
1.	Substrate: Properly cleaned and prepared wood surface:
2.	Sealer/Finish Coat:
a.	PPG Paints. Flood CWF-UV Penetrating Wood Finish, FLD520 Series. Apply 1 coat.
b.	PPG Paints. Flood CWF-UV5 Penetrating Wood Finish, FLD565 Series. Apply 1 coat.
D.	Alkyd-Based Semi-Transparent Wood Finish: Penetrating sealer/finish system.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints. Flood Semi-Transparent Alkyd-Oil Wood Finish, FLD802 Series. Apply 1 coat.
E.	Acrylic-Oil Semi-Transparent Wood Finish: Penetrating sealer/finish systems.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints. Flood Semi-Transparent Acrylic-Oil Wood Finish, FLD812 Series. Apply 1 coat.
b.	PPG Paints. Flood. Flood Semi-Transparent Acrylic-Oil Wood Finish, FLD832 Series. Apply 1 coat.
F.	Acrylic Based Semi-Transparent Wood Finish: Penetrating sealer/finish system.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints: ProLuxe SRD Semi-Transparent Wood Finish (Matte), SIK500 Series. Apply 1 coat.
G.	Alkyd-Oil Semi-Opaque Wood Finish: Penetrating sealer/finish system.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints: Flood Semi-Opaque Alkyd-Oil Wood Finish, FLD842 Series. Apply 2 coats using a wet-on-wet application.
H.	Acrylic Solid Color Wood Finish: Acrylic topcoat system.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints. Flood Acrylic Solid Color Matte Wood Finish, FLD820 Series. Apply 2 coats.
b.	PPG Paints. ProLuxe Premium Solid Stain Wood Finish (Matte), SIK710 Series. Apply 2 coats.
2.5	EXTERIOR NATURAL FINISH WOODWORK SYSTEMS - STAINED FINISHES OVER NEW WOODWORK.
A.	Alkyd-Based Varnish Finish: Two finish coats of alkyd based clear varnish.
1.	Substrate: Properly prepared wood surface. Provide wood filler on open-grain wood before applying first varnish coat. Not for deck applications.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Finish Coat:
a.	PPG Paints. Deft Defthane Polyurethane Interior/Exterior Oil-Based 275 g/L; Satin, DFT26.
b.	PPG Paints. Deft Defthane Polyurethane Interior/Exterior Oil-Based 275 g/L; Semi-Gloss, DFT123.
c.	PPG Paints. Deft Defthane Polyurethane Interior/Exterior Oil Based 275 g/L; Gloss, DFT21.
B.	Waterborne Varnish Finish: Two finish coats of waterborne clear varnish.
1.	Substrate: Properly prepared wood surface. Wipe wood filler before applying stain. Not for deck applications.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Finish Coat:
a.	PPG Paints: Clear Deft Polyurethane Interior/Exterior Water-Based Acrylic Satin, DFT259.
b.	PPG Paints: Clear Deft Polyurethane Interior/Exterior Water-Based Acrylic Semi-Gloss, DFT258.
c.	PPG Paints: Clear Deft Polyurethane Interior/Exterior Water-Based Acrylic Gloss, DFT257.
C.	Clear Penetrating Wood Finish: Penetrating sealer/finish system.
1.	Substrate: Properly cleaned and prepared wood surface.
2.	Sealer/Finish Coat:
a.	PPG Paints: Flood CWF Multi-Surface Waterproofing Clear Sealant, FLD540XI. Apply 2 coats using a wet-on-wet application.
b.	PPG Paints: Flood CWF-UV Clear/Natural Penetrating Wood Finish, FLD542 Series. Apply 1 coat.
c.	PPG Paints: Flood CWF-UV5 Clear/Natural Penetrating Wood Finish, FLD565 Series. Apply 1 coat.
2.6	INTERIOR PAINT SYSTEMS
A.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Concrete and masonry other than concrete unit masonry.
b.	Gypsum board.
c.	Plaster.
d.	Acoustical plaster.
e.	Wood and hardboard.
2.	Primer:
a.	PPG Paints. Seal Grip Gripper Interior/Exterior 100 Percent Acrylic Latex Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
b.	PPG Paints. Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Speedhide Interior Quick-Drying Latex Sealer, 6-2. Applied Dry Film Thickness: 1.0 mils min.
3.	Primer-Zero VOC:
a.	PPG Paints. Speedhide Zero Interior Zero VOC Latex Primer, 6-4900XI. Applied Dry Film Thickness: 1.2 mils min.
4.	Primer for Alkyd-Enamel Finishes:
a.	PPG Paints. Seal Grip Interior/Exterior Alkyd Primer, 17-941NF. Applied Dry Film Thickness: 2.2 mils min.
5.	Interior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Speedhide Interior Wall Flat-Latex Paint, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	PPG Paints. Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	PPG Paints. Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
6.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Flat Latex, 6-5110 Series. Applied Dry Film Thickness: 1.2 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
7.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Low-Sheen Eggshell Acrylic Latex Enamel, 6-4101 Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Speedhide Eggshell Acrylic Latex Enamel, 6-411 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint and Primer in One Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
8.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Eggshell Latex, 6-5310 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
9.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Satin Latex, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. UltraLast Interior Latex Paint & Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
10.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Speedhide Zero Interior Zero VOC Satin Latex, 6-5410 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Eggshell, 29-1310 Series. Applied Dry Film Thickness: 1.6 mils min.
11.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
12.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-310 Series. Applied Dry Film Thickness: 1.5 mils min.
13.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Lo Lustre Latex, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. V52-410 Series Breakthrough Interior/Exterior Waterborne Acrylic Satin. Applied Dry Film Thickness: 1.4 mils min.
14.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Satin, 29-1410 Series. Applied Dry Film Thickness: 1.6 mils min.
15.	Interior Gloss Level 5 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Semi-Gloss Latex, 6-500 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint and Primer in One Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
16.	Interior Gloss Level 5 Acrylic Enamel Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Semi-Gloss Latex, 6-5510 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
e.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Semi-Gloss, 29-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
17.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
18.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-510 Series. Applied Dry Film Thickness: 1.5 mils min.
19.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 1.5 mils min.
20.	Interior Gloss Level 6 and 7 Alkyd Enamel Low Odor Finish:
a.	PPG Paints. Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
b.	PPG Paints. 7-Line Industrial Gloss-Oil Interior/Exterior Enamel, 7-282 Series. Applied Dry Film Thickness: 2.0 mils min.
B.	Acrylic or Alkyd Finish: Two finish coats over a block filler.
1.	Substrate: Concrete Unit Masonry.
2.	Block Filler:
a.	PPG Paints. Speedhide Interior/Exterior Masonry Latex Block Filler, 6-7. Applied Dry Film Thickness: 6.0 to 14.0 mils min.
b.	PPG Paints. Speedhide Interior/Exterior Acrylic Masonry Block Filler, 6-15XI. Applied Dry Film Thickness: 8.0 mils min.
3.	Interior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Speedhide Interior Wall Flat-Latex Paint, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	PPG Paints. Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	PPG Paints. Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
4.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Flat Latex, 6-5110 Series. Applied Dry Film Thickness: 1.2 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
5.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Low-Sheen Eggshell Acrylic Latex Enamel, 6-4101 Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints. Speedhide Eggshell Acrylic Latex Enamel, 6-411 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint & Primer Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
6.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Eggshell Latex, 6-5310 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
7.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Satin Latex, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. UltraLast Interior Latex Paint & Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Speedhide Zero Interior Zero VOC Satin Latex, 6-5410 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Eggshell, 29-1310 Series. Applied Dry Film Thickness: 1.6 mils min.
9.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
10.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-310 Series. Applied Dry Film Thickness: 1.5 mils min.
11.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Lo-Lustre Latex, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. V52-410 Series Breakthrough Interior/Exterior Waterborne Acrylic Satin. Applied Dry Film Thickness: 1.4 mils min.
12.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Satin, 29-1410 Series. Applied Dry Film Thickness: 1.6 mils min.
13.	Interior Gloss Level 5 Acrylic Enamel:
a.	PPG Paints. Speedhide Interior Semi-Gloss Latex, 6-500 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint & Primer Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
14.	Interior Gloss Level 5 Acrylic Enamel-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Semi-Gloss Latex, 6-5510 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
e.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Semi-Gloss, 29-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
15.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
16.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-510 Series. Applied Dry Film Thickness: 1.5 mils min.
17.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 1.5 mils min.
18.	Interior Gloss Level 6 and 7 Alkyd Enamel Low Odor Finish:
a.	PPG Paints. Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
b.	PPG Paints. 7-Line Industrial Gloss-Oil Interior/Exterior Enamel, 7-282 Series. Applied Dry Film Thickness: 2.0 mils min.
C.	Acrylic or Alkyd Finish: Two finish coats over a primer.
1.	Substrates:
a.	Ferrous Metal.
b.	Zinc-Coated Metal.
2.	Acrylic Primer :
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Primer:
a.	PPG Paints. Speedhide Alkyd Metal Primer, 6-208 Series. Applied Dry Film Thickness: 2.3 mils min.
4.	Interior Gloss Level 1 Acrylic Finish:
a.	PPG Paints. Speedhide Interior Latex Ultra-Flat, 6-0011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Ultra-Flat, 679-10 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Speedhide Interior Wall Flat-Latex Paint, 6-70 Series. Applied Dry Film Thickness: 1.3 mils min.
d.	PPG Paints. Hi-Hide Interior Latex Flat, 689-10 Series. Applied Dry Film Thickness: 1.1 mils min.
e.	PPG Paints. Hi-Hide Interior Latex Ceramic Matte, 369-10 Series. Applied Dry Film Thickness: 1.1 mils min.
5.	Interior Gloss Level 1 Acrylic Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints: Speedhide Zero Interior Zero VOC Flat Latex, 6-5110 Series. Applied Dry Film Thickness: 1.2 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Flat, 9-110XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Flat, 84-3110 Series. Applied Dry Film Thickness: 1.8 mils min.
6.	Interior Gloss Level 2 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Low-Sheen Eggshell Acrylic Latex Enamel, 6-4101 Series. Applied Dry Film Thickness: 1.5 mils min.
b.	PPG Paints: Speedhide Eggshell Acrylic Latex Enamel, 6-411 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint & Primer Matte, 13-210 Series. Applied Dry Film Thickness: 1.7 mils min.
7.	Interior Gloss Level 2 Acrylic Enamel Finish-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Eggshell Latex, 6-5310 Series. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-310XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Eggshell, 84-3310 Series. Applied Dry Film Thickness: 1.6 mils min.
8.	Interior Gloss Level 3 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Satin Latex, 6-3511 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. UltraLast Interior Latex Paint & Primer Eggshell, 13-310 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Interior Gloss Level 3 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Speedhide Zero Interior Zero VOC Satin Latex, 6-5410 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Satin, 84-3410 Series. Applied Dry Film Thickness: 1.6 mils min.
c.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Eggshell, 29-1310 Series. Applied Dry Film Thickness: 1.6 mils min.
10.	Interior Gloss Level 3 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Satin, 39-10 Series. Applied Dry Film Thickness: 2.0 mils min.
11.	Interior Gloss Level 3 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-310 Series. Applied Dry Film Thickness: 1.5 mils min.
12.	Interior Gloss Level 4 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior Lo-Lustre Latex, 6-3011 Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Satin, 379-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. V52-410 Series Breakthrough Interior/Exterior Waterborne Acrylic Satin. Applied Dry Film Thickness: 1.4 mils min.
13.	Interior Gloss Level 4 Acrylic Enamel Finish Zero VOC:
a.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Satin, 29-1410 Series. Applied Dry Film Thickness: 1.6 mils min.
14.	Interior Gloss Level 5 Acrylic Enamel:
a.	PPG Paints. Speedhide Interior Semi-Gloss Latex, 6-500 Series. Applied Dry Film Thickness: 1.4 mils min.
b.	PPG Paints. Hi-Hide Interior Latex Eggshell, 389-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Semi-Gloss, 919-10 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. UltraLast Interior Latex Paint & Primer Semi-Gloss, 13-510 Series. Applied Dry Film Thickness: 1.5 mils min.
e.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Semi-Gloss, V62-510 Series. Applied Dry Film Thickness: 1.5 mils min.
f.	PPG Paints, Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
15.	Interior Gloss Level 5 Acrylic Enamel-Zero VOC:
a.	PPG Paints. Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series. Applied Dry Film Thickness: 1.3 mils min.
b.	PPG Paints. Speedhide Zero Interior Zero VOC Semi-Gloss Latex. Applied Dry Film Thickness: 1.5 mils min.
c.	PPG Paints, 6-5510 Series. Pure Performance Paint & Primer in One, 100 percent Acrylic Latex Eggshell, 9-510XI Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Prominence Interior 100 percent Acrylic Latex Paint & Primer in One, Semi-Gloss, 84-3510 Series. Applied Dry Film Thickness: 1.6 mils min.
e.	PPG Paints. Copper Armor Interior Latex Paint & Primer, Semi-Gloss, 29-1510 Series. Applied Dry Film Thickness: 1.6 mils min.
16.	Interior Gloss Level 5 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. HPC Urethane Alkyd Semi-Gloss Enamel, 4336H Series. Applied Dry Film Thickness: 2.0 mils min.
17.	Interior Gloss Level 5 Water-Based Epoxy Finish:
a.	PPG Paints. Pitt Glaze WB1 Interior Pre-Catalyzed Acrylic Epoxy, 16-510 Series. Applied Dry Film Thickness: 1.5 mils min.
18.	Interior Gloss Level 6 and 7 Acrylic Enamel Finish:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series. Applied Dry Film Thickness: 1.4 mils min.
c.	PPG Paints. Breakthrough Interior/Exterior Waterborne Acrylic Gloss, V72-610 Series. Applied Dry Film Thickness: 1.4 mils min.
d.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
19.	Interior Gloss Level 6 and 7 Alkyd Enamel Finish:
a.	PPG Paints. Glyptex Interior/Exterior Alkyd Gloss Enamel, 4139-10 Series. Applied Dry Film Thickness: 1.8 mils min.
b.	PPG Paints. 7-Line Industrial Gloss-Oil Interior/Exterior Enamel, 7-282 Series. Applied Dry Film Thickness: 2.0 mils min.
D.	Dry-Fall Finish- Two Finish Coats Over Primer:
1.	Substrates:
a.	Ferrous Metal Ceiling Deck.
b.	Zinc-Coated Metal Ceiling Deck.
2.	Acrylic Primer :
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
3.	Primer:
a.	PPG Paints. Series Speedhide Alkyd Metal Primer, 6-208. Applied Dry Film Thickness: 2.3 mils min.
4.	Interior Gloss Level 1 Water-Based Finish:
a.	PPG Paints. Series Speedhide Super Tech WB Interior Dry-Fog Flat Latex, 6-725XI. Applied Dry Film Thickness: 2.2 mils min.
5.	Interior Gloss Level 3 Water-Based Finish:
a.	PPG Paints. Speedhide Super Tech WB Interior 100 percent Acrylic Dry-Fog Eggshell Latex, 6-724XI. Applied Dry Film Thickness: 2.0 mils min.
6.	Interior Gloss Level 5 Water-Based Finish:
a.	PPG Paints. Speedhide Super Tech WB Interior 100 percent Acrylic Dry-Fog Semi-Gloss Latex, 6-727XI. Applied Dry Film Thickness: 2.2 mils min.
2.7	INTERIOR STAIN AND NATURAL FINISH WOODWORK SYSTEMS
A.	Alkyd Varnish Finish over Stain: Two finish coats of alkyd-based clear varnish over a sealer coat and wood stain. Wipe wood filler before applying stain.
1.	Substrate: Stained woodwork.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Stain Coat:
a.	PPG Paints. Deft Oil-Based Wood Stain, DFT400.
4.	Sealer Coat:
a.	PPG Paints. Deft Sanding Sealer Interior Water-Based, DFT61.
5.	Finish Coat:
a.	PPG Paints. Deft Polyurethane Interior Oil-Based 350 g/L Satin, DFT129.
b.	PPG Paints. Deft Polyurethane Interior Oil-Based 350 g/L Semi-Gloss, DFT128.
c.	PPG Paints. Deft Polyurethane Interior Oil-Based 350 g/L Gloss, DFT127.
B.	Waterborne Varnish Finish over Stain: Two finish coats of waterborne clear varnish over a sealer coat and wood stain. Wipe wood filler before applying stain.
1.	Substrate: Stained woodwork.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Stain Coat: PPG Paints. Deft Oil-Based Wood Stain, DFT400.
4.	Sealer Coat: PPG Paints. Deft Sanding Sealer Interior Water-Based, DFT61.
5.	Finish Coat:
a.	Deft. Clear Polyurethane Interior Water-Based Acrylic Satin, DFT159.
b.	PPG Paints. Deft Clear Polyurethane Interior Water-Based Acrylic Semi-Gloss, DFT158.
c.	PPG Paints. Deft Clear Polyurethane Interior Water-Based Acrylic Gloss, DFT157.
C.	Alkyd-Based Stain Wax-Polished Finish: Three finish coats of paste wax over a sealer coat and wood stain. Wipe wood filler before applying stain.
1.	Substrate: Stained woodwork.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Stain Coat: PPG Paints: Deft Oil-Based Wood Stain, DFT400.
4.	Sealer Coat: PPG Paints: Deft Sanding Sealer Interior Oil-Based, DFT60.
5.	Finish Coat: Paste wax.
D.	Alkyd-Based Varnish Finish: Two finish coats of alkyd based clear varnish over a sanding sealer. Provide wood filler on open-grain wood before applying first varnish coat.
1.	Substrate: Natural Finish Woodwork.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Sealer Coat: PPG Paints: Sanding Sealer Interior Water-Based, DFT61.
4.	Finish Coat:
a.	PPG Paints. Deft Polyurethane Interior Oil-Based 350 g/L Satin, DFT129.
b.	PPG Paints: Deft Polyurethane Interior Oil-Based 350 g/L Semi-Gloss, DFT128.
c.	PPG Paints. Deft Polyurethane Interior Oil-Based 350 g/L Gloss, DFT127.
E.	Waterborne Satin-Varnish Finish: Two finish coats of waterborne clear varnish over a sanding sealer. Wipe wood filler before applying stain.
1.	Substrate: Natural Finish Woodwork.
2.	Filler Coat: Open-Grain Wood Filler.
3.	Sealer Coat: PPG Paints. Deft Sanding Sealer Interior Water-Based, DFT61.
4.	Finish Coats:
a.	PPG Paints. Deft Clear Polyurethane Interior Water-Based Acrylic Satin, DFT159.
b.	PPG Paints. Deft Clear Polyurethane Interior Water-Based Acrylic Semi-Gloss, DFT158.
c.	PPG Paints. Deft Clear Polyurethane Interior Water-Based Acrylic Gloss, DFT157.
F.	Alkyd-Based Sealer Wax-Polished Finish: Three finish coats of paste wax over a sanding-sealer. Wipe wood filler before applying stain.
1.	Substrate: Natural Finish Woodwork.
2.	Filler Coat: Open-Grained Wood Filler.
3.	Sealer Coat: PPG Paints: Deft Sanding Sealer Interior Oil-Based, DFT60:
4.	Finish Coat: Paste wax.
G.	Waterborne Sealer Wax-Polished Finish: Three finish coats of paste wax over a sanding-sealer. Wipe wood filler before applying stain.
1.	Substrate: Natural Finish Woodwork.
2.	Filler Coat: Open-Grained Wood Filler.
3.	Sealer Coat: PPG Paints: Deft Sanding Sealer Interior Water-Based, DFT61.
4.	Finish Coat: Paste wax.
2.8	EXTERIOR HIGH PERFORMANCE COATING SYSTEMS
A.	Epoxy with Urethane Finish: One finish coat over an intermediate coat and a primer.
1.	Substrate: Concrete and Masonry, other than concrete masonry units.
2.	Primer:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
3.	Intermediate Coat: Epoxy:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
4.	Intermediate Coat: Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. Pitthane High Build Semi-Gloss Urethane Enamel, 95-8801/95-859 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Intermediate Coat: Polyester Acrylic Polyurethane:
a.	PPG Paints. Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
6.	Topcoat: Gloss Level 3 and 4, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Topcoat: Gloss Level 5, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane High Build Semi-Gloss Urethane Enamel, 95-8801/95-859 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Topcoat: Gloss Level 6 and 7, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Topcoat: Gloss Level 6 and 7, Polyester Acrylic Polyurethane
a.	PPG Paints. Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
B.	Epoxy with Urethane Finish: One finish coat over an intermediate coat and a block filler.
1.	Substrate: Concrete masonry units:
2.	Block Filler: PPG Paints. Amerlock 400BF Epoxy Block Filler, AK400B-30/AK400B-B. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat: Epoxy:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
4.	Topcoat: Gloss Level 3 and 4, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Topcoat: Gloss Level 5, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane High Build Semi-Gloss Urethane Enamel, 95-8801/95-859 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Topcoat: Gloss Level 6 and 7, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Topcoat: Gloss Level 6 and 7, Polyester Acrylic Polyurethane:
a.	PPG Paints. Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
C.	Acrylic Finish: One finish coat over an intermediate coat and a primer.
1.	Substrate: Exterior wood surfaces:
2.	Primer: PPG Paints. Seal Grip Gripper Interior/Exterior Interior/Exterior 100 Percent Acrylic Latex Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
3.	Intermediate Coat:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints: Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
d.	PPG Paints: Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat Gloss Level 3:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Topcoat Gloss Level 5:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Topcoat Gloss Level 6 and 7:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
D.	Epoxy with Urethane Finish: One finish coat over an intermediate coat and a primer.
1.	Substrate:
a.	Ferrous Metal.
b.	Nonferrous Metal.
2.	Primer:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
3.	Intermediate Coat:Epoxy:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
c.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
4.	Intermediate Coat: Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. Pitthane High Build Semi-Gloss Urethane Enamel, 95-8801/95-859 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Intermediate Coat: Polyester Acrylic Polyurethane:
a.	PPG Paints. Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
6.	Topcoat: Gloss Level 3 and 4, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra LS Low Sheen Urethane Enamel, 95-8901/95-899 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Topcoat: Gloss Level 5, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane High Build Semi-Gloss Urethane Enamel, 95-8801/95-859 Series. Applied Dry Film Thickness: 2.0 mils min.
8.	Topcoat: Gloss Level 6 and 7, Aliphatic Polyurethane Enamel:
a.	PPG Paints. Pitthane Ultra Gloss Urethane Enamel, 95-812/95-819 Series. Applied Dry Film Thickness: 2.0 mils min.
9.	Topcoat: Gloss Level 6 and 7, Polyester Acrylic Polyurethane:
a.	PPG Paints. Amershield VOC Low VOC Gloss Polyester Acrylic Polyurethane, AMV-3 Series. Applied Dry Film Thickness: 3.0 mils min.
E.	Fluoropolymer System: One finish coat applied over an epoxy primer.
1.	Substrate:
a.	Ferrous Metal.
b.	Nonferrous Metal.
2.	Primer: PPG Paints. Coraflon ADS Epoxy Primer, ADS 573/ADS574. Applied Dry Film Thickness: 3.0 mils min.
3.	Finish: PPG Paints. Coraflon ADS Fluoropolymer. Apply per instructions on the technical data bulletin. Metallic finishes may require an additional clear coat of Coraflon ADS.
2.9	INTERIOR HIGH PERFORMANCE COATING SYSTEMS
A.	Epoxy Finish: One finish coat over an intermediate coat and a primer.
1.	Substrate: Concrete and Masonry other than concrete masonry units:
2.	Primer:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Epoxy Primer, 98E-46/98E-99 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
3.	Intermediate Coat: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
e.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
f.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat Gloss Level 5: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
5.	Topcoat Gloss Level 6 and 7: Epoxy:
a.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
B.	Epoxy Finish over Block Filler: One finish coat over intermediate coat and block filler.
1.	Substrate: Concrete masonry units:
2.	Block Filler: PPG Paints. Amerlock 400BF Epoxy Block Filler, AK400B-30/AK400B-B. Applied Dry Film Thickness: 4.0 mils min.
3.	Intermediate Coat: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
e.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
f.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat Gloss Level 5: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
5.	Topcoat Gloss Level 6 and 7: Epoxy:
a.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
C.	Acrylic Finish: One finish coat over an intermediate coat and a primer.
1.	Substrates:
a.	Wood:
b.	Interior wood surfaces:
2.	Primer:
a.	PPG Paints. Seal Grip Gripper Interior/Exterior Interior/Exterior 100 Percent Acrylic Latex Primer, 17-921XI Series. Applied Dry Film Thickness: 1.6 mils min.
3.	Acrylic Primer:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic DTM Primer, 90-1912 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Intermediate Coat:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
b.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
d.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
5.	Topcoat Gloss Level 3:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Satin DTM Industrial Enamel, 90-1710 Series. Applied Dry Film Thickness: 2.0 mils min.
6.	Topcoat Gloss Level 5:
a.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Semi-Gloss DTM Industrial Enamel, 90-1610 Series. Applied Dry Film Thickness: 2.0 mils min.
7.	Topcoat Gloss Level 6 and 7:
a.	PPG Paints. Speedhide Interior/Exterior High Gloss Acrylic Paint, 6-8534 Series. Applied Dry Film Thickness: 1.2 mils min.
b.	PPG Paints. Pitt-Tech Plus EP Interior/Exterior Acrylic Gloss DTM Industrial Enamel, 90-1510 Series. Applied Dry Film Thickness: 2.0 mils min.
D.	Epoxy Finish: One finish coat over intermediate coat and a primer.
1.	Substrate:
a.	Ferrous metal.
b.	Nonferrous metal.
2.	Primer:
a.	PPG Paints. Pitt-Guard Rapid Coat DTR Polyamide Epoxy Coating, 95-245/95-249 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Epoxy Primer, 98E-46/98E-99 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
3.	Intermediate Coat: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
e.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
f.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
4.	Topcoat Gloss Level 5: Epoxy:
a.	PPG Paints. Aquapon High Build Semi-Gloss Polyamide Epoxy Coating, 97-1212/97-139 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Semi-Gloss Epoxy Coating, 98E-1/98E-100 Series. Applied Dry Film Thickness: 2.0 mils min.
c.	PPG Paints. Amerlock 2 VOC Fast Dry, High Solids Semi-Gloss Epoxy Coating, AK2V-3 Series. Applied Dry Film Thickness: 4.0 mils min.
d.	PPG Paints. Amerlock 600 High Build Semi-Gloss Epoxy Coating, AK600-3 Series. Applied Dry Film Thickness: 5.0 mils min.
5.	Topcoat Gloss Level 6 and 7: Epoxy.
a.	PPG Paints. High Gloss Polyamide-Epoxy Coating, 95-501/95-506 Series. Applied Dry Film Thickness: 4.0 mils min.
b.	PPG Paints. Aquapon WB EP Two-Component Waterborne Gloss Epoxy Coating, 98E-1/98E-98 Series. Applied Dry Film Thickness: 2.0 mils min.
E.	Fluoropolymer System: One finish coat applied over an epoxy primer.
1.	Substrate:
a.	Ferrous metal.
b.	Nonferrous metal.
2.	Primer: PPG Paints. Coraflon ADS Epoxy Primer, ADS 573/ADS574. Applied Dry Film Thickness: 3.0 mils min.
3.	Finish: PPG Paints. Coraflon ADS Fluoropolymer. Apply per instructions on the technical data bulletin. Metallic finishes may require an additional clear coat of Coraflon ADS.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Do not begin installation until substrates have been properly prepared.
B.	If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.
C.	Coordination of Work: Review other Sections in which primers are provided to ensure compatibility of the total system for various substrates. On request, furnish information on characteristics of finish materials to ensure use of compatible primers.
1.	Notify Architect about anticipated problems when using the materials specified over substrates primed by others.
2.	If a potential incompatibility of primers applied by others exists, obtain the following from the primer Applicator before proceeding:
a.	Confirmation of primer's suitability for expected service conditions.
b.	Confirmation of primer's ability to be top coated with materials specified.
3.2	PREPARATION
A.	General: Remove hardware and hardware accessories, plates, machined surfaces, lighting fixtures, and similar items already installed that are not to be painted. If removal is impractical or impossible because of size or weight of the item, provide surface-applied protection before surface preparation and painting.
1.	After completing painting operations in each space or area, reinstall items removed using workers skilled in the trades involved.
B.	Cleaning: Before applying paint or other surface treatments, clean substrates of substances that could impair bond of the various coatings. Remove oil and grease before cleaning.
1.	Schedule cleaning and painting so dust and other contaminants from the cleaning process will not fall on wet, newly painted surfaces.
C.	Surface Preparation: Clean and prepare surfaces to be painted according to manufacturer's written instructions for each particular substrate condition and as specified.
1.	Provide barrier coats over incompatible primers or remove and reprime.
2.	Provide barrier coats over incompatible primers or remove primers and reprime substrate.
3.	Cementitious Substrates: Prepare concrete, brick, concrete masonry block, and cement plaster surfaces to be coated. Remove efflorescence, chalk, dust, dirt, grease, oils, and release agents. Roughen as required to remove glaze. If hardeners or sealers have been used to improve curing, use mechanical methods to prepare surfaces.
a.	Use abrasive blast-cleaning methods if recommended by coating manufacturer.
b.	Determine alkalinity and moisture content of surfaces by performing appropriate tests. If surfaces are sufficiently alkaline to cause the finish paint to blister and burn, correct this condition before application. Do not coat surfaces if moisture content exceeds that permitted in manufacturer's written instructions.
4.	Wood Substrates: Clean surfaces of dirt, oil, and other foreign substances with scrapers, mineral spirits, and sandpaper, as required. Smoothly sand surfaces exposed to view and dust off.
a.	Scrape and clean small, dry, seasoned knots, and apply a thin coat of white shellac or other recommended knot sealer, before applying primer.
b.	Immediately on delivery, prime edges, ends, faces, undersides, and backsides of wood to be coated.
c.	After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.
5.	Ferrous Metal Substrates: Clean ungalvanized ferrous-metal surfaces that have not been shop coated: remove oil, grease, dirt, loose mill scale, and other foreign substances. Use solvent or mechanical cleaning methods that comply with SSPC recommendations.
a.	Blast-clean steel surfaces as recommended by coating manufacturer and according to SSPC-SP 10.
b.	Treat bare and sandblasted or pickled clean metal with a metal treatment wash coat before priming.
c.	Touch up bare areas and shop-applied prime coats that have been damaged. Wire brush, solvent clean, and touch up with same primer as the shop coat.
6.	Nonferrous-Metal Substrates: Clean nonferrous and galvanized surfaces according to manufacturer's written instructions for the type of service, metal substrate, and application required.
a.	Remove pretreatment from galvanized sheet metal fabricated from coil stock by mechanical methods.
D.	Material Preparation: Carefully mix and prepare coating materials according to manufacturer's written instructions.
1.	Maintain containers used in mixing and applying coatings in a clean condition, free of foreign materials and residue.
2.	Stir materials before applying to produce a mixture of uniform density. Stir as required during application. Do not stir surface film into the material. Remove film and, if necessary, strain coating material before using.
3.	Use only the type of thinners approved by manufacturer and only within recommended limits.
4.	Tinting: Tint each undercoat a lighter shade to simplify identification of each coat when multiple coats of same material are applied. Tint undercoats to match the color of the finish coat but provide sufficient differences in shade of undercoats to distinguish each separate coat.
3.3	APPLICATION
A.	General: Apply paint according to manufacturer's written instructions. Use applicators and techniques best suited for substrate and type of material being applied.
B.	General: Apply high-performance coatings according to manufacturer's written instructions.
1.	Use applicators and techniques best suited for the material being applied.
2.	Do not apply high-performance coatings over dirt, rust, scale, grease, moisture, scuffed surfaces, or conditions detrimental to forming a durable coating film.
3.	Coating surface treatments, and finishes are indicated in the coating system descriptions.
4.	Provide finish coats compatible with primers used.
5.	The term "exposed surfaces" includes areas visible when permanent or built-in fixtures, convector covers, grilles, covers for finned-tube radiation, and similar components are in place. Extend coatings in these areas, as required, to maintain system integrity and provide desired protection.
C.	Application Procedures: Apply coatings by brush, roller, spray, or other applicators according to manufacturer's written instructions.
1.	The number of coats and film thickness required is the same regardless of application method.
2.	Completed Work: Match approved Samples for color, texture, and coverage. Remove, refinish, or recoat work that does not comply with specified requirements.
3.4	FIELD QUALITY CONTROL
A.	Owner reserves the right to invoke the following test procedure at any time and as often as Owner deems necessary during the period when paint is being applied:
1.	Owner will engage a qualified independent testing agency to sample paint material being used. Samples of material delivered to Project will be taken, identified, sealed, and certified in the presence of Contractor.
2.	Owner may direct Contractor to stop painting if test results show material being used does not comply with specified requirements. Contractor shall remove noncomplying paint from Project site, pay for testing, and repaint surfaces previously coated with the noncomplying paint. If necessary, Contractor may be required to remove noncomplying paint from previously painted surfaces if, on repainting with specified paint, the two coatings are incompatible.
3.5	CLEANING
A.	After completing painting, clean glass and paint spattered surfaces. Remove spattered paint by washing and scraping without scratching or damaging adjacent finished surfaces.
3.6	PROTECTION
A.	Protect work of other trades, whether being painted or not, against damage from painting. Correct damage by cleaning, repairing, or replacing, and repainting, as approved by Architect.
B.	Provide "Wet Paint" signs to protect newly painted finishes. After completing painting operations, remove temporary protective wrappings provided by others to protect their work.
C.	After work of other trades is complete, touch up and restore damaged or defaced painted surfaces.

END OF SECTION