SECTION 09 01 90

PAINT AND GRAFFITI REMOVERS AND CLEANING SOLUTIONS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2018 -  2023 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Water-based removal and control systems including the following:
1.	Paint removers.
2.	Graffiti removers.
3.	Lead encapsulation compounds.
4.	Stone and masonry cleaners.
5.	Concrete panel cleaner and bond-breaker remover
6.	Deck strippers and cleaners.
7.	Goo and adhesive removers.
1.2	RELATED SECTIONS
A.	Section 09 90 00 - Painting and Coating.
1.3	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	Product Data:
1.	Manufacturer's data sheets on each product to be used.
2.	Preparation instructions and recommendations.
3.	Storage and handling requirements and recommendations.
4.	Typical installation methods.
C.	Field Test: For the project record, submit written report of field test performed for each application and results achieved.
1.4	QUALITY ASSURANCE
A.	Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.
B.	Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.
C.	Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.
D.	Field Test: Use manufacturer's test kit prior to application of any materials. Obtain Architect's approval of test results prior to starting subsequent operations.
1.	If required, repeat field test until Architect's acceptance.
1.5	DELIVERY, STORAGE, AND HANDLING
A.	Store and handle in strict compliance with manufacturer's written instructions and recommendations.
1.	Shelf Life, All Products: 3 years.
B.	Protect from damage due to weather, excessive temperature, and construction operations.
1.6	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.7	WARRANTY
A.	Manufacturer's Warranty: Provide manufacturer's standard limited warranty.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: Dumond, Inc., which is located at:<BR />253 S. Bailey Rd.<BR />Downingtown, PA 19335<BR />Toll Free Tel: 800-245-1191 <BR />Tel: 609-655-7700<BR />Fax: 609-655-7725<BR />Email: request info (abensen@dumondglobal.com);Web: https://dumondglobal.com 
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	PAINT REMOVERS
A.	Complete Paint Removal Test Kit as manufactured by Dumond Inc.
1.	Includes:
a.	Peel Away 1 Paint Remover.
b.	Smart Strip Advanced Paint Remover.
c.	Smart Strip PRO Paint Remover.
d.	Dumond Laminated Paper.
e.	Citri-Lize Neutralizer.
B.	Peel Away 1 Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Viscosity: 26.5.
b.	Specific Gravity: 1.44.
c.	Weight per Gallon: 12 lbs (5.4 kg).
d.	Flash Point: None.
e.	Solid Content: 58.0.
f.	pH Level: 12.
g.	Freeze Point: 32 degrees F (0 degrees C).
h.	Shelf Life: 3 years.
2.	Form: White Thick Paste.
3.	Characteristics: Does not contain methylene chloride or NMP. Removes up to 30 coats in one application. Non-flammable. 
a.	Best on pre-1980's paints and coatings, or when the base layer is an oil, alkyd, or lead based coating.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 20 to 22 sq ft per gallon (0.50 to 0.54 sq m per L).
6.	Dwell Time: 12 to 48 hours.
C.	Smart Strip Advanced Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 6.
d.	Freeze Point: 5 degrees F (Minus 15 degrees C).
e.	Shelf Life: 3 years in a tightly sealed container.
2.	Form: White paste.
3.	Characteristics: Does not contain methylene chloride, NMP, or any caustics, 
4.	Removes up to 15 coats in a single application. 
a.	Best on post 1980's coatings (oil, latex, acrylic, and water-based).
5.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
6.	Average Spread Rate: 40 to 45 sq ft (3.7 to 4.6 sq m) per gal.
7.	Dwell Time: 3 to 24 hours.
D.	Smart Strip PRO Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 2 to 3.
d.	Freeze Point: 5 degrees F (Minus 15 degrees C).
e.	Shelf Life: 3 years.
2.	Form: White Paste.
3.	Characteristics: Does not contain methylene chloride or NMP. Removes up to 20 coats in a single application. Non-flammable. Non-carcinogenic. 
a.	Best on post 1980's coatings (oil, latex, acrylic, and water-based). 
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 40 to 45 sq ft (3.7 to 4.2 sq m) per gal.
6.	Dwell Time: 1 to 24 hours.
E.	Peel Away ST-1, Steel Structures Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Flash Point: None.
b.	pH Level: 12.
c.	Freeze Point: 32 degrees F (0 degrees C).
d.	Shelf Life: 3 years.
2.	Form: Blue Paste.
3.	Characteristics: Does not contain methylene chloride or NMP. Removes up to 30 coats of oil and lead-based coatings from steel surfaces in a single application. 
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 20 sq ft (1.9 sq m) per gal.
6.	Dwell Time: 12 to 48 hours.
F.	Peel Away 7, Solvent-Based Paint Remover: Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	pH Level: 6.
b.	Freeze Point: 32 degrees F (0 degrees C).
c.	Shelf Life: 3 years.
2.	Form: Paste.
3.	Characteristics: Does not contain methylene chloride..
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 40 to 50 sq ft (3.7 to 4.6 sq m) per gal.
6.	Dwell Time: 12 to 48 hours
G.	Confined Space Paint Remover, Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs per gallon (4.5 kg).
b.	pH: 2 to 3.
c.	Freezing Point: 32 degrees F (0 degree C).
d.	Shelf Life: 3 years. In a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: White viscous gel.
3.	Characteristics: Contains no methylene chloride, NMP, or caustic chemicals. Removes up to 15 layers in one application.
4.	Application Temperature: 40 to 90 degrees F (4 to 32 degrees C).
5.	Average Spread Rate: 40 to 50 sq ft (3.7 to 4.6 sq m) per gal.
H.	Peel Away Marine: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Viscosity: 26.5.
b.	Specific Gravity: 1.44.
c.	Weight: 12 lbs (5.4 kg) per gal.
d.	Flash Point: None.
e.	Solid Content: 58.0.
f.	pH Level: 13.
g.	Freeze Point: 32 degrees F (0 degrees C).
h.	Shelf Life: 3 years.
2.	Form: White Thick Paste.
3.	Characteristics: Does not contain methylene chloride or NMP. Removes up to 30 coats in a single application.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 20 sq ft (1.9 sq m) per gal.
6.	Dwell Time: 12 to 48 hours.
I.	Smart Strip Marine Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	pH Level: 2 to 3.
c.	Freeze Point: 32 degrees F (0 degrees C).
d.	Shelf Life: 3 years in a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: White viscous liquid.
3.	Characteristics: Does not contain methylene chloride, NMP, or any caustics. Removes up to 15 coats in a single application.
4.	Application Temperature: 40 to 90 degrees F (4 to 32 degrees C).
5.	Average Spread Rate: 40 to 45 sq ft (3.7 to 4.6 sq m) per gal.
6.	Dwell Time: 1 to 24 hours.
J.	Confined Space Marine Paint Remover, Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs per gallon (4.5 kg).
b.	pH: 6.
c.	Freezing Point: 32 degrees F (0 degree C).
d.	Shelf Life: 3 years. In a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: White viscous liquid.
3.	Characteristics: Contains no methylene chloride or NMP. This water-based product removes up to 20 layers of marine coatings in a single application., 
4.	Application Temperature: 40 to 90 degrees F (4 to 32 degrees C).
5.	Average Spread Rate: 40 to 50 sq ft (3.7 to 4.6 sq m) per gal.
K.	Smart Strip Auto Paint Remover: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	pH Level: 2 to 3.
c.	Freeze Point: 32 degrees F (0 degrees C).
d.	Shelf Life: 3 years in a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: White viscous liquid.
3.	Characteristics: Does not contain methylene chloride or NMP. Removes up to 20 coats in a single application. For use on most vehicles.
4.	Application Temperature: 40 to 90 degrees F (4 to 32 degrees C).
5.	Average Spread Rate: 40 to 50 sq ft (3.7 to 4.6 sq m) per gal.
6.	Dwell Time: 1 to 4 hours.
L.	Dumond Laminated Paper as manufactured by Dumond Inc.
1.	Characteristics: Controls lead-dust dispersal by aiding containment of lead-based paints and hazardous materials. Decreases dwell time and reduces evaporation of paint removal products.
M.	Citri-Lize Neutralizer and Mill Glaze Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Flash Point: N/A.
b.	pH Level: 1.
c.	Freeze Point: 0 degrees F (-18 degrees C).
d.	Shelf Life: 3 years.
2.	Form: White powder.
3.	Characteristics: Lowers the pH level of substrates that are highly alkaline. Removes mill glaze. Use with Peel Away 1 and Peel Away Marine.
4.	Drying Time: 24 to 48 hours.
N.	Peel Away Neutralizer as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Flash Point: N/A.
b.	pH Level: 1.
c.	Freeze Point: 0 degrees F (minus 18 degrees C).
d.	Shelf Life: 3 years.
2.	Form: Clear liquid.
3.	Characteristics: Lowers the pH level of substrates that are highly alkaline. Non-flammable.
O.	Peel Away pH Test Tape as manufactured by Dumond Inc.
1.	Characteristics: Use for testing surface pH level.
P.	Peel Away After Strip Final Cleanup as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Flash Point: 200 degrees F (93 degrees C).
b.	pH Level: 6.
c.	Freeze Point: 0 degrees F (minus 18 degrees C).
d.	Shelf Life: 3 years.
2.	Form: Clear liquid.
3.	Characteristics: Prevents residue from clinging to substrates after stripping. Cleans and polishes marine surfaces.
2.3	GRAFFITI REMOVERS
A.	Watch Dog Smooth Surface Graffiti Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Flash Point: 154.
b.	pH Level: 10.
c.	Freeze Point: 32 degrees F (0 degrees C).
d.	Shelf Life: 3 years.
2.	Form: Clear liquid.
3.	Characteristics: Removes unwanted graffiti from aerosol spray paints, markers, inks, tapes, paints and coatings. For use on smooth, painted, or unpainted surfaces only.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 20 sq ft (1.9 sq m) per bottle.
6.	Dwell Time: 30 seconds to 10 minutes.
B.	Watch Dog Porous Surface Graffiti Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 8.9 lbs (4.0 kg).
b.	Flash Point: Over 200.
c.	pH Level: 11.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Amber gel.
3.	Characteristics: Removes unwanted graffiti from aerosol spray paints, markers, inks, tapes, paints and coatings. For use on unpainted porous surfaces only.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 100 to 150 sq ft (9.3 to 13.9 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes.
2.4	LEAD ENCAPSULATING COMPOUNDS
A.	Lead Stop Lead Encapsulating Compound: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight: 11 lbs (5.0 kg) per gal.
b.	Solids: 43.7 percent by volume.
c.	Freeze Point: 32 degrees F (0 degrees C) or greater.
d.	Shelf Life: 3 years in a tightly sealed container kept in a room temperature, clean, and dry environment.
e.	Compliant with US Department of Housing and Urban Development (H.U.D.) requirements.
f.	D.L. Litter Laboratories: Seal of approval.
2.	H.U.D. Warranty: 20 year.
3.	Form: White liquid.
4.	Contains Bitrex, an anti-ingestant.
5.	Characteristics: Provides a protective barrier coat that seals and locks in lead.
6.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
7.	Application Thickness: 14 mils wet.
8.	Drying Time: 24 hours.
9.	Spread Rate: 125 sq ft (11.6 sq m) per gal.
2.5	STONE AND MASONRY CLEANERS
A.	Smart 'n Easy Concrete Oil, Grease, and Stain Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 12.3.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Green/blue liquid.
3.	Characteristics: Water-based formula for cleaning oil, grease, and grime from porous masonry surfaces. Consumer and professional product.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 200 to 250 sq ft (18.6 to 23.2 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes, minimum.
B.	Smart 'n Easy Ultimate Stone and Masonry Cleaner as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 1.5.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Clear gel.
3.	Characteristics: More effective than conventional muriatic and hydrofluoric formulations. Water-based formula for cleaning masonry surfaces.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 200 to 250 sq ft (18.6 to 23.2 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes, minimum.
C.	Smart 'n Easy Limestone and Travertine Cleaner as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 1.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Clear liquid.
3.	Characteristics: More effective than conventional muriatic and hydrofluoric formulations. Water-based formula for cleaning limestone, travertine, honed or tumbled stone, and slate surfaces.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 200 to 250 sq ft (18.6 to 23.2 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes, minimum.
D.	Smart 'n Easy Masonry Rust Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
2.	Weight per Gallon: 10 lbs (4.5 kg).
a.	Flash Point: None.
b.	pH Level: 1.
c.	Freeze Point: 32 degrees F (0 degrees C).
d.	Shelf Life: 3 years.
3.	Form: Orange liquid.
4.	Characteristics: Penetrates to the substrate to remove years of rust accumulation on natural and man-made stone surfaces. Contains rust inhibitor.
5.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
6.	Average Spread Rate: 200 to 250 sq ft (18.6 to 23.2 sq m) per gal.
7.	Dwell Time: 15 to 30 minutes, minimum.
E.	Smart 'n Easy Efflorescence Remover as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 1.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Clear liquid.
3.	Characteristics: Water-based formulation to remove chalky white salt accumulation found on porous masonry surfaces.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 200 to 250 sq ft (18.6 to 23.2 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes, minimum.
F.	Smart ' n Easy Super Strength Metal Rust Remover. Water based. Manufactured by Dumond Inc. 
1.	Performance and Design Requirements:
a.	Wt./Gal: 10 lbs.
b.	pH: 1.0.
c.	Freeze Point: 32.
d.	Shelf Life: 3 years in a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: Orange liquid.
3.	Characteristics: Water-based formulation that penetrates to the surface to removes years of rust accumulation. Contains rust inhibitor.
4.	Application Temperature: 40 to 90 degrees F (4.4 to 32.2 degrees C).
5.	Average Spread Rate: 200 to 250 sq ft (18.58 to 23.23 sq m) per gal.
2.6	CONCRETE PANEL CLEANER AND BOND BREAKER REMOVER
A.	Tilt Wash PRO Low Toxicity Cleansing Solution: Water-based. Manufactured by Dumond Inc. Cleansing solution designed to remove bond-breakers from tilt-up or off-form concrete prior to the application of a paint or texture system.
1.	Performance Requirements:
a.	Meets all national, state, and local regulations for VOC compliance.
b.	Form: Liquid.
c.	Wt./Gal: 44 lbs per gal (5.27 kg per L).
d.	Flash Point: 167 degrees F (75 degrees C).
e.	pH Level: 7 to 9.
f.	Freeze Point: Less than 64 degrees F (17.78 degrees C).
g.	Shelf Life: 3 years.
2.	Characteristics:
a.	Quickly Removes Barrier-Type Bond-Breakers.
b.	Easy Spray Application and Clean-Up.
c.	Apply via power washer with an injection port for 5x concentrate formulation.
d.	Does not contain harmful caustic soda.
e.	Uses approximately 1/5 of water vs. high-pressure water-blaster methods.
f.	Cleans and conditions the concrete by removing stubborn contaminants.
3.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
4.	Average Spread Rate: Apply the product with an airless spray unit that can pump at least 3/4 gal per min (2.84 L per min) with a 0.15 to 0.19 textured tip size. As the product is applied, the panel should darken. If this does not happen, apply a second coat.
5.	Dwell Time: Rinse Tilt Wash PRO with a pressure washer before it dries on the surface. A second rinse should be applied immediately after the first. Check with your local municipality for local water run-off laws and regulations.
2.7	DECK STRIPPERS AND CLEANERS
A.	Peel Away Deck Stripper: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 12.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 2 years.
2.	Form: Liquid.
3.	Characteristics: Non-flammable. No harmful odors or fumes. Removes mildew, tannin, water stains, dirt, mill glaze, and stains caused by mold and mildew.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 100 to 125 sq ft (9.3 to 11.6 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes.
B.	Peel Away Deck Brightener/Neutralizer as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 1.1.
d.	Shelf Life: 3 years.
2.	Form: Clear/yellow viscous liquid.
3.	Characteristics: Removes tannin, rust stains, and mill glaze. Mild odor.
4.	Application Temperature: Minimum 50 degrees F (10 degrees C).
5.	Average Spread Rate: 1600 to 2400 sq ft (148.6 to 223.0 sq m) per gal.
C.	Peel Away Deck Restorer: Water-based. Manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 10 lbs (4.5 kg).
b.	Flash Point: None.
c.	pH Level: 12.
d.	Freeze Point: 32 degrees F (0 degrees C).
e.	Shelf Life: 3 years.
2.	Form: Liquid.
3.	Characteristics: Removes dirt, grime, moss, mold, mildew, algae, tannin, and water stains.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 200 to 300 sq ft (18.5 to 27.9 sq m) per gal.
6.	Dwell Time: 15 to 30 minutes.
D.	Peel Away Deck Cleaner as manufactured by Dumond Inc.
1.	Performance and Design Requirements:
a.	Weight per Gallon: 9 lbs (4.1 kg).
b.	Flash Point: None.
c.	pH Level: 12.
d.	Shelf Life: 3 years.
2.	Form: Pale yellow/green liquid.
3.	Characteristics: Mild chlorine odor. Removes mold, mildew, and algae.
4.	Application Temperature: Minimum 50 degrees F (10 degrees C).
5.	Average Spread Rate: 1600 to 2400 sq ft (148.6 to 223.0 sq m) per gal.
2.8	GOO AND ADHESIVE REMOVER
A.	Watch Dog Adhesive Remover. As manufactured by Dumond Inc. 
1.	Performance and Design Requirements:
a.	Weight/Gal: 8 lbs.
b.	pH: 6.
c.	Flash Point: None.
d.	Freezing Point: 32 degrees F / 0 degrees C.
e.	Shelf Life: 3 years in a tightly sealed container kept in a room temperature, clean, and dry environment.
2.	Form: Clear liquid.
3.	Characteristics: Removes tough, stuck on, unwanted adhesives from virtually any surface. Glues, tape, grout, caulking, sealants, adhesives, stickers, details, etc. Water-based formula.
4.	Application Temperature: 50 to 90 degrees F (10 to 32 degrees C).
5.	Average Spread Rate: 35 to 45 sq ft (3.25 to 4.18 sq m) per gal.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Do not begin installation until substrates have been properly constructed and prepared.
B.	If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.
3.2	PREPARATION
A.	Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.
B.	Protect adjacent surfaces as recommended by manufacturer.
C.	Clean surfaces and remove large particles as recommended by manufacturer.
3.3	APPLICATION
A.	Apply in accordance with manufacturer's instructions, approved submittals and approved mock-ups:
1.	Use tools and application methods recommended by manufacturer.
2.	Allow sufficient time for solution to remain on surface.
3.	Agitate as recommended by manufacturer.
4.	Rinse and remove product as recommended by manufacturer.
3.4	CLEANING AND PROTECTION
A.	When lead-based coatings are being removed, comply with regulations of US Environmental Protection Agency (EPA), and state and local agencies.
B.	Clean surfaces in accordance with the manufacturer's recommendations.

END OF SECTION