SECTION 08 87 00

WINDOW FILMS

Display hidden notes to specifier. (Don't know how? Click Here) 
 Copyright 2019 -  2024 ARCAT, Inc. - All rights reserved

PART 1    GENERAL
1.1	SECTION INCLUDES
A.	Window films for retrofit onto existing building doors, windows, storefront and curtain wall.
1.	Dual layer ceramic Tinite window film. (Tinite Ceramic 35) (Tinite Ceramic 45)
2.	Dual reflective window film. (Dual Reflective 05) (Dual Reflective 15) (Dual Reflective 25) (Dual Reflective 35)
3.	Silver reflective window film. (Silver 15) (Silver 30) (Silver 50)
4.	Spectrally selective high definition window film. (High Definition 70)
5.	Transitional window film. (CV55/35) (CV35/20) (CV25/15)
1.2	RELATED SECTIONS
A.	Section 08 40 00 - Entrances, Storefronts, and Curtain Walls.
B.	Section 08 50 00 - Windows.
C.	Section 08 60 00 - Roof Windows and Skylights.
D.	Section 08 83 13 - Mirrored Glass Glazing.
1.3	SUBMITTALS
A.	Submit under provisions of Section 01 30 00 - Administrative Requirements.
B.	Product Data:
1.	Manufacturer's data sheets on each product to be used.
2.	Preparation instructions and recommendations.
3.	Storage and handling requirements and recommendations.
4.	Typical installation methods.
C.	Verification Samples: Two representative units of each type, size, pattern and color.
D.	Shop Drawings: Include details of materials, construction and finish. Include relationship with adjacent construction. 
1.4	QUALITY ASSURANCE
A.	Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.
B.	Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.
C.	Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.
D.	Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.
1.	Intent of mock-up is to demonstrate quality of workmanship and visual appearance.
2.	If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.
3.	Retain mock-up during construction as a standard for comparison with completed work. 
4.	Do not alter or remove mock-up until work is completed or removal is authorized.
1.5	PRE-INSTALLATION CONFERENCE
A.	Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.
1.6	DELIVERY, STORAGE, AND HANDLING
A.	Store and handle in strict compliance with manufacturer's written instructions and recommendations.
B.	Protect from damage due to weather, excessive temperature, and construction operations.
1.7	PROJECT CONDITIONS
A.	Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
1.8	WARRANTY
A.	Manufacturer's Warranty: Manufacturer's standard 10 year limited warranty. Will not blister, peel, change color, or bubble.
1.	Photochromic reactions are warranted for a minimum of five (5) years from date of installation. Extended warranty option available.
PART 2    PRODUCTS
2.1	MANUFACTURERS
A.	Acceptable Manufacturer: CoolVu, LLC, which is located at:<BR />4939 Lower Roswell Rd., Bldg. B<BR />Marietta, GA 30068<BR />Tel: 844-426-6588<BR />Email: request info (info@coolvu.com);Web: https://www.coolvu.com 
B.	Substitutions: Not permitted.
C.	Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.
2.2	PERFORMANCE REQUIREMENTS
A.	Energy Performance:
1.	Block Ultraviolet Radiation: 99 percent.
2.	Block Infrared Energy: 80 percent.
3.	Transition: Up to 35 percent.
4.	Control Sun Glare: Up to 80 percent.
B.	View Enhancement: 
1.	Allow for clear vision through glass at all times and lighting conditions.
2.	Glare control.
2.3	COOLVU DUAL LAYER CERAMIC TINITE WINDOW FILM
A.	Basis of Design: Tinite Ceramic 35; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 56 percent.
b.	Visible Light Transmitted: 37 percent.
c.	Visible Light Reflected to Interior: 10 percent.
d.	Visible Light Reflected to Exterior: 10 percent.
e.	Total Solar Energy Reflected: 13 percent.
f.	Total Solar Energy Absorbed: 60 percent.
g.	Total Solar Energy Transmitted: 27 percent.
h.	Glare Reduction: 62 percent.
i.	Shading Coefficient: 0.50.
j.	Solar Heat Gain Coefficient (SHGC): 0.44.
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: 83 percent.
m.	IR 0.9-1.0 Block: 77 percent.
B.	Basis of Design: Tinite Ceramic 45; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 52 percent.
b.	Visible Light Transmitted: 43 percent.
c.	Visible Light Reflected to Interior: 9 percent.
d.	Visible Light Reflected to Exterior: 9 percent.
e.	Total Solar Energy Reflected: 12 percent.
f.	Total Solar Energy Absorbed: 56 percent.
g.	Total Solar Energy Transmitted: 32 percent.
h.	Glare Reduction: 55 percent.
i.	Shading Coefficient: 0.55.
j.	Solar Heat Gain Coefficient (SHGC): 0.48.
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: 81 percent.
m.	IR 0.9-1.0 Block: 72 percent.
2.4	COOLVU DUAL REFLECTIVE
A.	Basis of Design: Dual Reflective 05; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 80 percent.
b.	Visible Light Transmitted: 6 percent.
c.	Visible Light Reflected to Interior: 11 percent.
d.	Visible Light Reflected to Exterior: 50 percent.
e.	Total Solar Energy Reflected: 52 percent.
f.	Total Solar Energy Absorbed: 37 percent.
g.	Total Solar Energy Transmitted: 11 percent.
h.	Glare Reduction: 92 percent.
i.	Shading Coefficient: 0.24.
j.	Solar Heat Gain Coefficient (SHGC): 0.20.
k.	UV Block: 99 percent
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
B.	Basis of Design: Dual Reflective 15; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 70 percent.
b.	Visible Light Transmitted: 17 percent.
c.	Visible Light Reflected to Interior: 13 percent.
d.	Visible Light Reflected to Exterior: 37 percent.
e.	Total Solar Energy Reflected: 37 percent.
f.	Total Solar Energy Absorbed: 45 percent.
g.	Total Solar Energy Transmitted: 18 percent.
h.	Glare Reduction: 81 percent.
i.	Shading Coefficient: 0.24
j.	Solar Heat Gain Coefficient (SHGC): 0.29
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
C.	Basis of Design: Dual Reflective 25; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 63 percent.
b.	Visible Light Transmitted: 28 percent.
c.	Visible Light Reflected to Interior: 18 percent.
d.	Visible Light Reflected to Exterior: 31 percent.
e.	Total Solar Energy Reflected: 31 percent.
f.	Total Solar Energy Absorbed: 44 percent.
g.	Total Solar Energy Transmitted: 25 percent.
h.	Glare Reduction: 68 percent.
i.	Shading Coefficient: 0.35
j.	Solar Heat Gain Coefficient (SHGC): 0.36
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
D.	Basis of Design: Dual Reflective 35; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 52 percent.
b.	Visible Light Transmitted: 38 percent.
c.	Visible Light Reflected to Interior: 12 percent.
d.	Visible Light Reflected to Exterior: 18 percent.
e.	Total Solar Energy Reflected: 19 percent.
f.	Total Solar Energy Absorbed: 46 percent.
g.	Total Solar Energy Transmitted: 35 percent.
h.	Glare Reduction: 57 percent.
i.	Shading Coefficient: 0.47
j.	Solar Heat Gain Coefficient (SHGC): 0.48
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
2.5	COOLVU SILVER REFLECTIVE WINDOW FILM
A.	Basis of Design: Silver 15; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 85 percent.
b.	Visible Light Transmitted: 14 percent.
c.	Visible Light Reflected to Interior: 64 percent.
d.	Visible Light Reflected to Exterior: 64 percent.
e.	Total Solar Energy Reflected: 60 percent.
f.	Total Solar Energy Absorbed: 29 percent.
g.	Total Solar Energy Transmitted: 11 percent.
h.	Glare Reduction: 84 percent.
i.	Shading Coefficient: 0.21
j.	Solar Heat Gain Coefficient (SHGC): 0.16
k.	UV Block: 99 percent
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
B.	Basis of Design: Silver 30; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 64 percent.
b.	Visible Light Transmitted: 33 percent.
c.	Visible Light Reflected to Interior: 41 percent.
d.	Visible Light Reflected to Exterior: 42 percent.
e.	Total Solar Energy Reflected: 39 percent.
f.	Total Solar Energy Absorbed: 37 percent.
g.	Total Solar Energy Transmitted: 24 percent.
h.	Glare Reduction: 63 percent.
i.	Shading Coefficient: 0.40
j.	Solar Heat Gain Coefficient (SHGC): 0.35
k.	UV Block: 99 percent
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
C.	Basis of Design: Silver 50; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 56 percent.
b.	Visible Light Transmitted: 48 percent.
c.	Visible Light Reflected to Interior: 26 percent.
d.	Visible Light Reflected to Exterior: 28 percent.
e.	Total Solar Energy Reflected: 29 percent.
f.	Total Solar Energy Absorbed: 36 percent.
g.	Total Solar Energy Transmitted: 35 percent.
h.	Glare Reduction: 47 percent.
i.	Shading Coefficient: 0.54
j.	Solar Heat Gain Coefficient (SHGC): 0.45
k.	UV Block: 99 percent
l.	IR 0.78-2.5 Block Full Spectrum: Not measured.
m.	IR 0.9-1.0 Block: Not measured.
2.6	COOLVU SPECTRALLY SELECTIVE HD WINDOW FILM
A.	Basis of Design: High Definition 70; as manufactured by CoolVu Window Films.
1.	Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
a.	Solar Energy Rejected (TSER): 53 percent.
b.	Visible Light Transmitted: 70 percent.
c.	Visible Light Reflected to Interior: 10 percent.
d.	Visible Light Reflected to Exterior: 9 percent.
e.	Total Solar Energy Reflected: 34 percent.
f.	Total Solar Energy Absorbed: 25 percent.
g.	Total Solar Energy Transmitted: 41 percent.
h.	Glare Reduction: 20 percent.
i.	Shading Coefficient: 0.56
j.	Solar Heat Gain Coefficient (SHGC): 0.49
k.	UV Block: 99 percent.
l.	IR 0.78-2.5 Block Full Spectrum: 80 percent.
m.	IR 0.9-1.0 Block: 95 percent.
2.7	COOLVU TRANSITIONAL WINDOW FILM
A.	Basis of Design: CV55/35; as manufactured by CoolVu Transitional Window Films.
1.	Performance under Normal Conditions:
a.	Solar Energy Transmitted: 46.0 percent.
b.	Solar Energy Reflected: 11.0 percent.
c.	Solar Energy Absorbed: 43.0 percent.
d.	Visible Light Transmitted: 54.0 percent.
e.	Visible Light Reflected to Exterior: 11.0 percent.
f.	Visible Light Reflected to Interior: 8.0 percent.
g.	Glare Reduction: 39.0 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.43.
i.	Shading Coefficient: 0.49.
j.	Total Solar Energy Rejection: 54.0 percent.
k.	Infrared Rejection: 81.0 percent.
l.	U-Factor: 1.9.
m.	Emissivity: 0.9.
n.	Ultraviolet Rejection: More than 99 percent.
2.	Performance Fully Transitioned:
a.	Solar Energy Transmitted: 43.0 percent.
b.	Solar Energy Reflected: 11.0 percent.
c.	Solar Energy Absorbed: 46.0 percent.
d.	Visible Light Transmitted: 35.0 percent.
e.	Visible Light Reflected to Exterior: 11.0 percent.
f.	Visible Light Reflected to Interior: 8.0 percent.
g.	Glare Reduction: 60.2 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.41.
i.	Shading Coefficient: 0.56.
j.	Total Solar Energy Rejection: 58.0 percent.
k.	Infrared Rejection: 81.0 percent.
l.	U-Factor: 1.9.
m.	Emissivity: 0.85.
n.	Ultraviolet Rejection: More than 99 percent.
B.	Basis of Design: CV35/20; as manufactured by CoolVu Transitional Window Films.
1.	Performance under Normal Conditions:
a.	Solar Energy Transmitted: 44.0 percent.
b.	Solar Energy Reflected: 15.0 percent.
c.	Solar Energy Absorbed: 41.0 percent.
d.	Visible Light Transmitted: 35.0 percent.
e.	Visible Light Reflected to Exterior: 18.0 percent.
f.	Visible Light Reflected to Interior: 15.0 percent.
g.	Glare Reduction: 61.0 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.40.
i.	Shading Coefficient: 0.46.
j.	Total Solar Energy Rejection: 56.0 percent.
k.	Infrared Rejection: 83.0 percent.
l.	U-Factor: 1.0.
m.	Emissivity: 0.9.
n.	Ultraviolet Rejection: More than 99 percent.
2.	Performance Fully Transitioned:
a.	Solar Energy Transmitted: 36.0 percent.
b.	Solar Energy Reflected: 15.0 percent.
c.	Solar Energy Absorbed: 49.0 percent.
d.	Visible Light Transmitted: 25.0 percent.
e.	Visible Light Reflected to Exterior: 18.0 percent.
f.	Visible Light Reflected to Interior: 15.0 percent.
g.	Glare Reduction: 71.5 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.36.
i.	Shading Coefficient: 0.42.
j.	Total Solar Energy Rejection: 60.0 percent.
k.	Infrared Rejection: 83.0 percent.
l.	U-Factor: 1.0.
m.	Emissivity: 0.9.
n.	Ultraviolet Rejection: More than 99 percent.
C.	Basis of Design: CV25/15; as manufactured by CoolVu Transitional Window Films.
1.	Performance under Normal Conditions:
a.	Solar Energy Transmitted: 36.0 percent.
b.	Solar Energy Reflected: 20.0 percent.
c.	Solar Energy Absorbed: 44.0 percent.
d.	Visible Light Transmitted: 28.0 percent.
e.	Visible Light Reflected to Exterior: 23.0 percent.
f.	Visible Light Reflected to Interior: 21.0 percent.
g.	Glare Reduction: 69.0 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.35.
i.	Shading Coefficient: 0.40.
j.	Total Solar Energy Rejection: 64.0 percent.
k.	Infrared Rejection: 85.0 percent.
l.	U-Factor: 1.0.
m.	Emissivity: 0.9.
n.	Ultraviolet Rejection: More than 99 percent.
2.	Performance Fully Transitioned:
a.	Solar Energy Transmitted: 33.0 percent.
b.	Solar Energy Reflected: 20.0 percent.
c.	Solar Energy Absorbed: 47.0 percent.
d.	Visible Light Transmitted: 18.0 percent.
e.	Visible Light Reflected to Exterior: 23.0 percent.
f.	Visible Light Reflected to Interior: 21.0 percent.
g.	Glare Reduction: 79.5 percent.
h.	Solar Heat Gain Coefficient (SHGC): 0.33.
i.	Shading Coefficient: 0.38.
j.	Total Solar Energy Rejection: 66.0 percent.
k.	Infrared Rejection: 85.0 percent.
l.	U-Factor: 1.0.
m.	Emissivity: 0.9.
n.	Ultraviolet Rejection: More than 99 percent.
2.8	COOLVU CERAMIC WINDOW FILM
A.	Basis of Design: Signature Ceramic Tinted; as manufactured by CoolVu Transitional Window Films. a single layer of ceramic nanoparticles, retrofit window film solution. Non-mirror appearance on window and door glass both day and night. "True" ceramic TiN construction.
1.	Performance Under Normal Conditions:
a.	VLT: 45 percent.
b.	IR Block: 70 percent.
c.	UV Block: 99 percent.
d.	Ext. Reflection: 13 percent.
e.	Int. Reflection: 12 percent.
f.	TSER: 56 percent.
B.	Basis of Design: Signature Ceramic Clear; as manufactured by CoolVu Transitional Window Films. a single layer of ceramic nanoparticles, retrofit window film solution. Non-mirror appearance on window and door glass both day and night. "True" ceramic TiN construction.
1.	Performance Under Normal Conditions:
a.	VLT: 66 percent.
b.	IR Block: 70 percent.
c.	UV Block: 99 percent.
d.	Ext. Reflection: 8 percent.
e.	Int. Reflection: 8 percent.
f.	TSER: 38 percent.
PART 3    EXECUTION
3.1	EXAMINATION
A.	Do not begin installation until substrates have been properly constructed and prepared.
B.	If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.
3.2	PREPARATION
A.	Clean surfaces thoroughly prior to installation.
B.	Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.
3.3	INSTALLATION
A.	Install in accordance with manufacturer's instructions approved submittals and in proper relationship with adjacent construction.
3.4	CLEANING AND PROTECTION
A.	Clean products in accordance with the manufacturer's recommendations. 
B.	Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION