SECTION 08 87 00

WINDOW FILMS

Display hidden notes to specifier. (Don't know how? [Click Here](https://www.arcat.com/sd/display_hidden_notes.shtml))

*Copyright 2019 - 2024 ARCAT, Inc. - All rights reserved*

\*\* NOTE TO SPECIFIER \*\* CoolVu, LLC; photochromic or transitional window films.  
This section is based on the products of CoolVu, LLC, which is located at:4939 Lower Roswell Rd., Bldg. BMarietta, GA 30068Tel: 844-426-6588Email: [request info (info@coolvu.com)](https://arcat.com/rfi?action=email&company=CoolVu%252C%252BLLC&message=RE%253A%2520Spec%2520Question%2520(08870coo)%253A%2520&coid=52450&spec=08870coo&rep=&fax=)  
Web: <https://www.coolvu.com>   
 [ [Click Here](https://arcat.com/company/coolvu-llc-52450) ] for additional information.  
From commercial building facades and retail storefronts to modern architectural applications, CoolVu Window Films are some of the most functional and attractive options on the market today. Unlike static window film and tinting solutions, CoolVu Window Films are recognized by their ability to adapt to the intensity of sunlight, dynamically optimizing the indoor environment for energy efficiency and thermal comfort.  
Engineered using proprietary photochromic technology, CoolVu Window Film activates from clear to tinted when exposed to sunlight. By adapting to the amount of sunlight exposure, CoolVu provides much needed sun control only when you really need it. In turn, you can enjoy 99% blockage of UV rays and up to 80% reduction in solar-induced heat increases without compromising the sun's natural light.  
The CoolVu™ brand is available throughout the US and Canada from trained and certified franchisees by CoolVu, LLC.

1. GENERAL
   1. SECTION INCLUDES
      1. Window films for retrofit onto existing building doors, windows, storefront and curtain wall.
         1. Dual layer ceramic Tinite window film. (Tinite Ceramic 35) (Tinite Ceramic 45)
         2. Dual reflective window film. (Dual Reflective 05) (Dual Reflective 15) (Dual Reflective 25) (Dual Reflective 35)
         3. Silver reflective window film. (Silver 15) (Silver 30) (Silver 50)
         4. Spectrally selective high definition window film. (High Definition 70)
         5. Transitional window film. (CV55/35) (CV35/20) (CV25/15)
   2. RELATED SECTIONS

\*\* NOTE TO SPECIFIER \*\* Delete any sections below not relevant to this project; add others as required.

* + 1. Section 08 40 00 - Entrances, Storefronts, and Curtain Walls.
    2. Section 08 50 00 - Windows.
    3. Section 08 60 00 - Roof Windows and Skylights.
    4. Section 08 83 13 - Mirrored Glass Glazing.
  1. SUBMITTALS
     1. Submit under provisions of Section 01 30 00 - Administrative Requirements.
     2. Product Data:
        1. Manufacturer's data sheets on each product to be used.
        2. Preparation instructions and recommendations.
        3. Storage and handling requirements and recommendations.
        4. Typical installation methods.

\*\* NOTE TO SPECIFIER \*\* Delete if not applicable to product type.

* + 1. Verification Samples: Two representative units of each type, size, pattern and color.
    2. Shop Drawings: Include details of materials, construction and finish. Include relationship with adjacent construction.
  1. QUALITY ASSURANCE
     1. Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.
     2. Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.
     3. Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

\*\* NOTE TO SPECIFIER \*\* Include mock-up if the project size or quality warrant the expense. The following is one example of how a mock-up on might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.

* + 1. Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.
       1. Intent of mock-up is to demonstrate quality of workmanship and visual appearance.
       2. If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.
       3. Retain mock-up during construction as a standard for comparison with completed work.
       4. Do not alter or remove mock-up until work is completed or removal is authorized.
  1. PRE-INSTALLATION CONFERENCE
     1. Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.
  2. DELIVERY, STORAGE, AND HANDLING
     1. Store and handle in strict compliance with manufacturer's written instructions and recommendations.
     2. Protect from damage due to weather, excessive temperature, and construction operations.
  3. PROJECT CONDITIONS
     1. Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.
  4. WARRANTY
     1. Manufacturer's Warranty: Manufacturer's standard 10 year limited warranty. Will not blister, peel, change color, or bubble.
        1. Photochromic reactions are warranted for a minimum of five (5) years from date of installation. Extended warranty option available.

1. PRODUCTS
   1. MANUFACTURERS
      1. Acceptable Manufacturer: CoolVu, LLC, which is located at:4939 Lower Roswell Rd., Bldg. BMarietta, GA 30068Tel: 844-426-6588Email: [request info (info@coolvu.com)](https://arcat.com/rfi?action=email&company=CoolVu%252C%252BLLC&message=RE%253A%2520Spec%2520Question%2520(08870coo)%253A%2520&coid=52450&spec=08870coo&rep=&fax=);Web: <https://www.coolvu.com>

\*\* NOTE TO SPECIFIER \*\* Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

* + 1. Substitutions: Not permitted.
    2. Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

CoolVu photochromic window films adapt to the intensity of sunlight on your window and door glass. CoolVu "transitions" from a lighter state to a darker, tinted state when exposed to direct sun. The patented photochromic molecular structure of CoolVu is the world's first stable climate responsive window film. Now you can enjoy clear windows when wanted and tinted windows when needed.

* 1. PERFORMANCE REQUIREMENTS
     1. Energy Performance:
        1. Block Ultraviolet Radiation: 99 percent.
        2. Block Infrared Energy: 80 percent.
        3. Transition: Up to 35 percent.
        4. Control Sun Glare: Up to 80 percent.
     2. View Enhancement:
        1. Allow for clear vision through glass at all times and lighting conditions.
        2. Glare control.

\*\* NOTE TO SPECIFIER \*\* CoolVu "TiN" dual layer ceramic window film series is constructed with two layers of titanium nitride (TiN) ceramic nanoparticles creating the richest looking and highest performing ceramic window film in the world. Manufactured in the US, the unique process and highest quality base materials behind CoolVu Tinite ensures that customers enjoy the clearest possible views through glass with the lowest interior and exterior reflection while experiencing impressive solar heat and UV block. Delete article if not required.

* 1. COOLVU DUAL LAYER CERAMIC TINITE WINDOW FILM

\*\* NOTE TO SPECIFIER \*\* Delete basis of design option not required.

* + 1. Basis of Design: Tinite Ceramic 35; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 56 percent.
          2. Visible Light Transmitted: 37 percent.
          3. Visible Light Reflected to Interior: 10 percent.
          4. Visible Light Reflected to Exterior: 10 percent.
          5. Total Solar Energy Reflected: 13 percent.
          6. Total Solar Energy Absorbed: 60 percent.
          7. Total Solar Energy Transmitted: 27 percent.
          8. Glare Reduction: 62 percent.
          9. Shading Coefficient: 0.50.
          10. Solar Heat Gain Coefficient (SHGC): 0.44.
          11. UV Block: 99 percent.
          12. IR 0.78-2.5 Block Full Spectrum: 83 percent.
          13. IR 0.9-1.0 Block: 77 percent.
    2. Basis of Design: Tinite Ceramic 45; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 52 percent.
          2. Visible Light Transmitted: 43 percent.
          3. Visible Light Reflected to Interior: 9 percent.
          4. Visible Light Reflected to Exterior: 9 percent.
          5. Total Solar Energy Reflected: 12 percent.
          6. Total Solar Energy Absorbed: 56 percent.
          7. Total Solar Energy Transmitted: 32 percent.
          8. Glare Reduction: 55 percent.
          9. Shading Coefficient: 0.55.
          10. Solar Heat Gain Coefficient (SHGC): 0.48.
          11. UV Block: 99 percent.
          12. IR 0.78-2.5 Block Full Spectrum: 81 percent.
          13. IR 0.9-1.0 Block: 72 percent.

\*\* NOTE TO SPECIFIER \*\* CoolVu DR series provide residential and light commercial consumers all the benefits of strong sun and glare control while maintaining clear viewing from the inside - out both day and night. Manufactured in the US, CoolVu DR architectural window films incorporate premium grade materials ensuring your home or building glass performs and looks Cool for a lifetime. Delete article if not required.

* 1. COOLVU DUAL REFLECTIVE

\*\* NOTE TO SPECIFIER \*\* Delete basis of design options not required.

* + 1. Basis of Design: Dual Reflective 05; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 80 percent.
          2. Visible Light Transmitted: 6 percent.
          3. Visible Light Reflected to Interior: 11 percent.
          4. Visible Light Reflected to Exterior: 50 percent.
          5. Total Solar Energy Reflected: 52 percent.
          6. Total Solar Energy Absorbed: 37 percent.
          7. Total Solar Energy Transmitted: 11 percent.
          8. Glare Reduction: 92 percent.
          9. Shading Coefficient: 0.24.
          10. Solar Heat Gain Coefficient (SHGC): 0.20.
          11. UV Block: 99 percent
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.
    2. Basis of Design: Dual Reflective 15; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 70 percent.
          2. Visible Light Transmitted: 17 percent.
          3. Visible Light Reflected to Interior: 13 percent.
          4. Visible Light Reflected to Exterior: 37 percent.
          5. Total Solar Energy Reflected: 37 percent.
          6. Total Solar Energy Absorbed: 45 percent.
          7. Total Solar Energy Transmitted: 18 percent.
          8. Glare Reduction: 81 percent.
          9. Shading Coefficient: 0.24
          10. Solar Heat Gain Coefficient (SHGC): 0.29
          11. UV Block: 99 percent.
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.
    3. Basis of Design: Dual Reflective 25; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 63 percent.
          2. Visible Light Transmitted: 28 percent.
          3. Visible Light Reflected to Interior: 18 percent.
          4. Visible Light Reflected to Exterior: 31 percent.
          5. Total Solar Energy Reflected: 31 percent.
          6. Total Solar Energy Absorbed: 44 percent.
          7. Total Solar Energy Transmitted: 25 percent.
          8. Glare Reduction: 68 percent.
          9. Shading Coefficient: 0.35
          10. Solar Heat Gain Coefficient (SHGC): 0.36
          11. UV Block: 99 percent.
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.
    4. Basis of Design: Dual Reflective 35; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 52 percent.
          2. Visible Light Transmitted: 38 percent.
          3. Visible Light Reflected to Interior: 12 percent.
          4. Visible Light Reflected to Exterior: 18 percent.
          5. Total Solar Energy Reflected: 19 percent.
          6. Total Solar Energy Absorbed: 46 percent.
          7. Total Solar Energy Transmitted: 35 percent.
          8. Glare Reduction: 57 percent.
          9. Shading Coefficient: 0.47
          10. Solar Heat Gain Coefficient (SHGC): 0.48
          11. UV Block: 99 percent.
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.

\*\* NOTE TO SPECIFIER \*\* Manufactured in the US, these films provide an economical solution for solar control keeping your building running cool while saving on HVAC costs. Daytime privacy is enhanced with CoolVu silver reflective window films. A manufacturer's commercial warranty of up to 15 years is available protecting you from bubbles, de-lamination and discoloration for the lifetime of your installation. Delete article if not required.

* 1. COOLVU SILVER REFLECTIVE WINDOW FILM

\*\* NOTE TO SPECIFIER \*\* Delete basis of design options not required.

* + 1. Basis of Design: Silver 15; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 85 percent.
          2. Visible Light Transmitted: 14 percent.
          3. Visible Light Reflected to Interior: 64 percent.
          4. Visible Light Reflected to Exterior: 64 percent.
          5. Total Solar Energy Reflected: 60 percent.
          6. Total Solar Energy Absorbed: 29 percent.
          7. Total Solar Energy Transmitted: 11 percent.
          8. Glare Reduction: 84 percent.
          9. Shading Coefficient: 0.21
          10. Solar Heat Gain Coefficient (SHGC): 0.16
          11. UV Block: 99 percent
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.
    2. Basis of Design: Silver 30; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 64 percent.
          2. Visible Light Transmitted: 33 percent.
          3. Visible Light Reflected to Interior: 41 percent.
          4. Visible Light Reflected to Exterior: 42 percent.
          5. Total Solar Energy Reflected: 39 percent.
          6. Total Solar Energy Absorbed: 37 percent.
          7. Total Solar Energy Transmitted: 24 percent.
          8. Glare Reduction: 63 percent.
          9. Shading Coefficient: 0.40
          10. Solar Heat Gain Coefficient (SHGC): 0.35
          11. UV Block: 99 percent
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.
    3. Basis of Design: Silver 50; as manufactured by CoolVu Window Films.
       1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
          1. Solar Energy Rejected (TSER): 56 percent.
          2. Visible Light Transmitted: 48 percent.
          3. Visible Light Reflected to Interior: 26 percent.
          4. Visible Light Reflected to Exterior: 28 percent.
          5. Total Solar Energy Reflected: 29 percent.
          6. Total Solar Energy Absorbed: 36 percent.
          7. Total Solar Energy Transmitted: 35 percent.
          8. Glare Reduction: 47 percent.
          9. Shading Coefficient: 0.54
          10. Solar Heat Gain Coefficient (SHGC): 0.45
          11. UV Block: 99 percent
          12. IR 0.78-2.5 Block Full Spectrum: Not measured.
          13. IR 0.9-1.0 Block: Not measured.

\*\* NOTE TO SPECIFIER \*\* Manufactured in the US utilizing a proprietary blend of titanium nitride and exotic metals, CoolVu's HD window films feature superior optical clarity, block 99% of the sun's UV radiation and have a soft, natural appearance on glass. A manufacturer's commercial warranty of up to 15 years is available protecting you from bubbles, de-lamination and discoloration for the lifetime of your installation. Delete article if not required.

* 1. COOLVU SPECTRALLY SELECTIVE HD WINDOW FILM
     1. Basis of Design: High Definition 70; as manufactured by CoolVu Window Films.
        1. Performance Requirements: Substrate of 1/8 inch (3 mm) clear glass,
           1. Solar Energy Rejected (TSER): 53 percent.
           2. Visible Light Transmitted: 70 percent.
           3. Visible Light Reflected to Interior: 10 percent.
           4. Visible Light Reflected to Exterior: 9 percent.
           5. Total Solar Energy Reflected: 34 percent.
           6. Total Solar Energy Absorbed: 25 percent.
           7. Total Solar Energy Transmitted: 41 percent.
           8. Glare Reduction: 20 percent.
           9. Shading Coefficient: 0.56
           10. Solar Heat Gain Coefficient (SHGC): 0.49
           11. UV Block: 99 percent.
           12. IR 0.78-2.5 Block Full Spectrum: 80 percent.
           13. IR 0.9-1.0 Block: 95 percent.

\*\* NOTE TO SPECIFIER \*\* Adaptive to the amount of sunlight on glass, CV Transitional window films are made using a proprietary manufacturing process resulting in the world's only patented "stable photochromic" film technology. CoolVu photochromic window films adapt to the intensity of sunlight on your window and door glass. CoolVu "transitions" from a lighter state to a darker, tinted state when exposed to direct sun. The patented photochromic molecular structure of CoolVu is the world's first stable climate responsive window film. Now you can enjoy clear windows when wanted and tinted windows when needed. Delete article if not required.

* 1. COOLVU TRANSITIONAL WINDOW FILM

\*\* NOTE TO SPECIFIER \*\* Delete basis of design products not required.

* + 1. Basis of Design: CV55/35; as manufactured by CoolVu Transitional Window Films.
       1. Performance under Normal Conditions:
          1. Solar Energy Transmitted: 46.0 percent.
          2. Solar Energy Reflected: 11.0 percent.
          3. Solar Energy Absorbed: 43.0 percent.
          4. Visible Light Transmitted: 54.0 percent.
          5. Visible Light Reflected to Exterior: 11.0 percent.
          6. Visible Light Reflected to Interior: 8.0 percent.
          7. Glare Reduction: 39.0 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.43.
          9. Shading Coefficient: 0.49.
          10. Total Solar Energy Rejection: 54.0 percent.
          11. Infrared Rejection: 81.0 percent.
          12. U-Factor: 1.9.
          13. Emissivity: 0.9.
          14. Ultraviolet Rejection: More than 99 percent.
       2. Performance Fully Transitioned:
          1. Solar Energy Transmitted: 43.0 percent.
          2. Solar Energy Reflected: 11.0 percent.
          3. Solar Energy Absorbed: 46.0 percent.
          4. Visible Light Transmitted: 35.0 percent.
          5. Visible Light Reflected to Exterior: 11.0 percent.
          6. Visible Light Reflected to Interior: 8.0 percent.
          7. Glare Reduction: 60.2 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.41.
          9. Shading Coefficient: 0.56.
          10. Total Solar Energy Rejection: 58.0 percent.
          11. Infrared Rejection: 81.0 percent.
          12. U-Factor: 1.9.
          13. Emissivity: 0.85.
          14. Ultraviolet Rejection: More than 99 percent.
    2. Basis of Design: CV35/20; as manufactured by CoolVu Transitional Window Films.
       1. Performance under Normal Conditions:
          1. Solar Energy Transmitted: 44.0 percent.
          2. Solar Energy Reflected: 15.0 percent.
          3. Solar Energy Absorbed: 41.0 percent.
          4. Visible Light Transmitted: 35.0 percent.
          5. Visible Light Reflected to Exterior: 18.0 percent.
          6. Visible Light Reflected to Interior: 15.0 percent.
          7. Glare Reduction: 61.0 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.40.
          9. Shading Coefficient: 0.46.
          10. Total Solar Energy Rejection: 56.0 percent.
          11. Infrared Rejection: 83.0 percent.
          12. U-Factor: 1.0.
          13. Emissivity: 0.9.
          14. Ultraviolet Rejection: More than 99 percent.
       2. Performance Fully Transitioned:
          1. Solar Energy Transmitted: 36.0 percent.
          2. Solar Energy Reflected: 15.0 percent.
          3. Solar Energy Absorbed: 49.0 percent.
          4. Visible Light Transmitted: 25.0 percent.
          5. Visible Light Reflected to Exterior: 18.0 percent.
          6. Visible Light Reflected to Interior: 15.0 percent.
          7. Glare Reduction: 71.5 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.36.
          9. Shading Coefficient: 0.42.
          10. Total Solar Energy Rejection: 60.0 percent.
          11. Infrared Rejection: 83.0 percent.
          12. U-Factor: 1.0.
          13. Emissivity: 0.9.
          14. Ultraviolet Rejection: More than 99 percent.
    3. Basis of Design: CV25/15; as manufactured by CoolVu Transitional Window Films.
       1. Performance under Normal Conditions:
          1. Solar Energy Transmitted: 36.0 percent.
          2. Solar Energy Reflected: 20.0 percent.
          3. Solar Energy Absorbed: 44.0 percent.
          4. Visible Light Transmitted: 28.0 percent.
          5. Visible Light Reflected to Exterior: 23.0 percent.
          6. Visible Light Reflected to Interior: 21.0 percent.
          7. Glare Reduction: 69.0 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.35.
          9. Shading Coefficient: 0.40.
          10. Total Solar Energy Rejection: 64.0 percent.
          11. Infrared Rejection: 85.0 percent.
          12. U-Factor: 1.0.
          13. Emissivity: 0.9.
          14. Ultraviolet Rejection: More than 99 percent.
       2. Performance Fully Transitioned:
          1. Solar Energy Transmitted: 33.0 percent.
          2. Solar Energy Reflected: 20.0 percent.
          3. Solar Energy Absorbed: 47.0 percent.
          4. Visible Light Transmitted: 18.0 percent.
          5. Visible Light Reflected to Exterior: 23.0 percent.
          6. Visible Light Reflected to Interior: 21.0 percent.
          7. Glare Reduction: 79.5 percent.
          8. Solar Heat Gain Coefficient (SHGC): 0.33.
          9. Shading Coefficient: 0.38.
          10. Total Solar Energy Rejection: 66.0 percent.
          11. Infrared Rejection: 85.0 percent.
          12. U-Factor: 1.0.
          13. Emissivity: 0.9.
          14. Ultraviolet Rejection: More than 99 percent.

\*\* NOTE TO SPECIFIER \*\* Delete article if not required.

* 1. COOLVU CERAMIC WINDOW FILM

\*\* NOTE TO SPECIFIER \*\* CoolVu Ceramic Series window film is constructed witha single layer of ceramic nanoparticlescreating a rich looking and high performing retrofit window film solution. The soft, natural look of the Ceramic Series provides for non-mirror appearance on window and door glass both day and night, perfect for home and building glass. Manufactured in the US, the unique process and high-quality materials behind CoolVu Ceramic Series ensures that customers enjoy clear views through glass with low interior and exterior reflection while experiencing impressive solar heat and UV block. Delete basis of design products not required.

* + 1. Basis of Design: Signature Ceramic Tinted; as manufactured by CoolVu Transitional Window Films. a single layer of ceramic nanoparticles, retrofit window film solution. Non-mirror appearance on window and door glass both day and night. "True" ceramic TiN construction.
       1. Performance Under Normal Conditions:
          1. VLT: 45 percent.
          2. IR Block: 70 percent.
          3. UV Block: 99 percent.
          4. Ext. Reflection: 13 percent.
          5. Int. Reflection: 12 percent.
          6. TSER: 56 percent.
    2. Basis of Design: Signature Ceramic Clear; as manufactured by CoolVu Transitional Window Films. a single layer of ceramic nanoparticles, retrofit window film solution. Non-mirror appearance on window and door glass both day and night. "True" ceramic TiN construction.
       1. Performance Under Normal Conditions:
          1. VLT: 66 percent.
          2. IR Block: 70 percent.
          3. UV Block: 99 percent.
          4. Ext. Reflection: 8 percent.
          5. Int. Reflection: 8 percent.
          6. TSER: 38 percent.

1. EXECUTION
   1. EXAMINATION
      1. Do not begin installation until substrates have been properly constructed and prepared.
      2. If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.
   2. PREPARATION
      1. Clean surfaces thoroughly prior to installation.
      2. Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.
   3. INSTALLATION
      1. Install in accordance with manufacturer's instructions approved submittals and in proper relationship with adjacent construction.
   4. CLEANING AND PROTECTION
      1. Clean products in accordance with the manufacturer's recommendations.
      2. Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION