SECTION 06 13 00

REDWOOD LUMBER AND TIMBERS

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2016 -    2022 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** Humboldt Sawmill; Redwood Lumber and Timbers
This section is based on the products of Humboldt Sawmill, which is located at:<BR />169 Main St.<BR />Scotia, CA 95565<BR />Tel: 707-764-4472 <BR />Fax: 707-764-4444<BR />Email: request info (marketing@mendoco.com)
Web: http://www.getredwood.com    
 [ Click Here ] for additional information.
Humboldt Sawmill is the leading supplier of Forest Stewardship Council (FSC® C013133) certified redwood and Douglas-fir lumber products; logs are sourced from 440,000 acres of company-owned timberlands in California. An additional 400,000 acres are available under a long-term log purchase agreement. Products manufactured at company-owned mills include redwood decking, timbers, and uppers, as well as Douglas-fir joists and planks, posts and beams. All products available FSC certified at dealers and distributors throughout the Western U.S. and beyond.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Redwood products including the following:

      - Timbers.

      - Decking.

      - Siding.

      - Lumber.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 06 10 00 - Rough Carpentry.

  - REFERENCES

    - Redwood Inspection Service (RIS) Standard Specifications for Grades of California Redwood Lumber 2019 Edition.

    - PS 20 - American Softwood Lumber Standard - US Department of Commerce, National Institute of Standards and Technology.

    - ASTM E84: Standard Test Method for Surface Burning Characteristics of Building Materials.

    - California Building Code Chapter 7A: Materials and Construction Methods for Exterior Wildfire Exposure.

    - Forest Stewardship Council (FSC) Certification: Humboldt Sawmill.

      - FSC 100 percent; FSC Mix, FSC Controlled Wood

        - Certificate Code: SCS-COC-000180 Trademark License Code: FSC C013133

      - Well Managed Multiple Natural Forest Management Units Certification

        - Certificate Code: SCS-FM/COC-00120N Trademark License Code: FSC C031337

    - Redwood Lumber Patterns No. 17.

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data: Manufacturer's data sheets on each product to be used, including:

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Installation methods.

** NOTE TO SPECIFIER ** Delete the following if LEED certification is not applicable.

    - LEED v4 Submittals: Provide documentation of how the requirements shall be met for the following credits:

      - Building product disclosure and optimization - sourcing of raw materials

        - Option 2. Leadership extraction practices (1 point). Wood products. Wood products must be certified by the Forest Stewardship Council (FSC) or USGBC-approved equivalent. Products meeting wood products criteria are valued at 100 percent of their cost for the purposes of credit achievement calculation.

** NOTE TO SPECIFIER ** Delete the following if SITES certification is not applicable.

    - SITES v2 Submittals: Provide documentation of how the requirements shall be met for the following credits:

      - Credit 5.7: Support responsible extraction of raw materials

        - Option 3. Support raw material suppliers and/or manufacturers that meet or exceed standards for raw material extraction (5 points). New wood products: be certified by the Forest Stewardship Council (FSC) (or local equivalent for products outside the United States).

** NOTE TO SPECIFIER ** Delete the following if FSC certification is not applicable.

    - FSC Submittals: Provide documentation indicating manufacturer is FSC Chain-of-Custody certified.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver and store products in manufacturer's unopened packaging bearing the brand name and manufacturer's identification until ready for installation.

    - Handle materials to avoid damage.

    - Store on a level surface with blocking to keep boards off the ground and provide uniform and adequate support.

    - Redwood timbers contain water soluble extractives (tannins) which can stain concrete or other masonry. If stored over concrete, cover the concrete with a tarp to prevent staining in the event of rain.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - SEQUENCING

    - Ensure that products of this section are supplied to affected trades in time to prevent interruption of construction progress.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: Humboldt Sawmill, which is located at:<BR />169 Main St.<BR />Scotia, CA 95565<BR />Tel: 707-764-4472 <BR />Fax: 707-764-4444<BR />Email: request info (marketing@mendoco.com);Web: http://www.getredwood.com

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

** NOTE TO SPECIFIER ** Delete if not required.

  - TIMBERS

** NOTE TO SPECIFIER ** Select material required. Reference Redwood Inspection Service (RIS) Standard Specifications for Grades of California Redwood Lumber.

    - Material: Redwood.

    - Posts and Timbers:

      - Grade: No. 2 Structural.

      - Grade: Heart B.

      - Grade: Construction Heart.

** NOTE TO SPECIFIER ** Select either rough green or surfaced four sides.

      - Rough green.

      - Surfaced four sides.

      - Posts: 4 x 4.

      - NOTE TO SPECIFIER ** Select post size required. Posts are typically 4 x 4 or larger (standard nominal sizes). Larger sizes are special order.

      - Posts: 6 x 6.

      - Posts: 8 x 8.

      - Posts: 10 x 10.

      - Posts: 12 x 12.

** NOTE TO SPECIFIER ** Select beam size required. Beams are typically 4 x 6 or larger (standard nominal sizes). Larger sizes are special order.

      - Beams: 4 x 6.

      - Beams: 4 x 8.

      - Beams: 4 x 10.

      - Beams: 4 x 12

      - Beams: 6 x 8.

      - Beams: 6 x 10.

      - Beams: 6 x 12.

      - Beams: 8 x 10.

      - Beams: 8 x 12.

      - Beams: 10 x 12.

** NOTE TO SPECIFIER ** Available lengths are 8 to 24 feet.

      - Length: 8 feet minimum.

      - Length: 24 feet maximum.

** NOTE TO SPECIFIER ** Delete if not required.

  - DECKING

    - Material: Redwood.

      - Flame Spread per ASTM E84: Class B.

      - California Building Code Chapter 7A: Materials and Construction Methods for Exterior Wildfire Exposure.

    - Wood Decking:

** NOTE TO SPECIFIER ** Select grade required.

      - Grade: Heart B.

      - Grade: Construction Heart.

      - Grade: B Grade.

      - Grade: Construction Common.

      - Grade: Heart Clear.

      - Grade: Clear.

** NOTE TO SPECIFIER ** Select decking size required. Grades may be available in other sizes.

        - Size: 2 x 4.

        - Size: 2 x 6.

** NOTE TO SPECIFIER ** Select length required. Available lengths are 6 to 20 feet.

        - Length: 6 feet minimum.

        - Length: 20 feet maximum.

** NOTE TO SPECIFIER ** Select spacing required.

      - Support Spacing, Decking Perpendicular to Supports: 24 inches (2x6).

      - Support Spacing, Decking Perpendicular to Supports: 16 inches (2x4).

      - Support Spacing, Decking Diagonal to Supports: 16 inches (2x6).

      - Support Spacing, Decking Diagonal to Supports: 12 inches (2x4).

** NOTE TO SPECIFIER ** Delete if not required.

  - SIDING

    - Material: Redwood.

    - Grade:

** NOTE TO SPECIFIER ** Delete grades not required.

      - Heart Clear.

      - Heart B.

      - Clear.

      - B Grade.

    - Texture:

** NOTE TO SPECIFIER ** Delete texture not required.

      - Surfaced.

      - Saw-textured.

    - Thickness: 1 inch, nominal.

    - Width:

** NOTE TO SPECIFIER ** Delete widths not required.

      - 4 inch, nominal.

      - 6 inch, nominal.

      - 8 inch, nominal.

      - 10 inch, nominal.

    - Length:

** NOTE TO SPECIFIER ** Select length required. Available lengths are 6 to 20 feet.

      - Length: 6 feet, minimum.

      - Length: 20 feet, maximum.

    - Siding Patterns:

** NOTE TO SPECIFIER ** Delete types not required. Reference California Redwood Association Redwood Lumber Patterns No. 17.

      - Bevel.

      - Board and Batten.

      - Rabbeted Bevel.

      - Shiplap.

      - Tongue and Groove.

    - Pattern Number: Refer to Reference document, "Redwood Lumber Patterns No. 17".

** NOTE TO SPECIFIER ** Delete if not required.

  - LUMBER

    - Material: Redwood.

    - Grade:

** NOTE TO SPECIFIER ** Select grades required.

      - Construction Heart.

      - Heart B.

      - Heart Clear.

      - Construction Common.

      - B Grade.

      - Clear.

    - Surface:

** NOTE TO SPECIFIER ** Select surfacing required.

      - Rough.

      - Surfaced Four Sides.

      - Surfaced One Side, Two Edges.

    - Sizes:

** NOTE TO SPECIFIER ** Select sizes required. Available in 1 x 2 through 1 x 12 and 2 x 2 through 2 x 12.

      - 1 x 2.

      - 1 x 4.

      - 1 x 6.

      - 1 x 8.

      - 1 x 10.

      - 1 x 12.

      - 2 x 2.

      - 2 x 4.

      - 2 x 6.

      - 2 x 8.

      - 2 x 10.

      - 2 x 12.

    - Lengths:

** NOTE TO SPECIFIER ** Select lengths required. Available lengths are 6 to 20 feet.

      - Length: 6 feet, minimum.

      - Length: 20 feet, maximum.

  - FASTENERS

** NOTE TO SPECIFIER ** Delete type of fastener not required.

    - Material: Stainless steel.

    - Material: Hot-dip galvanized steel.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly prepared.

    - If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions.

    - Finish products in accordance with manufacturer's instructions.

    - Use only corrosion resistant fasteners. Acceptable are stainless steel or hot-dipped galvanized nails.

    - Joints shall fall over framing lumber and shall be double nailed. Do not nail any less than 1/2 inch from any edge and fasten at a minimum of every 24 inches on center.

    - Drive nails perpendicular to the framing lumber and the wood product; drive nails flush with the product's surface. Nails shall penetrate at least 1-1/4 inches into the structural framing.

  - PROTECTION

    - Protect installed products until completion of project.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION