SECTION 05 51 00

METAL STAIRS, LADDERS, HANDRAILS, AND GUARD RAILS

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2022 -    2022 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** Panel Built Inc.; In-plant Offices, Mezzanine Platforms, Security Booths, Ballistic Rated Buildings and Cleanrooms.
This section is based on the products of Panel Built Inc., which is located at:<BR />302 Beasley St., P. O. Box 2658    <BR />Blairsville, GA 30514<BR />Toll Free Tel: 800-636-3873 <BR />Tel: 706-745-6540 <BR />Fax: 800-594-3245 <BR />Email: request info (info@panelbuilt.com)
Web: https://www.panelbuilt.com    
 [ Click Here ] for additional information.
Panel Built was founded in 1995 by brothers Pat and Mike Kiernan and began with the construction of pre-manufactured buildings. Today, Panel Built offers a complete line of custom modular offices, mezzanines, security booths, pre-assembled exterior buildings, and cleanrooms. All our multiple product lines are produced on-site, in four state-of-the-art manufacturing facilities. We offer "A Better Way to Create Space" for all of your building projects.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Metal Stairs:

      - Stairs with concrete treads.

      - Stairs with grating treads.

      - Stairs with metal treads.

      - Structural steel stair framing and supports.

    - Handrails and rail guards.

    - Ladders

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section [5-digit section no.] - [Section Title in initial caps].

    - Section [5-digit section no.] - [Section Title].

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

  - REFERENCE STANDARDS

    - 36 CFR 1191 - Americans with Disabilities Act Accessibility Guidelines for Buildings and Facilities; Final Rule; current edition; (ADA Standards for Accessible Design).

    - ASTM International (ASTM):

      - ASTM A6/A6M - Standard Specification for General Requirements for Rolled Structural Steel Bars, Plates, Shapes, and Sheet Piling; current edition.

      - ASTM A36/A36M - Standard Specification for Carbon Structural Steel; current edition.

      - ASTM A53/A53M - Standard Specification for Pipe, Steel, Black and Hot-Dipped, Zinc-Coated, Welded and Seamless; current edition.

      - ASTM A123/A123M - Standard Specification for Zinc (Hot-Dip Galvanized) Coatings on Iron and Steel Products; current edition.

      - ASTM A153/A153M - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware; current edition.

      - ASTM A167 - Standard Specification for Stainless and Heat-Resisting Chromium-Nickel Steel Plate, Sheet, and Strip; current edition.

      - ASTM A283/A283M - Standard Specification for Low and Intermediate Tensile Strength Carbon Steel Plates; current edition.

      - ASTM A325 - Standard Specification for Structural Bolts, Steel, Heat Treated, 120/105 ksi Minimum Tensile Strength; current edition.

      - ASTM A325M - Standard Specification for Structural Bolts, Steel, Heat Treated 830 MPa Tensile Strength (Metric); current edition.

      - ASTM A786/A786M - Standard Specification for Hot-Rolled Carbon, Low-Alloy, High-Strength Low-Alloy, and Alloy Steel Floor Plates; current edition.

    - American Welding Society(AWS):

      - AWS A2.4 - Standard Symbols for Welding, Brazing, and Nondestructive Examination; American Welding Society; current edition.

      - AWS D1.1/D1.1M - Structural Welding Code - Steel; American Welding Society; current edition.

    - International Accreditation Service (IAS):

      - IAS AC172 - Accreditation Criteria for Fabricator Inspection Programs for Structural Steel; current edition.

    - National Association of Architectural Metal Manufacturers (NAAM):

      - NAAMM AMP 510 - Metal Stairs Manual; The National Association of Architectural Metal Manufacturers; current edition.

      - NAAMM MBG 531 - Metal Bar Grating Manual; The National Association of Architectural Metal Manufacturers; current edition.

      - NAAMM MBG 532 - Heavy Duty Metal Bar Grating Manual; current edition (ANSI/NAAMM MBG 532).

    - Society for Protective Coatings (SSPC):

      - SSPC-Paint 15: Steel Joist Shop Primer; Society for Protective Coatings; current edition.

      - SSPC-SP 2: Hand Tool Cleaning; Society for Protective Coatings; current edition.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data:

      - Manufacturer's data sheets on each product to be used.

      - Preparation instructions and recommendations.

      - Storage and handling requirements and recommendations.

      - Typical installation methods.

    - Shop Drawings: Indicate profiles, sizes, connection attachments, reinforcing, anchorage, size and type of fasteners, and accessories.

      - Indicate welded connections using standard AWS A2.4 welding symbols. Indicate net weld lengths.

    - Welders' Certificates.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.

    - Structural Designer Qualifications: Professional Structural Engineer experienced in design of this work and licensed in the State in which the Project is located, or personnel under direct supervision of such an engineer.

    - Welder Qualifications: Show certification of welders employed on the Work, verifying AWS qualification within the previous 12 months.

    - Fabricator Qualifications: A qualified steel fabricator that is accredited by the International Accreditation Service (IAS) Fabricator Inspection Program for Structural Steel (AC172).

    - Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

** NOTE TO SPECIFIER ** Include mock-up if the project size or quality warrant the expense. The following is one example of how a mock-up on might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project.

    - Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - Intent of mock-up is to demonstrate quality of workmanship and visual appearance.

      - If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Store and handle in strict compliance with manufacturer's written instructions and recommendations.

    - Protect from damage due to weather, excessive temperature, and construction operations.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - WARRANTY

    - Manufacturer's standard limited warranty unless indicated otherwise.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: Panel Built Inc., which is located at:<BR />302 Beasley St., P. O. Box 2658    <BR />Blairsville, GA 30514<BR />Toll Free Tel: 800-636-3873 <BR />Tel: 706-745-6540 <BR />Fax: 800-594-3245 <BR />Email: request info (info@panelbuilt.com);Web: https://www.panelbuilt.com

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

  - PERFORMANCE AND DESIGN REQUIREMENTS

    - Delegated Design: Engage a qualified professional engineer, as defined in Section 01 40 00 - Quality Requirements "Quality Requirements," to design the following:

      - Metal stairs.

      - Metal ladders.

      - Railings and guard rails.

    - Structural Performance for Railings and Guard Rails: Including attachment to building construction, withstanding the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

      - Handrails and Guard Top Rails:

        - Uniform Load: 50 lbf/ft (0.73 kN/m) in any direction.

        - Concentrated Load: 200 lbf (0.89 kN) in any direction.

        - Uniform and Concentrated Loads: Need not be assumed to act concurrently.

      - Guard Infill:

        - Concentrated Load: 50 lbf (0.22 kN) applied horizontally on area of 1 sq ft (0.093 sq m).

        - Infill and Other Loads: Need not be assumed to act concurrently.

    - Provide items, of design specified, complete with landing platforms, vertical and horizontal supports, railings, and guards, fabricated accurately for anchorage to each other and to building structure.

      - Regulatory Requirements: Complying with the most stringent requirements of local, state, and federal regulations; where requirements of the contract documents exceed those of regulations, comply with the contract documents.

      - Dimensions: As indicated on drawings.

      - Shop assemble components; disassemble into largest practical sections suitable for transport and access to site.

      - No sharp or rough areas on exposed travel surfaces and surfaces accessible to touch.

      - Separate dissimilar metals using paint or permanent tape.

    - Metal Jointing and Finish Quality Levels:

      - Architectural: All joints as inconspicuous as possible, whether welded or mechanical.

        - Welded Joints: Continuously welded and ground smooth and flush.

        - Mechanical Joints: Butted tight, flush, and hairline; concealed fastenings only.

        - Exposed Edges and Corners: Eased to small uniform radius.

      - Industrial: All joints made neatly.

        - Welded Joints: Welded on back side wherever possible.

        - Welds Exposed to Touch: Ground smooth.

        - Bolts Exposed to Touch in Travel Area: No nuts or screw threads exposed to touch.

    - Fasteners: Same material or compatible with materials being fastened; type consistent with design and specified quality level.

    - Anchors and Related Components: Same material and finish as item to be anchored, except where specifically indicated otherwise; provide all anchors and fasteners required.

** NOTE TO SPECIFIER ** Delete article not required or delete stair tread paragraphs not required.

  - METAIL STAIRS

    - Metal Stairs with Concrete Treads:

      - Jointing and Finish Quality Level: Industrial.

** NOTE TO SPECIFIER ** Delete risers, treads, and tread attachments options not required.

      - Risers: Closed.

      - Risers: Open.

      - Treads: Abrasive-Surface Metal Floor Plate: Abrasive materials adhered to surface.

      - Treads: Abrasive-Surface Metal Floor Plate: Abrasive materials metallically bonded to steel.

      - Treads: Checkered steel tread plate.

      - Tread Attachments: Bolted.

      - Tread Attachments: Welded.

      - Nosing: Galvanized checkered plate.

      - Nosing Width: 1-1/4 inch (31 mm), minimum.

      - Stringers: Rolled steel channels.

        - Stringer Depth: 1O inches (250 mm).

        - End Closure: Sheet steel of same thickness as risers welded across ends.

      - Railings: Galvanized steel pipe and tube railings.

    - Metal Stairs with Concrete Treads:

      - Jointing and Finish Quality Level: Industrial.

      - Risers: Closed.

      - Treads: Metal pan with field-installed concrete fill.

        - Concrete Depth: 1-1/2 inches (38 mm), minimum.

        - Tread Pan Material: Steel sheet.

        - Tread Pan Thickness: As required by design; 14 gage, 0.075 inch (1.9 mm) minimum.

        - Concrete Reinforcement: None.

        - Concrete Finish: For resilient floor covering.

      - Risers: Same material and thickness as tread pans.

        - Nosing Depth: Not more than 1-1/2 inch (38 mm) overhang.

        - Nosing Return: Flush with top of concrete fill, not more than 1/2 inch (12 mm) wide.

      - Stringers: Galvanized rolled steel channels.

        - Stringer Depth: 1O inches (250 mm).

        - End Closure: Sheet steel of same thickness as risers welded across ends.

      - Railings: Galvanized steel pipe and tube railings.

    - Metal Stairs with Grating Treads:

      - Jointing and Finish Quality Level: Industrial.

      - Risers: Open.

      - Treads: Galvanized steel bar grating.

        - Grating Type: Welded.

        - Bearing Bar Depth: 3/4 inch (19 mm), minimum.

        - Top Surface: Standard.

        - Nosing: Galvanized checkered plate.

        - Nosing Width: 1-1/4 inch (31 mm), minimum.

        - Anchorage to Stringers: End plates welded to grating, bolted to stringers.

      - Stringers: Rolled steel channels.

        - Stringer Depth: 1O inches (250 mm).

        - End Closure: Sheet steel of same thickness as risers welded across ends.

      - Railings: Galvanized steel pipe and tube railings.

    - Prefabricated Egress Stairs: Welded steel unit, factory fabricated to greatest degree practical and in the largest components possible.

  - HANDRAILS AND RAIL GUARDS

    - Railing Materials:

      - Tubing: [ASTM A500/A500M (cold formed)] [or] [ASTM A513/A513M, Type 5].

      - Pipe: ASTM A53/A53M, Type F or Type S, Grade A, Standard Weight (Schedule 40), unless another grade and weight are required by structural loads.

** NOTE TO SPECIFIER ** Delete if not required. Or delete Metal options not required.

    - Infill Guard Panels:

      - Expanded Metal: ASTM F1267

** NOTE TO SPECIFIER ** Delete type and style designations options not required.

        - Type I expanded. Class 1 uncoated.

        - Type II expanded and flattened. Class 1 uncoated.

        - Style Designation: 3/4 number 13

        - Style Designation: 1-1/2 number 10

        - Style Designation: ________.

      - Perforated-Metal:

        - Cold-Rolled Steel Sheet: ASTM A1008/A1008M commercial steel, Type B.

** NOTE TO SPECIFIER ** Delete thickness and perforations options not required.

          - Thickness: 0.060 inch (1.52 mm)

          - Thickness: ___ inch( ___ mm)

          - Perforations: 1/4 inch (6.4 mm) holes 3/8 inch (9.5 mm) on center in staggered rows.

          - Perforations: ________.

        - Hot-Rolled Steel Sheet: ASTM A1011/A1011M commercial steel, Type B.

** NOTE TO SPECIFIER ** Delete thickness and perforations options not required.

          - Thickness: 0.060 inch (1.52 mm)

          - Thickness: ___ inch( ___ mm)

          - Perforations: 1/4 inch (6.4 mm) holes 3/8 inch (9.5 mm) on center in staggered rows.

          - Perforations: ________.

        - Galvanized-Steel Sheet: ASTM A653/A653M, G90 (Z275) coating, commercial steel Type B,

** NOTE TO SPECIFIER ** Delete thickness and perforations options not required.

          - Thickness: 0.064 inch (1.63 mm)

          - Thickness: ___ inch( ___ mm)

          - Perforations: 1/4 inch (6.4 mm) holes 3/8 inch (9.5 mm) on center in staggered rows.

          - Perforations: 1/8 x 1 inch (3.2 x 25.4 mm) round end slotted holes in staggered rows.

          - Perforations: ________.

      - Woven-Wire Mesh Infill Panels: Intermediate-crimp. 0.134 inch (3.42 mm) diameter steel wire complying with ASTM A510.

** NOTE TO SPECIFIER ** Delete panel option not required.

        - Pattern: Diamond 2 inch (50 mm) woven-wire mesh.

        - Pattern: Square 2 inch (50 mm) woven-wire mesh.

    - Fasteners:

      - Anchor Railings to Other Construction: Fasteners types, grades, and classes needed to produce connections and withstand design loads.

      - Interconnecting Railings:

** NOTE TO SPECIFIER ** Delete one of the two options below.

        - Concealed fasteners unless otherwise indicated.

        - Concealed fasteners unless exposed fasteners are unavoidable.

    - Post-Installed Anchors: Working capacity greater than or equal to design load, according to evaluation report acceptable to authorities having jurisdiction, based on:

      - ICC-ES AC193: Mechanical anchors.

      - ICC-ES AC308: Adhesive anchors.

      - Material for Interior Locations: Carbon-steel components zinc-plated to comply with ASTM B633 or ASTM F1941/F1941M, Class Fe/Zn 5, unless otherwise indicated.

  - METAL LADDERS

** NOTE TO SPECIFIER ** ANSI A14.3 specifies minimum design requirements for ladders.

    - Comply with ANSI A14.3.

** NOTE TO SPECIFIER ** Delete if not required.

      - For Elevator Pit Ladders: ASME A17.1

    - Steel Ladders:

** NOTE TO SPECIFIER ** Delete siderail spacing option not required.

      - Siderail Spacing: ___inches (___ mm)

      - Siderail Spacing: As indicated on Drawings.

      - Siderail Spacing: To be determined by the Architect.

** NOTE TO SPECIFIER ** Delete continuous siderails if not required.

      - Continuous Siderails: ___ x ___ inch (___ x ___ mm).

        - Steel flat bars, with eased edges.

      - Rungs: Fit in centerline of siderails, Plug-weld and grind smooth on outer rail faces.

      - Rung Size: ___ inch (___ mm).

** NOTE TO SPECIFIER ** Delete rung shape option not required.

      - Rung Shape: Round steel bars.

      - Rung Shape: Square steel bars.

      - Nonslip Surfaces: On top of each rung from single manufacturer.

        - Aluminum-oxide granules in epoxy-resin adhesive.

        - Manufactured rung filled with aluminum-oxide grout.

      - Coating with abrasive material metallically bonded to rung.

      - Platforms: Fabricate from welded or pressure-locked steel bar grating, supported by steel angles.

** NOTE TO SPECIFIER ** Delete grate openings option not required.

        - Grate Openings: 1/2 inch (12 mm) in least dimension.

        - Grate Openings: 3/4 inch (19 mm) in least dimension.

      - Ladder Support: At top and bottom and not more than 60 inches (1500 mm) on center with bolted steel brackets.

      - Ladder Finish: Galvanize and prime ladders, including brackets.

        - Prime Ladders: Brackets and fasteners, with zinc-rich primer.

  - MATERIALS

    - Metal Surfaces: Smooth and flat unless otherwise specified.

      - Fabrications Exposed to View: Materials without seam marks, roller marks, rolled trade names, or blemishes.

    - Steel Sections: ASTM A 36/A 36M.

    - Checkered Plate: ASTM A786/A786M, rolled steel floor plate; pattern no. 2.

    - Gratings: Bar gratings complying with NAAMM MBG 531 or NAAMM MBG 532, whichever applies based on bar sizes.

    - Steel Bolts, Nuts, and Washers: ASTM A325 (ASTM A325M), Type 1, and galvanized to ASTM A153/A153M where connecting galvanized components.

    - Welding Materials: AWS D1.1; type required for materials being welded.

    - Stairs - Interior and exterior to be galvanized.

  - SHOP FINISHING

    - Clean surfaces of rust, scale, grease, and foreign matter prior to finishing.

    - Do not prime surfaces in direct contact with concrete or where field welding is required.

    - High-Performance Coating: Apply epoxy topcoats to prime-coated surfaces per manufacturer's written instructions and with requirements in SSPC-PA 1 for shop painting.

      - Apply at spreading rates recommended by coating manufacturer.

        - Colors: ________

        - Colors: As selected by Architect from manufacturer's full range.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed and prepared.

    - If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

      - When field welding is required, clean and strip primed steel items to bare metal.

    - Supply items required to be cast into concrete and embedded in masonry with setting templates.

  - INSTALLATION

    - Install in accordance with manufacturer's instructions, approved submittals, and in proper relationship with adjacent construction.

      - Install components plumb and level, accurately fitted, free from distortion or defects.

      - Allow for erection loads, and for sufficient temporary bracing to maintain true alignment until completion of erection and installation of permanent attachments.

      - Provide welded field joints where specifically indicated on drawings. Perform field welding in accordance with AWS D1.1.

      - Other field joints may be either welded or bolted provided the result complies with the limitations specified for jointing quality levels.

      - Obtain approval prior to site cutting or creating adjustments not scheduled.

      - After erection, prime welds, abrasions, and surfaces not shop primed or galvanized, except surfaces to be in contact with concrete.

    - Tolerances:

      - Maximum Variation from Plumb: 1/4 inch (6 mm) per story, non-cumulative.

      - Maximum Offset from True Alignment: 1/4 inch (6 mm).

  - FIELD QUALITY CONTROL

    - Field Inspection: Coordinate field inspection in accordance with appropriate sections in Division 01.

** NOTE TO SPECIFIER ** Include if manufacturer provides field quality control with onsite personnel for instruction or supervision of product installation, application, erection, or construction. Delete if not required.

    - Manufacturer's Services: Coordinate manufacturer's services in accordance with appropriate sections in Division 01.

  - CLEANING AND PROTECTION

    - Clean products in accordance with the manufacturers recommendations.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION